FURNITURE MACHINE OPERATOR

PM01 OPERATE A RANGE OF MACHINES IN THE WOOD MACHINE SHOP TO CUT COMPONENTS FOR FURNITURE MANUFACTURING

FACILITATOR GUIDE

Table of Contents

PM-01	3

PM-01-PS01: Identify and Categorise Typical Wooden Furniture Products and Accessories	4

PA0101 – Identify and Categorise the Product According to Types, Uses and Styles	6

PA0102 – Identify and Categorise the Products According to the Raw Materials Used in the Manufacturing Process	9

PA0103 – Identify and Categorise the Accessories According to the Uses and Furniture Design	12

Applied Knowledge	15

AK0101 – Furniture Types, Uses, Styles and Designs	15

Integrated Assessment Task	18

Facilitator Assessment Briefing	21

PM-01-PS02: Identify Timber and Board Used in the Manufacturing of Wooden Furniture	23

PA0201 – Identify Types of Solid Wood (Soft and Hard Wood)	25

PA0202 – Identify Types of Composite Boards (Supa Wood, Chipboard, Melamine, Veneer Board, Ply Board, Hardboard)	28

PA0203 – Inspect Wood and Boards for Defects and Defaults Visually	31

PA0204 – Use a Metal Detector to Inspect Reclaimed Wood	34

PA0205 – Use a Moisture Meter to Determine the Moisture Content of the Wood	37

PA0206 – Identify Standard Sizes According to the Product to be Manufactured in Order to Reduce Waste	40

PA0207 – Handle and Store Raw Material Such as Lifting or Pallet Jacks in a Safe Manner	42

PA0208 – Identify and Interpret the Labelling and Coding System Used to Identify and Trace Raw Material and Products	44

Applied Knowledge	47

AK0201 – Timber and Board Characteristics and Quality	49

AK0202 – Stacking Requirements and Techniques	52

Integrated Assessment Task	54

Facilitator Assessment Briefing	58

PM-01-PS03: Identify Consumables and Accessories Used in Furniture Manufacturing	60

PA0301 – Identify Consumables According to Uses	62

PA0302 – Identify Accessories Matched to Specific Uses and Furniture Styles	65

PA0303 – Inspect Consumables and Accessories for Faults and Defects	68

PA0304 – Handle and Store Chemicals According to Safety Requirements and to Prolong Product Lifetime	71

PA0305 – Identify Standard Sizes	74

PA0306 – Handle and Store Consumables Safely and According to Requirements	77

Applied Knowledge	80

AK0301 – Types of Consumables, Accessories, Their Use and Characteristics	80

Integrated Assessment Task	83

Facilitator Assessment Briefing	87

PM-01-PS04: Identify a Range of Machines, Machine Parts, Machine Attachments and Tools in the Furniture Machine Shop	89

PA0401 – Identify the Machines, Parts, Attachments and Tools Used in the Break-out Operation	91

PA0402 – Identify the Machines, Parts, Attachments and Tools Used in the Planing Operation	94

PA0403 – Identify the Machines, Parts, Attachments and Tools Used in the Sanding Operation	97

PA0404 – Identify the Machines, Parts, Attachments and Tools Used in the Laminating Operation	100

PA0405 – Identify the Safety Mechanisms Applicable to Various Machines	103

PA0406 – Identify the Control Systems for Operating the Machine	106

PA0407 – Identify and Explain Different Colour Coding Used on the Machines	109

PA0408 – Identify the Pneumatic Machines and the Required Pressures	112

Applied Knowledge	115

AK0401 – Machines in the Wood Workshop	117

AK0402 – Meaning of Signals, Switches, Alarms, Guides and Gauges	120

AK0403 – Safety When Using Machines, Equipment and Tools	124

# PM-01

Title: Operate a Range of Machines in the Wood Machine Shop to Cut Components for Furniture Manufacturing
NQF Level: 2 Credits: 20

1. Introduction to the Practical Module

This Practical Module introduces the learner to foundational machining operations within the furniture manufacturing environment. It equips the learner with hands-on skills to prepare, set up and operate various woodworking machines, hand tools, power tools and pneumatic tools used in the production of timber or board-based furniture components. The module forms a critical part of the learner’s journey toward becoming a competent Furniture Maker, by laying the groundwork for accurate, safe and efficient component production in alignment with industrial standards.

The learner will acquire operational competence in using cross-cut saws, rip saws, planers, sanders, and pneumatic tools, among others. The training focuses on safety, accuracy, quality, and proper handling of materials in the machining department. Learners will be introduced to routine cleaning and maintenance of machines as part of instilling a responsible work ethic and an understanding of production efficiency and quality assurance.

By the end of this module, learners will be expected to demonstrate their ability to interpret component specifications, conduct machine setup, apply safe machining techniques, and produce components that meet quality and dimensional specifications. The development of these skills is essential for successful participation in more advanced machining, assembling and finishing operations as learners progress in the qualification.

2. Purpose of the Practical Skill Module

The purpose of PM-01 is to provide learners with practical exposure to wood machining operations, thereby enabling them to:

- Understand the function and application of woodworking machinery, tools and materials.

- Identify and handle materials appropriately.

- Apply health and safety practices within a machining environment.

- Produce components that comply with specified tolerances and quality requirements.

- Perform maintenance and housekeeping activities necessary for sustainable machine operations.

## PM-01-PS01: Identify and Categorise Typical Wooden Furniture Products and Accessories

1. Introduction to the Practical Skill

This learning session introduces the learner to the diverse world of wooden furniture products and the accessories used in their construction and design. An understanding of furniture categories, uses, and stylistic classifications forms the foundation for all downstream activities in furniture manufacturing. It also develops the learner’s capacity to interpret design specifications and select appropriate materials and components in the machining and assembly processes.

The identification and categorisation of furniture are not only about recognising an item visually; it requires learners to consider the product’s functional role, design context, and the materials from which it is made. By examining physical samples, photographs or catalogue images, learners will develop the ability to differentiate between classic, modern, and contemporary styles, and classify items such as tables, chairs, desks, and cabinets based on intended use and construction approach.

In addition to furniture products, the learner will explore various accessories, including handles, hinges, drawer runners, fasteners, and decorative elements. These are to be understood not only in isolation but also in terms of how they complement the overall furniture design and purpose. The knowledge gained in this session is essential for future modules focused on machining, assembling, and finishing operations, where material choice and accessory application significantly influence manufacturing outcomes.

2. Scope of Practical Skill

Given a range of samples or images of different wooden furniture products and accessories, the learner must be able to:

- PA0101 Identify and categorise the product according to types, uses and styles.

- PA0102 Identify and categorise the products according to the raw materials used in the manufacturing process.

- PA0103 Identify and categorise the accessories according to their uses and relevance to furniture design.

3. Applied Knowledge (AK0101)

- Furniture types, uses, styles and designs.

4. Internal Assessment Criteria

- IAC0101 Furniture products are accurately identified according to the various categories.

- IAC0102 Accessories identified are relevant to the specified use in the furniture manufacturing process.

### PA0101 – Identify and Categorise the Product According to Types, Uses and Styles

Facilitator Purpose

The purpose of this session is to enable learners to correctly identify and categorise a range of wooden furniture products by examining their type (what it is), use (what it is for), and style (how it looks/design era). The facilitator should encourage active learner engagement by using images, sample furniture items, and catalogues, while facilitating discussions that highlight how form follows function and style aligns with customer preferences or historical trends.

Key Concepts to Cover

- Types of Wooden Furniture Products

  - Tables (e.g. dining tables, coffee tables, side tables)

  - Chairs (e.g. dining chairs, armchairs, office chairs)

  - Storage (e.g. cupboards, chests of drawers, wardrobes)

  - Surfaces and worktops (e.g. kitchen counters, office desks)

  - Beds and bedroom suites

  - Children’s furniture

  - Office furniture

  - Built-in units (e.g. shelving, fitted wardrobes)

- Uses of Furniture

  - Residential: Used in homes (e.g. bedroom, lounge, dining)

  - Commercial: Used in offices, restaurants, or hotels

  - Special-purpose: School desks, laboratory tables

  - Outdoor: Garden benches, patio furniture

- Styles and Design Movements

  - Traditional: Ornate carving, rich wood finishes (e.g. Victorian, Colonial)

  - Modern: Sleek lines, functional (e.g. Scandinavian, Bauhaus)

  - Contemporary: Current design trends, often minimalist

  - Rustic: Natural wood, rugged finishes

  - Industrial: Metal + wood fusion, exposed joints

  - Eclectic: A mix of styles and influences

Facilitator Tip: Demonstration Method

Bring in photos, actual mini furniture pieces, or catalogues. Use a projector or flipchart to classify them under "Type", "Use", and "Style" columns. Encourage learners to take part in matching exercises and group discussions.

Practical Examples

| Product | Type | Use | Style |
| --- | --- | --- | --- |
| Oak dining table | Table | Residential | Traditional |
| Plywood stacking chair | Chair | Commercial | Modern |
| Pine TV unit | Storage | Residential | Rustic |
| MDF study desk | Desk | Educational | Contemporary |
| Garden bench (slatted) | Seating | Outdoor | Industrial |

Case Study: Makhanda School Furniture Project

The Eastern Cape Department of Education commissioned a local furniture maker to produce school desks and teacher tables for rural classrooms in Makhanda. The products had to be cost-effective, durable, and suitable for learners aged 7 to 12.

Learners are asked to examine images of the final products, identify the furniture type (e.g. single-seater desk), determine the use (education – classroom seating and writing), and describe the style (basic, functional, safety-oriented with rounded edges). The case shows how local demand shapes both the design and classification of furniture.

Critical Thinking Questions

- Why is it important for a furniture maker to understand both the use and style of a product when beginning the machining process?

- How would the classification of furniture change if the same item was used in a different context (e.g. a dining chair in an office)?

- What challenges might arise if the furniture type is misidentified before manufacturing begins?

- Can a single piece of furniture belong to more than one style? Give an example.

- In your own home or community, identify three furniture items and classify them according to type, use and style.

### PA0102 – Identify and Categorise the Products According to the Raw Materials Used in the Manufacturing Process

Facilitator Purpose

This session enables learners to recognise and categorise wooden furniture products based on the raw materials used in their manufacture. Learners will be introduced to a range of common raw materials such as solid wood, composite boards, and decorative finishes, as well as how material choice influences durability, aesthetics, cost, and function.

Facilitators should aim to cultivate an appreciation for material selection as a critical part of the design and production process, especially in the context of South Africa’s furniture industry where cost and resource efficiency are important.

Key Concepts to Cover

- Types of Raw Materials in Furniture Manufacturing

  - Solid Wood (Timber)

    - Indigenous (e.g. Kiaat, Yellowwood, Stinkwood)

    - Exotic/Imported (e.g. Oak, Mahogany, Beech)

  - Engineered Wood / Boards

    - Medium-Density Fibreboard (MDF)

    - Chipboard / Particle board

    - Plywood

    - Hardboard

    - Blockboard

  - Laminates and Veneers

    - Plastic laminates (e.g. Formica)

    - Wood veneer sheets

  - Glass, Metal and Plastic Accents

    - Used in modern/contemporary or hybrid furniture designs

  - Eco-materials and Reclaimed Wood

    - Sustainable or recycled materials

- Properties of Materials

  - Durability, moisture resistance, cost, ease of machining, surface finish potential

  - Suitability for indoor/outdoor use

  - Impact on style and design (e.g. visible grain in timber vs. smooth paintable board)

Facilitator Tip: Interactive Materials Table

Set up a tactile station with labelled samples of solid wood, MDF, plywood, chipboard, and veneer. Allow learners to feel the textures, compare weights, and observe finishes. Use a chart to help them record their observations under:

- Material Name

- Common Use

- Advantages/Disadvantages

- Example Product

Practical Examples

| Furniture Product | Raw Material(s) Used | Notes |
| --- | --- | --- |
| Budget kitchen cupboard | White melamine chipboard | Low cost, smooth finish, easy to clean |
| Designer coffee table | Solid Oak with glass top | Durable, luxurious, high-end furniture |
| Student desk | MDF with PVC edging | Easy to machine, smooth surface for painting or foil |
| Wardrobe | Plywood carcass, veneer | Good balance of strength and cost |
| Garden bench | Reclaimed pine and steel | Eco-friendly, rustic design |

Case Study: Durban Furniture Cooperative

A small manufacturing cooperative in Durban received a government contract to furnish municipal libraries. Their challenge was to produce durable reading tables and computer stations within budget. They opted to use laminated chipboard for carcasses and hardwood trim for high-wear areas like table edges.

Learners are asked to evaluate whether the cooperative made an appropriate choice of materials, considering usage environment, cost constraints, and user traffic in a public space.

Critical Thinking Questions

- What are the advantages and disadvantages of using chipboard versus solid wood in furniture production?

- Which raw material would you recommend for furniture in a coastal area and why?

- In what types of furniture products would you most likely find veneer finishes?

- How does the selection of raw material impact the overall cost of the final product?

- Why is it important for a furniture maker to understand how different raw materials behave during machining processes?

### PA0103 – Identify and Categorise the Accessories According to the Uses and Furniture Design

Facilitator Purpose

This session focuses on developing the learner's ability to identify, classify, and explain the purpose of various furniture accessories, and how they contribute to the functionality, appearance, and style of furniture products. Accessories include mechanical fittings (like hinges and runners), decorative elements (like handles and trims), and structural reinforcements.

Learners will gain insights into selecting appropriate accessories for different types of furniture and design styles, with emphasis on usability, aesthetic value, durability, and end-user comfort.

Key Concepts to Cover

- Types of Furniture Accessories

  - Functional Accessories

    - Hinges (butt hinge, concealed hinge, piano hinge)

    - Drawer runners (roller runners, ball bearing slides, push-to-open mechanisms)

    - Connectors and fasteners (screws, cam locks, dowels, brackets)

  - Decorative Accessories

    - Handles, knobs, trims

    - Legs, castors, and feet

    - Edging strips (PVC, veneer edging)

  - Support Accessories

    - Corner blocks, shelf pegs, support braces

    - Pneumatic lift mechanisms (e.g. gas-lift in office chairs)

- Categorisation by Use

  - Opening/closing (e.g. hinges, slides)

  - Supporting weight or movement (e.g. legs, castors)

  - Providing access or grip (e.g. handles, knobs)

  - Decorative enhancement (e.g. trims, scrollwork)

  - Mechanical or adjustable functions (e.g. height adjustment)

- Categorisation by Design Context

  - Modern: Sleek stainless steel handles, soft-close runners, invisible fixings

  - Traditional: Brass knobs, ornate hinges, decorative inlays

  - Rustic: Forged iron handles, exposed brackets, rough edge trims

  - Office furniture: Ergonomic castors, lockable drawers, cable management grommets

Facilitator Tip: Hands-on Demonstration

Bring a "furniture accessory kit" to class with physical examples of handles, hinges, runners, screws, and fasteners. Group learners to explore and identify each accessory. Ask them to link the accessory to:

- A furniture item they have seen or used

- Its function

- The type of design it would suit

Create a classification chart or wall display for ongoing reference.

Practical Examples

| Accessory | Use | Furniture Design Context |
| --- | --- | --- |
| Ball-bearing runners | Smooth drawer movement | Modern kitchen cabinets |
| Brass pull handle | Grip and decorative feature | Traditional chest of drawers |
| PVC edging strip | Seals and finishes cut edges | Office desks |
| Castors | Mobility | Mobile pedestal or filing cabinet |
| Gas-lift cylinder | Height adjustment | Executive office chair |

Case Study: Alexandra Youth Workshop

A group of youth in Alexandra Township received training to manufacture small bedroom units for low-income housing projects. Their challenge was to design cupboards and bedside pedestals that were aesthetically appealing, easy to use, and cost-effective. Given budget constraints, they opted for plastic handles, basic butt hinges, and roller drawer runners.

Learners should evaluate the decisions made:

- Were the chosen accessories appropriate for the target market?

- How would upgrading to concealed hinges or soft-close runners affect the usability and appeal of the furniture?

- What would be the impact on production cost and complexity?

Critical Thinking Questions

- What is the risk of selecting accessories that do not match the intended use of the furniture?

- How does the choice of accessory impact the final cost and perceived quality of a furniture product?

- Can the same accessory be used across multiple styles of furniture? Provide examples.

- What types of accessories would you recommend for a child’s bedroom set? Justify your choices.

- Which accessories would you avoid in humid or coastal environments, and why?

## Applied Knowledge

### AK0101 – Furniture Types, Uses, Styles and Designs

Facilitator Purpose

The aim of this session is to build the learner’s foundational knowledge of how furniture is classified in terms of its type (what it is), use (where and how it is used), and style and design (how it looks and is constructed). This applied knowledge underpins the learner’s ability to make informed decisions during machining, assembling, and finishing tasks. The facilitator should guide learners to recognise how cultural preferences, technological advancement, and design movements influence furniture-making today.

This knowledge is essential for interpreting design briefs, selecting appropriate raw materials, choosing fittings and accessories, and ensuring the final product meets both practical and aesthetic expectations.

1. Types of Furniture

Facilitators should introduce learners to the broad categories of furniture, often grouped by function or room placement:

- Seating: chairs, sofas, benches, stools

- Tables: dining tables, coffee tables, bedside tables, desks

- Storage: wardrobes, cabinets, drawers, bookshelves

- Beds: bunk beds, platform beds, sleigh beds

- Workstations: office desks, counters, school furniture

- Built-in units: kitchen cabinetry, TV units, shelving systems

🛈 Tip: Use printed flashcards or a projected image slideshow to show visual representations of each type.

2. Uses of Furniture

Furniture is typically classified by end-use environment:

- Residential: Living room suites, bedroom furniture, dining sets

- Commercial: Office desks, boardroom tables, reception units

- Hospitality: Hotel headboards, bar counters, restaurant chairs

- Educational: School desks, library shelving, science lab benches

- Retail: Display cabinets, checkout counters, product shelves

- Outdoor: Patio chairs, picnic benches, pergolas

Encourage learners to identify the use of furniture pieces they have seen at home, school, clinics, malls or offices.

3. Furniture Styles

Styles describe the visual and design characteristics of a piece of furniture, often tied to specific eras or philosophies. Discuss the following key styles with examples:

| Style | Description | Visual Traits |
| --- | --- | --- |
| Traditional | Inspired by classical European or African motifs | Rich wood finishes, ornate carvings |
| Modern | 20th-century clean-line movement | Geometric forms, minimal ornamentation |
| Contemporary | Present-day trends | Soft curves, functional simplicity |
| Rustic | Country or farm-style appearance | Raw edges, visible grain, thick timbers |
| Industrial | Urban factory aesthetic | Exposed metal, bolts, reclaimed wood |
| Eclectic | Blend of various styles | Contrasting elements, creative expression |

🛈 South African Context: Encourage learners to explore styles influenced by local artisanship (e.g. Zulu carving motifs, Cape Dutch cabinetry, or recycled pallet furniture trends).

4. Design Considerations

Furniture design goes beyond appearance. Facilitate discussions on:

- Functionality: Does it serve the intended purpose?

- Ergonomics: Is it comfortable and user-friendly?

- Aesthetics: Does it look appealing or suit the space?

- Materials: Are the materials appropriate for style and use?

- Sustainability: Are environmentally friendly materials used?

Facilitator Activity Suggestion

Design Board Group Exercise: Divide learners into groups and provide each with:

- A furniture type (e.g. dining chair)

- A style (e.g. modern)

- A use context (e.g. café)

Each group must sketch, label, and describe their ideal furniture piece on a poster or board and present to class. This enhances their understanding of how type, use, and style intersect.

Case Study: Office Furniture Upgrade – Eastern Cape Department of Education

A procurement tender for new office furniture required products that are ergonomic, durable, and in line with modern design trends. The winning supplier used L-shaped particle board desks with PVC edging, ergonomic mesh-back chairs, and minimalist cable-managed pedestals.

Learners are asked to:

- Classify each item by type, use, and style

- Explain why these design decisions suit a public sector office

- Propose alternatives for an NGO or a creative agency

Critical Thinking Questions

- How does the intended use of furniture influence its design and material selection?

- Why is it important for a furniture maker to recognise different styles of furniture?

- Which style do you believe is most in demand in South African homes today, and why?

- Can a piece of furniture fall under more than one category (type/style)? Provide an example.

- How do trends in fashion, architecture, or media influence furniture design choices?

## Integrated Assessment Task

Practical Module: PM-01 – Operate a Range of Machines in the Wood Machine Shop to Cut Components for Furniture Manufacturing
Sub-task: PM-01-PS01: Identify and Categorise Typical Wooden Furniture Products and Accessories
NQF Level: 2 Credits: 20
Assessment Type: Integrated Practical Knowledge Assessment
Duration: 1 hour
Assessment Format: Case Study with Structured Questions

Case Study: “Furniture for the Future” Youth Co-operative

A youth co-operative based in George, Western Cape, received funding from a local development agency to produce multi-purpose furniture for small apartments. Their first product line includes:

- A modular coffee table that converts into a dining table.

- A wall-mounted folding desk designed for remote workers.

- A compact storage bench that doubles as hallway seating.

- A basic nightstand with one drawer and a shelf.

Each item is made from a combination of MDF, solid pine, and melamine-coated chipboard, and is fitted with modern accessories such as concealed hinges, full-extension ball-bearing runners, aluminium handles, and rubber bumpers for doors.

The learners are asked to assist with cataloguing the furniture products and checking the accessory selection for suitability.

Assessment Questions

Question 1
Refer to the case study. Identify and categorise each furniture item according to:
a) Furniture type
b) Use
c) Style

Question 2
For each item, list the accessory mentioned in the case study and explain whether it is suitable for its intended use and furniture design.

Model Answers

Question 1: Categorisation of Furniture Products

| Product | Type | Use | Style |
| --- | --- | --- | --- |
| Modular coffee/dining table | Table | Residential – dual use | Contemporary |
| Folding wall-mounted desk | Desk | Home office/remote use | Minimalist/Modern |
| Compact storage bench | Seating + Storage | Entryway furniture | Functional/Rustic |
| Nightstand | Bedside cabinet | Bedroom storage | Simple/Modern |

Question 2: Accessories and Suitability

| Product | Accessory | Suitable? | Reason |
| --- | --- | --- | --- |
| Modular table | Rubber bumpers | Yes | Prevents damage when shifting parts; silent closure. |
| Wall-mounted folding desk | Concealed hinges | Yes | Allows for a clean, flush look when folded up. |
| Storage bench | Aluminium handles | Yes | Durable and modern; suits functional style. |
| Nightstand | Ball-bearing full-extension drawer runners | Yes | Provides full access to the drawer contents; modern style. |

MARKING MEMO

Question 1 – Furniture Categorisation (IAC0101)

- Type identified for all 4 products – 1 mark each = 4 marks

- Use described correctly – 1 mark each = 4 marks

- Style appropriately matched – 1 mark each = 4 marks
Total for Q1: 12 marks

Question 2 – Accessories and Relevance (IAC0102)

- Correct accessory listed – 1 mark each = 4 marks

- Suitability explained and justified – 2 marks each = 8 marks
Total for Q2: 12 marks

Total Marks Available: 24 Marks

Assessment Rubric

| Criteria | Outstanding (4) | Competent (3) | Developing (2) | Not Yet Competent (1) |
| --- | --- | --- | --- | --- |
| Identification of furniture type, use and style (IAC0101) | All furniture products are accurately classified with clear justifications. | Most furniture products are classified correctly; minor omissions. | Some furniture types or styles are misidentified or unclear. | Unable to categorise or mostly incorrect. |
| Identification and relevance of accessories (IAC0102) | All accessories correctly identified and well explained in relation to use and design. | Most accessories correctly identified; rationale mostly appropriate. | Some inaccuracies in accessory use or reasoning. | Incorrect identification with no reasoning provided. |

### Facilitator Assessment Briefing

Practical Module: PM-01 – Operate a Range of Machines in the Wood Machine Shop to Cut Components for Furniture Manufacturing
Sub-task: PM-01-PS01 – Identify and Categorise Typical Wooden Furniture Products and Accessories
Credits: 20 NQF Level: 2
Internal Assessment Criteria:

- IAC0101 Furniture products are accurately identified according to the various categories

- IAC0102 Accessories identified are relevant to the specified use in the furniture manufacturing process

1. Purpose of the Assessment

This integrated assessment is designed to evaluate the learner’s ability to identify and classify wooden furniture products and their associated accessories in a realistic work scenario. It links theoretical knowledge to practical understanding, while encouraging critical thinking and informed decision-making.

2. Assessment Context

This assessment is based on a case study of a South African youth co-operative designing furniture for compact urban spaces. The context mimics an authentic work situation in which learners are required to evaluate product design, use, material application, and accessory selection.

3. Facilitator Instructions

- Introduce the case study to learners and explain the purpose of the assessment.

- Allow learners time to read and analyse the scenario.

- Learners should answer the structured questions in writing, based on the case study.

- Group discussion may precede the written task, but answers must be completed individually.

- Assess using the provided marking memo and rubric.

- Ensure feedback is provided after the assessment, with corrective guidance where required.

4. Resources Required

- Case study and question paper (provided below)

- Pen and paper or printed worksheets

- Sample catalogue/images (optional, for enrichment)

- Assessment rubric and memo for marking

5. Assessment Duration

- Suggested time: 1 hour

- Can be adapted for classwork or homework depending on the training schedule

## PM-01-PS02: Identify Timber and Board Used in the Manufacturing of Wooden Furniture

1. Introduction to the Practical Skill

This session introduces the learner to the foundational skills and knowledge required to identify, inspect, and correctly handle timber and board materials used in furniture manufacturing. As raw material selection directly influences product quality, durability, and cost-effectiveness, it is essential that learners develop a deep understanding of both solid woods and engineered boards, including their characteristics, uses, and storage requirements.

In this practical task, learners will engage with actual samples of timber and boards (or images where samples are unavailable) to visually and physically inspect material quality, identify types of defects, and use measurement instruments to assess moisture levels and the presence of embedded metal objects. Learners will also be taught how to match material sizes to manufacturing specifications in order to optimise usage and reduce waste. Proper handling techniques, including the use of lifting equipment and adherence to health and safety guidelines, are integral to this learning experience.

Furthermore, learners will become familiar with labelling and coding systems applied to raw materials in a professional manufacturing environment, enabling traceability and quality assurance throughout the production process.

This sub-task develops the learner’s capacity to exercise judgement and care in the selection and management of materials — a core responsibility of any wood machinist or furniture maker.

2. Scope of Practical Skill

Given a range of different types of timber and boards (which may be samples or available in a timber store), the learner must be able to:

- PA0201 Identify types of solid wood (soft and hard wood)

- PA0202 Identify types of composite boards (supa wood, chip board, melamine, veneer board, ply board, hard board)

- PA0203 Inspect wood and boards for defects and defaults visually

- PA0204 Use a metal detector to inspect reclaimed wood

- PA0205 Use a moisture meter to determine the moisture content of the wood

- PA0206 Identify standard sizes according to the product to be manufactured in order to reduce waste

- PA0207 Handle and store raw material such as lifting or pallet jacks in a safe manner in order to prevent injury to self and damage to the material

- PA0208 Identify and interpret the labelling and coding system used to identify and trace raw material and products

3. Applied Knowledge

- AK0201 Timber and board characteristics and quality

- AK0202 Stacking requirements and techniques

4. Internal Assessment Criteria

- IAC0201 Timber and board is correctly identified in terms of type and size and matched to the product specifications

- IAC0202 Raw materials are checked for quality and defects to ensure high quality end products

- IAC0203 Machinery and tools are correctly used to check, handle and store raw materials

### PA0201 – Identify Types of Solid Wood (Soft and Hard Wood)

Facilitator Purpose

The purpose of this session is to equip learners with the ability to correctly identify softwoods and hardwoods commonly used in furniture manufacturing. Learners will explore the visual, tactile, and structural differences between these wood categories, and understand how their unique properties influence machining, joining, finishing, and final product performance.

This knowledge will support informed decision-making when selecting raw materials for specific furniture components, thereby ensuring functionality, quality, and cost-efficiency in production.

Key Concepts to Cover

1. What is Solid Wood?

- Derived directly from felled trees, as opposed to composite or engineered boards.

- Cut into planks or boards and processed for furniture, cabinetry, or structural components.

- Categorised into hardwood and softwood, based on botanical characteristics, not density alone.

2. Hardwoods

- Come from broadleaf, deciduous trees (shed leaves annually)

- Generally denser, more durable, and with more prominent grain patterns

- Often used for high-end or structural furniture parts

Common Hardwoods in South Africa:

| Local Name | Botanical Source | Characteristics | Applications |
| --- | --- | --- | --- |
| Kiaat | Pterocarpus angolensis | Golden-brown, stable, easy to machine | Cabinets, high-end furniture |
| Stinkwood | Ocotea bullata | Dark, fine-grained, valuable | Antiques, traditional furniture |
| Oak | Quercus spp. | Strong, open grain | Tables, chairs, flooring |
| Meranti | Shorea spp. | Reddish, medium-hard, easy to work | Joinery, doors, interior furniture |
| Beech | Fagus sylvatica | Pale, fine grain, good for turning | Children's furniture, bentwood |

3. Softwoods

- Come from coniferous, evergreen trees (retain leaves year-round)

- Lighter and easier to cut, but often less durable

- Suitable for framing, carcasses, budget furniture

Common Softwoods in South Africa:

| Local Name | Botanical Source | Characteristics | Applications |
| --- | --- | --- | --- |
| Pine (SA Pine) | Pinus patula/radiata | Pale yellow, lightweight, easy to nail | Carcasses, bed frames, shelving |
| Spruce | Picea spp. | Soft, white, uniform texture | Musical instruments, drawer sides |
| Cedar | Cedrus spp. | Aromatic, insect-resistant | Chests, wardrobes |

Facilitator Demonstration and Activity Tips

Wood Identification Station:
Prepare a hands-on station with samples of:

- At least 3 hardwoods and 3 softwoods

- Identification tags removed

- Ask learners to classify them based on:

  - Texture

  - Colour and grain

  - Weight and hardness

Learners may record their observations in a comparison chart provided in their learner workbook.

🛈 Optional Enrichment: Include offcuts from reclaimed wood and ask learners to guess whether it is hardwood or softwood and justify their answers.

Case Study: Choosing the Right Wood for a School Desk

A furniture manufacturer receives an order from a school for 200 classroom desks. They must choose between using pine or meranti for the desktop and legs.

Discussion Prompt:

- Which wood would you recommend for the legs and why?

- Which would you choose for the desktop and why?

- Consider: strength, cost, weight, appearance, availability, and machining properties.

Critical Thinking Questions

- What are the advantages and disadvantages of using hardwood in furniture manufacturing?

- Why might a manufacturer choose pine over oak for a student bunk bed?

- Can a hardwood ever be lighter than a softwood? Explain with examples.

- What factors, other than wood type, affect the decision to use solid wood in a product?

- Which wood would you recommend for an outdoor garden bench and why?

### PA0202 – Identify Types of Composite Boards (Supa Wood, Chipboard, Melamine, Veneer Board, Ply Board, Hardboard)

Facilitator Purpose

This session equips learners with the knowledge and skills to accurately identify, compare, and categorise composite board types commonly used in the furniture manufacturing industry. Understanding the unique properties and applications of each board type supports informed material selection, cost-effective production, and high-quality furniture construction.

Learners will explore the composition, strength, surface finish, machinability, and appropriate usage of each type of engineered wood product, building their capacity to align board selection with specific design and manufacturing requirements.

Key Concepts to Cover

1. What are Composite Boards?

Composite or engineered boards are man-made wood products manufactured by binding wood fibres, particles, or veneers with adhesives under pressure. They provide uniform strength, are cost-effective, and are available in large panel sizes ideal for furniture making.

2. Common Types of Composite Boards

| Board Type | Description | Typical Use |
| --- | --- | --- |
| Supa Wood (MDF) | Medium-Density Fibreboard; smooth surface; uniform density | Painted finishes, CNC routing, shaped components |
| Chipboard | Compressed wood particles with rough surface; often requires lamination | Carcasses, internal structures, budget furniture |
| Melamine-faced board | Chipboard or MDF coated with melamine resin film | Kitchen cupboards, wardrobes, desks |
| Veneer board | MDF or chipboard covered with a thin layer of real wood veneer | High-end finishes, cabinet doors |
| Ply board | Multiple thin wood veneers glued in layers with alternating grain direction | Strong panels, shelving, drawer bottoms |
| Hardboard | Very dense fibreboard; smooth one side, textured reverse | Back panels, drawer bottoms, picture frames |

🛈 Note: Supa Wood is a common trade name for high-quality MDF in South Africa.

Facilitator Activity Tips

Board Identification Station
Provide physical samples of the boards listed above. Have learners examine and describe each board using the following characteristics:

- Surface texture

- Edge crumbling or clean cut

- Resistance to bending

- Weight and density

- Reaction to water (where possible to demonstrate)

Learners may complete a Board Comparison Chart noting appearance, feel, strength, and best use.

Discussion Prompt: Ask learners to sort the boards from cheapest to most expensive, and from weakest to strongest.

Case Study: Choosing a Board for Wardrobe Manufacturing

A furniture manufacturer is commissioned to produce 100 budget-friendly wardrobes for a university residence. They must select a material for the internal carcass, the doors, and the back panel.

Class Questions:

- Which board would be suitable for the carcass and why?

- Which board would be used for the doors to allow for a luxury wood look at a lower cost?

- What material would be most appropriate for the back panel of the wardrobe?

Model Discussion Answer:

- Carcass: Melamine-faced chipboard – cost-effective and neat appearance.

- Doors: Veneer board – gives the look of real wood affordably.

- Back panel: Hardboard – inexpensive and light.

Critical Thinking Questions

- What are the advantages of using composite boards over solid wood in mass furniture production?

- Why might a manufacturer choose veneer board over melamine?

- Which board would you avoid in a humid bathroom cabinet, and why?

- How does the surface finish of supa wood (MDF) influence its usage in furniture design?

- What safety considerations should be taken when machining composite boards like MDF and chipboard?

### PA0203 – Inspect Wood and Boards for Defects and Defaults Visually

Facilitator Purpose

The purpose of this session is to enable learners to visually inspect raw timber and composite boards for defects and faults that may compromise the structural integrity, machinability, or appearance of the final furniture product. By developing this skill, learners will be able to make informed decisions regarding material selection, rejection, and optimal use, thereby reducing waste and improving the quality of outputs in the machining department.

Key Concepts to Cover

1. Definition of Defects and Defaults

- Defects: Natural irregularities found in solid wood (due to growth or environmental damage)

- Defaults: Manufacturing faults or physical damage found in processed boards or timber

2. Common Defects in Solid Wood (Natural)

| Defect | Description | Effect on Product |
| --- | --- | --- |
| Knots | Dark circular grain from where branches once grew | Can weaken structure or cause tool damage |
| Splits/Checks | Cracks along or across the grain | May extend during machining |
| Warping | Deformation including bowing, cupping, twisting | Causes misalignment and poor fitting |
| Wane | Missing wood on edge due to bark or irregular trunk | Weakens edge and causes gaps in joints |
| Resin Pockets | Sticky deposits found in coniferous timber | Difficult to finish or paint |
| Decay/Rots | Discolouration and weakening due to fungi or moisture | Unsafe and must be discarded |

3. Common Defaults in Composite Boards (Man-Made)

| Default | Description | Likely Cause |
| --- | --- | --- |
| Delamination | Layers separating in ply or veneer boards | Poor bonding or moisture |
| Edge Crumbling | Weak edge integrity in chipboard | Poor compaction or damage |
| Surface Bubbling/Peeling | Raised or loose laminates or veneer films | Adhesive failure or heat |
| Swelling | Water absorption in unsealed areas | Exposure to moisture |
| Indentations/Scratches | Handling or storage damage | Physical mishandling |

Facilitator Demonstration Tip

Create a Defect and Default Display Board with labelled samples or photos. Encourage learners to:

- Touch and observe real materials where possible

- Use magnifying lenses for fine defects

- Compare “acceptable” and “reject” examples

Practical Activity

Sorting Task:
Provide learners with a mix of timber and board offcuts. In pairs, they:

- Identify and name any defects/defaults

- Recommend whether the material is fit for:

  - Cutting large parts

  - Making small components

  - Scrap/rejection

Each pair justifies their decisions to the class.

Case Study: Rejecting Faulty Material in a Workshop

A furniture apprentice receives a delivery of pine planks and melamine chipboard sheets. On inspection, some pine planks show signs of twist and open knots, while several chipboard sheets have swollen edges and peeling laminate.

Discussion Prompts:

- Which defects are acceptable for hidden parts or cut-down use?

- What safety risks arise from machining defective materials?

- What process should the learner follow to report material faults?

Critical Thinking Questions

- How can early identification of wood defects reduce workshop costs and time delays?

- Which types of defects are acceptable in secondary components (e.g. drawer runners)?

- What is the difference between a natural defect and a processing default?

- What visual signs might suggest moisture damage in composite boards?

- Why is it important to document and trace rejected materials in a formal workplace?

### PA0204 – Use a Metal Detector to Inspect Reclaimed Wood

Facilitator Purpose

This session introduces learners to the correct use of a handheld metal detector to inspect reclaimed or recycled wood before it is machined. The presence of hidden metal objects, such as nails, screws, or staples, poses significant risks to operator safety and can severely damage woodworking machines and tools.

Learners will gain the ability to systematically scan and clear reclaimed timber, understand the limitations of detection, and apply appropriate safety procedures before approving wood for further use.

Key Concepts to Cover

1. Reclaimed Wood in Furniture Manufacturing

- Sourced from old furniture, pallets, demolished buildings, or discarded structural wood

- Popular in rustic, eco-friendly, or cost-reduction furniture designs

- May contain embedded metal from previous use

2. Risks of Hidden Metal in Wood

- Personal Injury: Shards from struck metal can injure the operator

- Machine Damage: Blades, bits and cutting heads may break or become blunt

- Fire Hazard: Sparks from metal contact can ignite wood dust

- Production Delays: Downtime due to equipment damage

3. Types of Metal Objects Commonly Found

- Nails (round-head, brads, finishing)

- Screws

- Staples or tacks

- Wire fencing fragments

- Bolts or steel plates (from frames or bracing)

- Broken drill bits lodged in old timber

4. Metal Detector Usage Procedure

- Prepare a Clear Scanning Area

  - Lay wood flat on a stable surface away from metal tools or benches

- Check the Detector

  - Ensure batteries are full; test detection on known metal object

- Systematically Scan the Wood

  - Move the detector slowly over the entire surface and edges

  - Scan both faces and sides thoroughly

- Mark Detected Areas

  - Use chalk or marker to highlight embedded metal zones

- Remove Detectable Items

  - Extract with pliers, punch tool, or claw hammer as appropriate

- Re-scan to Confirm

  - Re-scan until no further signal is detected

Facilitator Demonstration Tip

Perform a live demonstration using:

- Reclaimed wood with known embedded nails or screws

- A standard handheld wood-metal detector

- A visual aid (flipchart or slide) showing detection zones and scanning paths

Then, supervise learners as they perform a step-by-step scan, followed by removal and verification.

Case Study: Preventing Machine Damage in a Community Workshop

At a community-based workshop in Mpumalanga, an apprentice neglected to scan reclaimed fence planks before using a surface planer. The blade struck a concealed nail, resulting in a damaged cutterhead and a day’s production delay. The incident caused a safety scare and led to the revision of the standard operating procedure.

Discussion Prompts:

- What steps could have prevented the damage?

- What should the workshop include in its material intake process?

- What could be the cost implications of not scanning reclaimed wood?

Critical Thinking Questions

- Why is it especially important to inspect reclaimed wood, as opposed to newly purchased timber?

- Can a metal detector miss smaller or deeply embedded objects? What alternatives exist?

- What safety risks are posed to the operator and other workers when metal goes undetected?

- How can a workshop create a checklist or system to ensure all reclaimed wood is scanned?

- Would you recommend the use of reclaimed wood for furniture exposed to high stress? Why or why not?

### Bottom of Form

### PA0205 – Use a Moisture Meter to Determine the Moisture Content of the Wood

Facilitator Purpose

This session trains learners in the correct use of a moisture meter to determine whether wood is adequately dried for furniture manufacturing. Timber that is too wet or too dry can lead to warping, cracking, joint failure, or poor surface finishing. This task ensures that learners understand how moisture content affects wood performance, and how to apply moisture testing as a preventative quality control step.

Key Concepts to Cover

1. Why Moisture Content Matters

- Timber is a hygroscopic material: it absorbs or releases moisture based on surrounding humidity

- High moisture = shrinkage, warping, glue failure

- Low moisture = brittleness, splitting during machining

- For indoor furniture, the ideal moisture content is typically 8%–12%

2. Types of Moisture Meters

| Type | Description | Common Use |
| --- | --- | --- |
| Pin-type Meter | Uses two metal probes inserted into the wood to measure resistance | Most common and cost-effective |
| Pinless (Capacitive) | Uses electromagnetic waves to scan moisture without puncturing | Non-destructive, useful for veneers |

🛈 Pin-type meters may leave small marks on soft timber — avoid on visible surfaces.

3. Procedure for Using a Pin-type Moisture Meter

- Ensure the meter is calibrated – Follow the manufacturer’s instructions

- Insert the pins into the wood surface – Perpendicular to the grain

- Hold steady until reading appears – Typically in percentage (%)

- Record the reading – Take at least three readings per board (centre and ends)

- Compare results to acceptable moisture range – Refer to furniture specs

Practical Considerations

- Measure in a room with stable humidity, similar to the intended installation environment

- Avoid testing immediately after rain or kiln unloading

- Wood should be acclimatised before machining

Facilitator Demonstration Tip

Demonstrate with:

- A pin-type moisture meter

- Three timber samples at different moisture levels (e.g. freshly sawn, kiln-dried, reclaimed)

- Ask learners to predict and then verify moisture content using the meter

Provide a recording sheet where learners document:

- Wood type

- Reading (%)

- Fit for use (Yes/No)

- Comments

Case Study: Moisture Defect in a Furniture Contract

A small business delivered 50 solid pine tables to a restaurant in Bloemfontein. Within weeks, the table tops began to crack and warp. An inspection revealed the wood had not been dried below 20% moisture before cutting.

Discussion Prompts:

- What quality control step was missed?

- How could the business have prevented product failure?

- What impact would this have on their client relationship?

Critical Thinking Questions

- Why is it necessary to test moisture content even if the timber looks dry?

- What could happen if glue is applied to wood that is too wet?

- How does regional climate affect the ideal moisture content of wood?

- In what situations would a pinless meter be preferred over a pin-type meter?

- What should a wood machinist do if a batch of timber tests above 15% moisture?

### PA0206 – Identify Standard Sizes According to the Product to be Manufactured in Order to Reduce Waste

Facilitator Purpose

This session helps learners understand how to select the most appropriate timber or board sizes for a given product in order to minimise off-cuts, reduce material waste, and lower production costs. The ability to plan cuts efficiently using standard board and timber dimensions is a key competency in any machine shop environment.

Learners will also gain awareness of how product design and component layout influence raw material usage, and how proper sizing supports environmental sustainability and profitability.

Key Concepts to Cover

1. Standard Sizes in Timber and Board Products

| Material Type | Common Standard Sizes (SA context) |
| --- | --- |
| Solid Timber | Supplied in rough sawn or planed forms, variable widths (100–300 mm), lengths (1.8–3.6 m) |
| MDF/Chipboard | Full sheets: 2750 mm x 1830 mm (most common in SA) |
| Plyboard | 2440 mm x 1220 mm (also available in 1830 mm x 1220 mm) |
| Thicknesses | 12 mm, 16 mm, 18 mm, 22 mm, 32 mm (standard furniture grades) |

🛈 Material supply sheets or catalogues from merchants like PG Bison or Sonae can be used in class.

2. Product Planning and Optimisation Principles

- Always align board dimensions with product size and number of components

- Use cutting lists and optimisation software (e.g. CutList Plus, MaxCut) where available

- Consider grain direction, edge banding space, and saw blade kerf (cut thickness)

- Match thickness and finish to product function (e.g. thicker for tops, thinner for backs)

Facilitator Demonstration Tip

Using a whiteboard or projector:

- Sketch the layout of a cabinet door set (e.g. 2 large doors, 1 drawer front)

- Ask learners to map out how to cut these from a 2750 x 1830 mm board

- Calculate how many sets can be made per board, and what off-cuts will remain

Repeat with a poorly planned layout that causes excess waste.

Practical Exercise

Board Cutting Exercise: Provide a sample cutting list:

- e.g. 4 drawer sides (500 x 150 mm), 2 drawer fronts (500 x 200 mm), 2 backs (500 x 120 mm)

- Ask learners to choose a board size and draw a layout plan to minimise waste

Case Study: Reducing Off-Cuts in a Small Furniture Workshop

A workshop in Pretoria noticed high wastage of melamine board when making wardrobe carcasses. On investigation, they found the layout was not optimised, and many panels were slightly over- or under-sized, requiring trimming and leading to discard. They implemented a cutting plan system and reduced material loss by 15% over two months.

Discussion Prompts:

- What caused the wastage?

- How did standard size knowledge help?

- What other benefits come from reduced waste?

Critical Thinking Questions

- How can understanding board sizes help reduce manufacturing costs?

- What are the environmental benefits of reducing timber and board waste?

- What tools or planning aids can a machinist use to optimise material usage?

- If only partial boards are available, how should a machinist decide which parts to cut first?

- Why is it important to account for blade kerf (cut thickness) when calculating layouts?

### PA0207 – Handle and Store Raw Material Such as Lifting or Pallet Jacks in a Safe Manner

Facilitator Purpose

This session equips learners with the knowledge and practical skills to safely lift, move, and store raw timber and board materials using manual techniques and material handling equipment such as pallet jacks and trolleys. Emphasis is placed on preventing injury, avoiding damage to material, and maintaining an organised workshop environment.

Incorrect handling is a major source of workplace injury and can lead to costly material damage. This sub-task develops foundational competencies in occupational health and safety (OHS) and promotes accountability and teamwork in shared spaces.

Key Concepts to Cover

1. Types of Handling Equipment

| Equipment | Description | Use Case |
| --- | --- | --- |
| Pallet jack | Manual hydraulic device for lifting and moving pallets | Heavy board stacks or timber bundles |
| Furniture dolly | Platform with wheels | Moving board sheets across short distances |
| Trolley/Cart | Flatbed or upright design | Loading material into storage or machines |
| Forklift (if used) | Requires certified operator | Large-scale lifting in factories |

2. Manual Handling Techniques

- Always assess the weight and size of the item first

- Use team lifting for long or heavy boards (especially over 2 m)

- Keep the back straight, bend at the knees, and lift with the legs

- Carry boards vertically on the side, not flat

- Use gloves and closed footwear for grip and protection

3. Storage Safety and Organisation

- Stack boards horizontally on level racks with support at multiple points

- Do not store timber directly on the floor – use pallets or battens

- Mark sections by material type, thickness, and moisture content

- Avoid leaning sheets against walls (risk of tipping)

- Apply first-in, first-out principle to prevent warping from long storage

Facilitator Demonstration Tip

Practical Handling Rotation:

- Demonstrate correct lifting posture with a board and a pallet jack

- Let learners practise in small groups, guided by the facilitator

- Ask learners to demonstrate storage layout principles in the storeroom or mock-up rack

Highlight unsafe practices as part of a peer learning moment.

Case Study: Workshop Injury from Improper Board Handling

A learner at a Gauteng training centre suffered a sprained wrist while attempting to carry an 18 mm MDF sheet alone across the floor. The board slipped and hit a bench, damaging the edge and injuring the learner. Investigation revealed that no trolley was used, and proper lifting techniques were not applied.

Discussion Prompts:

- What should the learner have done differently?

- How could the material damage have been avoided?

- What could the training centre implement to prevent similar incidents?

Critical Thinking Questions

- Why is team lifting recommended for board sheets over 2 metres long?

- What could happen if wet timber is stored at the bottom of a stack?

- What injuries are common in the workshop due to poor handling practices?

- What role does labelling and inventory play in maintaining safe storage?

- Why is it important to consider the balance and centre of gravity when moving large items?

### PA0208 – Identify and Interpret the Labelling and Coding System Used to Identify and Trace Raw Material and Products

Facilitator Purpose

This session provides learners with the ability to read, understand, and apply labelling and coding systems used in furniture manufacturing to trace the origin, specification, and status of raw materials and products. Effective identification and tracking contribute to improved stock control, production planning, and compliance with quality assurance procedures.

Learners will also be introduced to basic inventory identification practices such as batch numbers, supplier codes, thickness designations, and moisture status labels as part of material management in the wood machining department.

Key Concepts to Cover

1. Why Labelling and Coding is Important

- Ensures the right material is used for the right product

- Enables traceability for quality control and recalls

- Reduces mix-ups between similar-looking boards (e.g. MDF vs chipboard)

- Supports stock rotation (e.g. using older stock first)

- Links materials to delivery notes, specifications, and supplier information

2. Types of Information Found on Labels

| Label Element | Description |
| --- | --- |
| Material Type | MDF, chipboard, pine, etc. |
| Board Size | Dimensions (e.g. 2750 x 1830 x 16 mm) |
| Moisture Content | % moisture – sometimes colour-coded or marked by batch |
| Supplier Code | Unique code identifying the supplier/manufacturer |
| Batch/Delivery Number | Used to trace issues back to a specific delivery |
| Grade or Quality Mark | A/B/C grade, kiln-dried, commercial, etc. |
| Date of Entry/Processing | Useful for applying FIFO stock rotation |

🛈 Colour stickers or barcoded labels may also be used in larger factories.

3. Reading and Interpreting Typical Labels

Provide learners with printed sample labels or use photos of real stock labels from suppliers such as PG Bison, Sonae Arauco, or local timber yards. Teach learners to:

- Decode abbreviations (e.g. KD Pine 32x76x3.6 – S5S)

- Trace back to stock sheet or delivery note

- Determine if the material meets the job specification

Facilitator Demonstration Tip

Create a mock-up “material shelf” with various labelled timber and board samples.
Give learners a job card requiring a specific board type and thickness, and let them:

- Find the correct item based on label

- Explain what each part of the label means

- Verify if it matches the required product specification

Practical Activity

Label Matching Task
Prepare printed labels and a list of work orders. Learners must:

- Match the right label to each order

- Flag incorrect matches (e.g. wrong board thickness or moisture rating)

- Suggest appropriate actions if a mismatch is found (e.g. notify supervisor)

Case Study: Mislabelling at a Cabinet Shop

A cabinetmaker used what he believed to be 16 mm MDF for wardrobe doors. After machining, it was discovered the boards were 18 mm chipboard, leading to hinge misalignment and weight issues. Investigation showed that a mislabelled stack had not been verified by the operator.

Discussion Prompts:

- What went wrong?

- What step in the labelling and verification process was skipped?

- How can similar issues be avoided in future?

Critical Thinking Questions

- Why is material traceability important in case of product failure or customer complaint?

- What is the risk of not checking labels before machining a board?

- How can a colour-coded labelling system improve workshop efficiency?

- What should a learner do if a label is missing or unclear?

- How does the use of digital inventory systems (barcodes or QR codes) improve raw material tracking?

## Applied Knowledge

Introduction to Applied Knowledge

The Applied Knowledge components for this sub-task focus on developing the learner’s theoretical understanding of the behaviour, quality, and safe storage of timber and boards used in the furniture manufacturing process. These knowledge areas are fundamental to effective material preparation, safe handling, and maintaining production quality in the machining department.

AK0201 – Timber and Board Characteristics and Quality

Learners must understand the key characteristics of solid timber and composite boards, as these properties determine how the material behaves during machining, assembly, and finishing. Knowledge of timber quality and suitability for different applications is essential for minimising waste, improving the performance of furniture products, and ensuring customer satisfaction.

Important characteristics include:

- Grain direction and appearance (influences strength and aesthetics)

- Moisture content (affects shrinkage, expansion, and joint integrity)

- Density and hardness (determines tool selection and cutting speed)

- Defects and imperfections (such as knots, checks, splits, warping)

- Machinability and finish quality (ease of cutting, sanding, and coating)

A solid understanding of these features empowers learners to assess material suitability for a given task and to anticipate how different materials will respond during processing.

AK0202 – Stacking Requirements and Techniques

Correct stacking of timber and board materials is essential to preserve material quality, support safety in the workplace, and optimise space utilisation. Improper stacking may lead to warping, surface damage, or even injury from falling materials.

Learners must become familiar with:

- Horizontal and vertical stacking principles for different material types

- Use of spacers or stickers to allow airflow between timber layers

- Correct alignment and load distribution to avoid pressure points and sagging

- Moisture protection methods including elevation from the floor

- Safe handling zones, access lanes, and stack height restrictions

Adopting proper stacking practices ensures a neat, hazard-free workshop and demonstrates a professional approach to material management and care.

### AK0201 – Timber and Board Characteristics and Quality

Facilitator Purpose

This session provides learners with foundational knowledge of the physical, mechanical, and visual properties of timber and engineered board materials commonly used in the furniture manufacturing industry. Understanding these characteristics is essential for selecting the appropriate material for each product, achieving high-quality finishes, minimising waste, and ensuring structural durability.

This knowledge underpins several practical operations in machining, assembly, and finishing, and supports decisions that affect safety, cost-efficiency, and end-user satisfaction.

Key Characteristics of Timber and Boards

1. Physical Properties

| Characteristic | Timber | Board Products |
| --- | --- | --- |
| Density | Varies by species (e.g. pine is light, kiaat is medium-heavy) | Uniform across boards (e.g. MDF is denser than chipboard) |
| Moisture Content | Affects shrinkage and stability | Susceptible to swelling if exposed |
| Grain Direction | Influences strength and appearance | Absent in MDF, present in plywood |
| Surface Finish | May have knots or uneven texture | Typically smooth and consistent |

2. Mechanical Properties

- Strength and Load-Bearing Capacity
Hardwoods (e.g. oak, meranti) are typically stronger than softwoods. Boards such as plywood provide strength across a broad surface, while chipboard is weaker and best used in non-structural components.

- Machinability
Pine and meranti machine well, whereas very hard woods may blunt tools quickly. MDF offers excellent routing performance due to its consistent density.

- Glue and Fastener Holding
Solid timber holds screws well. Particle board and MDF require pilot holes and appropriate fasteners to prevent splitting.

3. Aesthetic and Functional Qualities

- Colour and Texture
Timber offers unique variations in colour and grain. Board products can be laminated or veneered to imitate high-end finishes.

- Durability and Wear Resistance
Hardwood is generally more wear-resistant than softwood. Laminated board surfaces offer resistance to stains and moisture.

Examples of Timber and Board Selection by Use

| Application | Recommended Material | Reason |
| --- | --- | --- |
| Bookshelves | Plywood or melamine-faced chipboard | Straight, stable, and easy to edge-band |
| Dining table legs | Solid hardwood (e.g. kiaat or oak) | Strength and resistance to impact |
| Drawer bottoms | Hardboard | Lightweight and cost-effective |
| Cabinet doors | Veneered MDF or supa wood | Smooth for painting or veneering |
| Kids' furniture | Pine or MDF with rounded corners | Soft, lightweight, and easy to finish |

Case Study: Moisture Issues in Wardrobe Production

A furniture manufacturer in KwaZulu-Natal used pine that had not been fully dried before production. Once installed in clients’ homes, many wardrobe doors began to warp, and the drawers no longer aligned properly. Investigation revealed that the moisture content was still above 18 percent at the time of machining.

Facilitator-led Discussion Prompts:

- What property of timber caused the warping?

- How could the issue have been detected earlier?

- What could the company have done differently before machining the wood?

Critical Thinking Questions

- How does the grain direction of timber influence machining and final strength in a furniture product?

- In what situations would MDF be a better choice than solid timber? Why?

- What characteristics make chipboard unsuitable for load-bearing furniture components?

- Why is it important to match timber or board quality with the intended furniture use?

- How do variations in material characteristics influence pricing, waste levels, and product lifespan?

### AK0202 – Stacking Requirements and Techniques

Facilitator Purpose

This session introduces learners to the correct methods for stacking timber and board materials in a way that ensures worker safety, preserves material quality, and supports smooth production processes. Proper stacking reduces the risk of material damage such as warping, cracking, and edge damage, while also ensuring accessibility and compliance with workplace safety standards.

This knowledge supports the practical operations of handling, storage, and material flow within a wood machining or furniture production facility.

Key Concepts to Cover

1. Purpose of Correct Stacking

- Prevents bending, warping, or sagging of boards

- Reduces tripping hazards and workplace injuries

- Protects materials from moisture and contamination

- Ensures easy identification and access

- Maintains inventory order and flow

2. Stacking Requirements for Solid Timber

- Use stickers (spacers) between each layer to allow for air circulation

- Align timber pieces lengthwise with even support along the entire board

- Stack timber on raised battens or pallets to avoid floor moisture

- Group similar species, thicknesses, and lengths together

- Ensure that sticker rows are vertically aligned from top to bottom

- Do not stack timber near direct sunlight or moisture sources

3. Stacking Requirements for Composite Boards

- Store boards flat and horizontal on even surfaces

- Place timber runners between board stacks to distribute weight

- Do not exceed recommended stacking height (usually 1.5–1.8 metres)

- Protect edges with corner protectors or soft buffers

- Avoid placing heavy materials on boards with unsupported overhang

- In large facilities, colour coding or labelling can assist in stock rotation

Examples of Poor vs Correct Stacking

| Practice | Result (Poor Practice) | Improved Technique |
| --- | --- | --- |
| Boards stored directly on concrete | Moisture absorption leading to swelling | Raise stacks using dry battens or pallets |
| Timber stacked without stickers | Uneven drying, mould growth | Use uniformly spaced stickers |
| Uneven board alignment | Edge damage and unstable stacks | Align and level all four sides |
| Mixed materials stacked together | Misidentification, safety hazard | Separate and label materials by type |

Case Study: Damage in a Cape Town Workshop

In a small workshop near Cape Town, an apprentice stacked MDF sheets directly onto the floor against the wall. After a week of rain, several of the lower boards began to swell and delaminate. The material had to be discarded, causing financial loss and production delay.

Discussion Prompts:

- What stacking errors occurred?

- How could this damage have been prevented?

- What lessons can be applied in other material storage situations?

Critical Thinking Questions

- Why is airflow important when stacking solid timber, but less critical for boards like MDF?

- What hazards can result from stacking materials too high or unevenly?

- How can a workshop create a stacking system that is both space-saving and safe?

- What should you do if you notice boards are beginning to warp while in storage?

- How does good stacking practice support the principle of first-in, first-out stock rotation?

## Integrated Assessment Task

Assessment Type: Practical Knowledge Integration

Duration: 60 minutes

NQF Level: 2 Credits: 20

Assessment Context: On-site simulated or workshop-based activity

Case Study: “Precision Furniture” Material Intake Station

You are working at the raw material intake area at Precision Furniture, a small workshop that manufactures custom wardrobes, desks, and bedside cabinets. A delivery of materials has just arrived. It includes:

- 10 full sheets of melamine-faced chipboard (2750 x 1830 x 16 mm)

- 6 solid pine planks (38 mm x 228 mm x 3.6 m)

- 4 sheets of plywood (2440 x 1220 x 18 mm)

- Loose offcuts from previous jobs

The next production order is for:

- 30 bedside cabinet carcasses

- 15 drawer units

- 5 desk tops (solid wood preferred)

You are required to:

- Identify which materials match the product specification

- Check the materials for quality and defects

- Use the correct tools and techniques to measure, move, and store the materials

Assessment Questions

Question 1
Using the information provided in the case study, identify which of the delivered materials would be suitable for each of the following products. Specify the material type and size.

a) Bedside cabinet carcass
b) Drawer sides and bottoms
c) Desk tops

Question 2
List four types of defects or quality issues you would check for when inspecting the timber and board materials before cutting or machining them.

Question 3
Describe the correct procedure for using the following tools safely during this task:
a) Measuring tape
b) Pallet jack
c) Moisture meter

Question 4
You observe that one stack of chipboard sheets is leaning against the wall and touching the floor. What are the risks associated with this, and how should you correct the situation?

✅ MODEL ANSWERS

Answer 1

a) Bedside cabinet carcass –
Material: Melamine-faced chipboard
Size: 2750 x 1830 x 16 mm
Reason: Smooth surface, cost-effective, ideal for internal cabinet components

b) Drawer sides and bottoms –
Material: Plywood for sides (18 mm), Hardboard offcuts for bottoms (if available)
Reason: Strength for drawer sides, thin and lightweight for bottoms

c) Desk tops –
Material: Solid pine planks (38 x 228 x 3600 mm)
Reason: Durable, visually appealing, can be laminated and sanded to finish

Answer 2

- Warping or cupping in timber

- Delamination or bubbling on melamine board

- Swollen edges or signs of moisture exposure

- Knots, cracks, or surface damage in solid wood

Answer 3

a) Measuring tape: Pull out the tape carefully, keep it taut, measure edge to edge without bending. Record length, width, and thickness accurately. Retract tape slowly.

b) Pallet jack: Check wheels and forks before use. Slide forks under the pallet, pump handle to lift. Move slowly and keep the path clear. Do not overload.

c) Moisture meter: Calibrate device. Insert pins (if pin-type) into the centre of the wood or place sensor on surface (pinless). Wait for reading, record moisture content. Check in multiple spots.

Answer 4

Risks:

- Moisture from the floor can cause board swelling

- Leaning stacks can fall and cause injury or damage

- Warping may occur due to uneven support

Correction:

- Lay boards flat on horizontal supports or pallets

- Elevate off the floor using battens

- Stack evenly with edge protection if needed

📝 MARKING MEMO

| Question | Criteria | Marks |
| --- | --- | --- |
| Q1 | Correct identification of material types and sizes (3 parts × 3 marks each) | 9 |
| Q2 | 4 defects listed, 1 mark each | 4 |
| Q3 | 3 correct tool procedures, 2 marks each | 6 |
| Q4 | Risk explanation (2 marks), corrective action (3 marks) | 5 |
|  | Total Marks | 24 |

📊 ASSESSMENT RUBRIC

| Criteria | Outstanding (4) | Competent (3) | Developing (2) | Not Yet Competent (1) |
| --- | --- | --- | --- | --- |
| IAC0201 – Identify timber and board | All materials correctly identified and accurately matched to size and product. Clear justification. | Most materials correctly identified and linked to product use. | Partial identification of materials or sizes; limited explanation. | Incorrect identification or unclear relevance to the product. |
| IAC0202 – Check for defects and quality | Clearly identifies defects with examples and explains the impact on product quality. | Lists common defects and recognises their importance. | Identifies some defects but lacks depth or connection to quality. | Fails to recognise key defects or their importance. |
| IAC0203 – Use tools and store materials | Demonstrates thorough knowledge of safe and correct tool use and understands material handling procedures in full. | Describes basic use of tools and safe handling procedures. | Demonstrates limited tool knowledge or basic handling only. | Incorrect tool use or storage procedure, showing lack of understanding. |

### Facilitator Assessment Briefing

Practical Module: PM-01 – Operate a Range of Machines in the Wood Machine Shop to Cut Components for Furniture Manufacturing

Sub-task: PM-01-PS02 – Identify Timber and Board Used in the Manufacturing of Wooden Furniture

Assessment Type: Integrated Practical Knowledge Assessment

Internal Assessment Criteria:

- IAC0201: Timber and board is correctly identified in terms of type and size and matched to the product specifications

- IAC0202: Raw materials are checked for quality and defects to ensure high quality end products

- IAC0203: Machinery and tools are correctly used to check, handle and store raw materials

Purpose of the Assessment

The purpose of this assessment is to evaluate the learner’s ability to apply practical knowledge and decision-making when working with timber and board materials. It ensures that learners can identify material types, inspect for quality, and use appropriate tools and techniques to manage raw materials in a production environment.

This assessment forms part of the internal quality assurance process and prepares learners for the external summative assessment.

Assessment Context

The assessment is based on a simulated case study set within a realistic workshop scenario. Learners will be expected to interpret a production order, match materials to specifications, and apply safe handling and inspection procedures using standard equipment. The task requires both written responses and critical thinking to demonstrate understanding of quality, safety, and operational requirements.

Facilitator Instructions

- Ensure learners are briefed on the purpose and format of the assessment.

- Read the case study aloud and confirm learner understanding before beginning.

- Monitor that all tools and materials referred to in the task are either physically available or clearly described.

- Learners must complete all questions individually under supervised conditions.

- Mark the completed assessment using the model answers, marking memo, and assessment rubric provided.

- Provide developmental feedback after assessment completion, with opportunities for remediation if needed.

## PM-01-PS03: Identify Consumables and Accessories Used in Furniture Manufacturing

1. Introduction to the Practical Skill

This sub-task introduces learners to the diverse range of consumables, chemicals, and accessories used in the furniture manufacturing process, particularly within cabinet making. Learners will develop the ability to identify, inspect, select, and safely store consumables and fittings, while also considering their suitability for different furniture styles and functional requirements.

This module places strong emphasis on health and safety, as many consumables and chemicals used in woodworking — such as adhesives, solvents, and fillers — require proper handling to prevent accidents and extend product shelf life. Similarly, the correct selection and installation of accessories (such as hinges, handles, runners, and brackets) are essential for both aesthetic and functional outcomes in furniture production.

Learners will also engage in activities related to interpreting job card requirements, identifying standard sizes, and ensuring that the correct tools are used for the fitting of accessories, supporting a high standard of workmanship.

This sub-task builds critical knowledge and judgement for preparing materials prior to machining, assembly, and final finishing.

2. Scope of Practical Skill

Given a range of consumables, chemicals, and accessories used in the cabinet making process, the learner must be able to:

- PA0301 Identify consumables according to their uses

- PA0302 Identify accessories matched to specific uses and furniture styles

- PA0303 Inspect consumables and accessories for faults and defects

- PA0304 Handle and store chemicals according to safety requirements and to prolong product lifetime

- PA0305 Identify standard sizes

- PA0306 Handle and store consumables safely and according to requirements

3. Applied Knowledge

- AK0301 Types of consumables and accessories, their use and characteristics

4. Internal Assessment Criteria

- IAC0301 Different types of consumables and accessories are identified and selected according to the job card specifications

- IAC0302 Consumables are handled and stored according to health and safety specifications

- IAC0303 Accessories are selected according to their design and characteristics

- IAC0304 Correct tools are used when fitting accessories (hinges, runners, handles)

### PA0301 – Identify Consumables According to Uses

Facilitator Purpose

The purpose of this session is to equip learners with the ability to identify different types of consumables used in the furniture manufacturing process and understand their intended applications. Consumables are non-durable materials that are used up during production processes such as machining, assembling, finishing, and installation.

Learners will become familiar with the range of consumables commonly used in cabinet making and related operations, including adhesives, screws, dowels, edge banding, fillers, sandpaper, and finishing cloths. The facilitator should guide learners in recognising each consumable, understanding its function, and matching it to the appropriate stage of furniture production.

Key Concepts to Cover

1. Definition and Categories of Consumables

Consumables are materials that:

- Are not part of the final structure (with exceptions like fasteners or edge banding)

- Are used up or replaced regularly during production

- Support the fabrication, assembly, finishing, or maintenance of products

2. Common Categories of Consumables and Their Uses

| Consumable Type | Examples | Typical Use |
| --- | --- | --- |
| Adhesives | PVA glue, contact adhesive, hot melt glue | Bonding wood panels, laminates, edge banding |
| Fasteners | Screws, nails, staples, dowels, confirmat screws | Assembly and structural joining |
| Abrasives | Sandpaper (grits 60–240), sanding blocks | Surface preparation before finishing |
| Fillers | Wood filler, putty, wax sticks | Filling nail holes, surface defects |
| Finishing consumables | Rags, tack cloths, masking tape | Applying stains, cleaning surfaces |
| Edge banding materials | PVC, ABS, veneer strips | Covering raw edges of composite boards |
| Sealants and lubricants | Silicone spray, drawer runners grease | Smoothing movement of fittings and edges |
| Cleaning chemicals | Thinners, acetone, general-purpose cleaner | Cleaning tools, removing glue or overspray |

Facilitator Tip: Tabletop Demonstration

Lay out a table with clearly labelled consumables used in cabinet making. Allow learners to handle, read labels, and discuss what each item is used for.

Activity: Ask learners to match each item to its correct function and stage of the production process (e.g. "preparation," "assembly," "finishing").

Examples for Practical Understanding

| Furniture Task | Recommended Consumable | Why? |
| --- | --- | --- |
| Assembling a melamine cabinet | Confirmat screws and white PVA glue | Provides strong, concealed joints |
| Filling nail holes on face panels | Wood filler (matching tone) | Prepares surface for seamless finishing |
| Applying veneer edge to desk top | Hot melt glue or contact adhesive | Ensures lasting bond under pressure |
| Smoothing a pine drawer front | 180-grit sandpaper | Prepares surface for paint or varnish |
| Cleaning after spray application | Thinners and clean rags | Removes overspray and residue |

Case Study: Assembly Station Error

At a cabinet assembly station, a new worker mistakenly used wood glue meant for solid wood on laminated chipboard carcasses. The joints failed within days. Upon inspection, it was found that contact adhesive should have been used for the specific surface treatment.

Facilitator Discussion Prompts:

- What went wrong in this situation?

- How could proper identification of consumables have prevented this?

- What label information should the worker have checked?

Critical Thinking Questions

- Why is it important to match the type of adhesive to the type of material?

- How can using the wrong consumable affect furniture quality and customer satisfaction?

- What risks are associated with storing all consumables in the same location without labelling?

- Why might an abrasive with a grit that is too coarse damage a cabinet door panel?

- What would happen if edge banding was applied using the wrong glue or at the wrong temperature?

### PA0302 – Identify Accessories Matched to Specific Uses and Furniture Styles

Facilitator Purpose

This session enables learners to identify and classify a variety of furniture accessories based on their intended use and design suitability for different furniture styles. Accessories are not only functional components such as hinges and runners, but also aesthetic elements that enhance the look and user experience of furniture products.

Learners will develop an appreciation for the importance of selecting the right accessory for the right function and design context, and will understand how improper selection can compromise both usability and customer satisfaction.

Key Concepts to Cover

1. Definition of Furniture Accessories

Accessories are fittings, fixtures, and finishing elements that:

- Contribute to the functionality of a furniture item (e.g. opening, closing, adjusting)

- Add aesthetic detail or complement a particular style

- Support ergonomics, ease of use, and modern convenience

2. Common Types of Accessories

| Accessory | Function | Furniture Style Compatibility |
| --- | --- | --- |
| Hinges (butt, concealed, piano) | Enable door movement and angle control | Concealed – modern/contemporary; Butt – traditional |
| Drawer runners (roller, ball bearing, soft-close) | Smooth drawer movement | Soft-close – luxury/custom cabinetry |
| Handles and knobs | Grip points for drawers and doors | Brass – vintage/traditional; Aluminium – modern |
| Adjustable legs | Height adjustment and levelling | Office desks, contemporary wardrobes |
| Glass shelf brackets | Support shelving | Display units, minimalist designs |
| Locks and catches | Provide security or magnetic closure | File drawers, wardrobes, office cabinets |

3. Matching Accessories to Furniture Styles

| Style | Design Traits | Recommended Accessories |
| --- | --- | --- |
| Traditional | Ornate, classic, often wooden or carved | Brass knobs, decorative hinges, exposed fittings |
| Modern | Minimalist, clean lines, flat panels | Concealed hinges, aluminium handles, push-to-open catches |
| Rustic | Natural textures, raw materials, farmhouse look | Iron handles, strap hinges, visible brackets |
| Contemporary | Current design trends, blended finishes | Soft-close runners, chrome handles, LED fittings |
| Industrial | Metal finishes, exposed fasteners | Steel frames, visible bolts, heavy-duty hinges |

Facilitator Demonstration Tip

Bring in a sample board or use a projector to display photos or physical examples of:

- Different handles, hinges, and runners

- Contrasting accessories used on different styles of cabinetry

Ask learners to group accessories into the following categories:

- Function-based (e.g. movement, grip, security)

- Style-based (e.g. modern, traditional, rustic)

Activity Suggestion: Accessory Selection Challenge

Provide learners with product scenarios and ask them to select suitable accessories. Example:

Scenario: A customer orders a built-in wardrobe in a modern townhouse. The design requires soft-close doors, hidden hardware, and clean aesthetics.

Task: Choose 3 accessories appropriate for this design and explain your choice.

Case Study: Aesthetic Mismatch in Kitchen Installation

A cabinetmaker used ornate brass knobs and butt hinges on a sleek, flat-panel kitchen design. The client was dissatisfied, saying the kitchen looked outdated and mismatched. The fittings had to be replaced at the manufacturer’s cost.

Facilitator Prompts:

- What went wrong in this project?

- How can understanding style compatibility prevent rework?

- How could the correct accessories have improved the customer’s satisfaction?

Critical Thinking Questions

- Why is it important to match the finish of accessories to the overall furniture design?

- What practical factors must be considered when selecting drawer runners or hinges?

- How do user needs (e.g. elderly clients, office staff) affect accessory selection?

- In what ways do accessories influence the perceived quality of furniture?

- What questions would you ask a client to guide your selection of fittings and accessories?

### PA0303 – Inspect Consumables and Accessories for Faults and Defects

Facilitator Purpose

The purpose of this session is to teach learners how to visually and physically inspect consumables and accessories before use in furniture manufacturing. Ensuring that materials are free from faults and defects is critical for maintaining high product standards, reducing waste, and ensuring customer satisfaction.

This competency helps learners build a quality-focused mindset and encourages accountability when selecting materials for machining, assembly, and finishing processes.

Key Concepts to Cover

1. Why Inspection is Important

- Prevents use of damaged or defective items that may affect structural integrity or appearance

- Reduces production rework and wastage

- Ensures consistency in appearance and performance

- Supports compliance with quality assurance systems

2. Common Defects in Consumables

| Consumable | Possible Defects | Impact |
| --- | --- | --- |
| Adhesives (glue) | Dried out, discoloured, expired | Weak bonds, joint failure |
| Sandpaper | Torn sheets, uneven grit, water-damaged | Uneven surface finish |
| Fillers and putty | Hardened, cracked inside tub | Difficult application, poor surface smoothness |
| Edge banding rolls | Warped, adhesive missing, cracked edges | Poor adhesion, unsightly finish |
| Fasteners (screws, nails) | Bent, rusted, inconsistent sizing | Loose joints, damaged wood during application |

3. Common Defects in Accessories

| Accessory | Defect | Effect on Product |
| --- | --- | --- |
| Hinges | Bent leaves, seized joints, misaligned holes | Door misalignment, poor opening/closing |
| Drawer runners | Jammed mechanism, missing components | Drawer does not glide properly |
| Handles and knobs | Scratches, coating peeling, faulty threads | Aesthetic damage, installation failure |
| Locks and catches | Key or latch not working, misaligned casing | Security risk, malfunctioning hardware |

Inspection Techniques

- Visual inspection under good lighting

- Touch test for cracks, roughness, sharp edges

- Movement test for runners, hinges, or mechanical parts

- Check expiry or batch numbers for adhesives and chemicals

- Compare against job card specifications and quantity checks

Facilitator Demonstration Tip

Prepare a mix of acceptable and faulty items. Ask learners to:

- Identify the type of defect

- Decide whether the item should be used, repaired, or replaced

- Suggest how to document or report the fault

Include both visual inspection (e.g. corroded screws, dried filler) and functional inspection (e.g. hinge movement).

Case Study: Undetected Defect in Drawer Mechanism

A furniture installer fitted drawer runners in a batch of bedroom cabinets. Some runners had internal factory defects that were not visible at first. After delivery, customers reported drawers sticking and falling off track. The installer had failed to test movement during quality control.

Facilitator Prompts:

- What should the quality control process have included?

- How would early detection have saved time and costs?

- How can records and batch tracking assist with warranty claims?

Critical Thinking Questions

- What is the risk of applying an expired adhesive to a kitchen cabinet panel?

- How can defective fasteners impact the structural integrity of furniture?

- Why is movement testing critical when checking mechanical accessories like drawer runners?

- What documentation procedures can support the return or replacement of defective items?

- In your opinion, who should be responsible for final quality inspection — the assembler, the storekeeper, or the supervisor? Why?

### PA0304 – Handle and Store Chemicals According to Safety Requirements and to Prolong Product Lifetime

Facilitator Purpose

This session prepares learners to correctly handle, use, and store chemical-based products that are commonly found in furniture manufacturing workshops. These include adhesives, thinners, solvents, sealants, and cleaning agents. Learners must understand both the safety risks associated with chemical exposure and the storage conditions required to maintain product quality and prolong usability.

Proper chemical management not only ensures personal and environmental safety, but also supports workshop efficiency and cost savings by reducing product wastage due to contamination, evaporation, or degradation.

Key Concepts to Cover

1. Common Chemicals in Furniture Manufacturing

| Chemical Type | Examples | Uses |
| --- | --- | --- |
| Adhesives | PVA glue, contact adhesive, epoxy | Joining panels, laminates, edge banding |
| Solvents and Thinners | Mineral spirits, acetone, lacquer thinner | Cleaning brushes and spray guns, thinning finishes |
| Sealants | Silicone, polyurethane-based sealants | Sealing edges, waterproofing |
| Cleaning agents | Degreasers, alcohol-based sprays | Surface preparation, removing residues |
| Lubricants | Silicone spray, WD-40 | Easing drawer runners, hinges |

2. Handling Guidelines

- Read and follow Safety Data Sheets (SDS) for each chemical product

- Wear appropriate PPE: gloves, goggles, masks

- Work in well-ventilated areas; use spray booths or extractors where applicable

- Avoid skin and eye contact

- Do not mix chemicals unless explicitly instructed to do so

- Use dispensing containers instead of transferring from bulk by hand

- Always label all decanted containers clearly

3. Storage Requirements

- Store in original containers with intact labels

- Keep in cool, dry, shaded areas, away from heat or direct sunlight

- Use flammable storage cabinets for hazardous substances

- Avoid storing near food or drinking areas

- Organise by chemical type (adhesives, flammables, cleaners)

- Check expiry dates and rotate stock (first in, first out)

Facilitator Demonstration Tip

Create a mock Chemical Safety Station with:

- Correctly labelled containers

- PPE on display

- Signage (flammable, corrosive, no smoking)

- Safety Data Sheets

Demonstrate how to:

- Identify chemical hazards using pictograms (GHS symbols)

- Respond to a spill or accidental skin contact

- Store opened adhesives to prevent drying or separation

Case Study: Chemical Mismanagement Incident

At a furniture training workshop, an apprentice stored open tins of solvent-based adhesive next to a sunny window and forgot to seal one properly. Within two days, the contents began to thicken, and fumes caused headaches among other learners. One learner spilled the container while moving it, as it was unlabelled.

Facilitator Prompts:

- Which handling and storage principles were violated?

- What short- and long-term consequences can arise from chemical vapour exposure?

- What should the workshop have done to prevent this?

Critical Thinking Questions

- Why is it important to keep chemicals in their original containers or clearly labelled alternatives?

- What risks could arise from storing adhesives or thinners near heat sources?

- How does improper chemical storage affect product lifespan and production costs?

- What are the environmental responsibilities of a furniture workshop when disposing of chemical waste?

- In your opinion, what should be included in a workshop’s chemical handling checklist for daily operations?

### PA0305 – Identify Standard Sizes

Facilitator Purpose

This session equips learners with the ability to recognise and apply standard material sizes used in furniture manufacturing. Knowing the correct dimensions of raw materials and accessories is essential for preparing cutting lists, optimising material use, preventing measurement errors, and aligning components during assembly.

This competency enhances the learner’s confidence in interpreting specifications, selecting the correct consumables and accessories, and ensuring efficiency during production planning.

Key Concepts to Cover

1. Standard Sizes of Composite Boards (South African Context)

| Board Type | Typical Sizes (Length × Width) | Common Thicknesses |
| --- | --- | --- |
| MDF (Supa Wood) | 2750 mm × 1830 mm | 12 mm, 16 mm, 18 mm, 22 mm |
| Melamine-faced Chipboard | 2750 mm × 1830 mm | 16 mm, 18 mm |
| Plywood | 2440 mm × 1220 mm | 6 mm to 25 mm |
| Hardboard | 2440 mm × 1220 mm | 3 mm, 4.8 mm |

🛈 Note: Availability may vary slightly by supplier (e.g. PG Bison, Sonae Arauco).

2. Standard Sizes of Timber Products

| Timber Type | Nominal Sizes (Thickness × Width) | Standard Lengths |
| --- | --- | --- |
| SA Pine | 22 × 44 mm, 38 × 76 mm, 50 × 152 mm | 1.8 m, 2.4 m, 3.6 m |
| Hardwoods (e.g. Kiaat, Meranti) | Vary based on order | Typically 2.1–3.6 m |

Timber may be sold as rough sawn or PAR (Planed All Round), which affects the final dimensions.

3. Standard Sizes of Consumables and Accessories

| Accessory or Consumable | Typical Standard Sizes |
| --- | --- |
| Confirmat screws | 5 × 50 mm, 5 × 70 mm |
| Handles (centre-to-centre) | 96 mm, 128 mm, 160 mm, 192 mm |
| Drawer runners | 300 mm, 350 mm, 400 mm, 450 mm |
| Edge banding tape | 22 mm, 32 mm widths; 0.4 mm to 2 mm thickness |
| PVA glue packaging | 250 ml, 500 ml, 1 Litre, 5 Litre |

Facilitator Demonstration Tip

Use physical samples (or printed templates) of boards, screws, edge banding, drawer runners, and timber. Let learners:

- Measure with a tape or ruler

- Record each item’s size and label accordingly

- Compare against a standard sizing chart

Discuss which sizes are most commonly used in:

- Kitchen units

- Office furniture

- Bedroom wardrobes

Activity Suggestion: Material Matching Task

Provide learners with a job card specifying dimensions for a small cabinet. Ask them to:

- Select the most suitable standard board and fasteners

- Justify their choice

- Identify how many pieces can be cut from one full-size board with minimal waste

Case Study: Misreading of Board Dimensions

A workshop assistant ordered 9 mm MDF instead of 18 mm for a batch of cupboard doors. As a result, the doors sagged, and the batch had to be redone. The issue was traced back to a misreading of the job card and lack of familiarity with board thicknesses.

Discussion Prompts:

- What were the consequences of the error?

- How could proper training in standard sizes have prevented the issue?

- What systems can support double-checking of material specifications?

Critical Thinking Questions

- Why is it important to standardise board and timber sizes across a production team?

- How do standard sizes help reduce offcuts and waste in the cutting process?

- What considerations must be made when choosing between 16 mm and 18 mm board for cabinet carcasses?

- Why is knowing the centre-to-centre measurement of handles important in the drilling process?

- What tools can be used to assist in converting job card dimensions into board cutting plans using standard board sizes?

### PA0306 – Handle and Store Consumables Safely and According to Requirements

Facilitator Purpose

This session introduces learners to the correct methods for handling and storing consumables used in the furniture manufacturing process. Consumables such as adhesives, edge banding, fillers, fasteners, and abrasives require careful management to ensure both workplace safety and material longevity.

Learners will gain an understanding of the risks associated with improper storage, the importance of correct labelling and organisation, and how environmental conditions can impact the usability and safety of consumables.

Key Concepts to Cover

1. Definition of Safe Handling

- Using personal protective equipment (PPE) where appropriate (e.g. gloves for adhesives, masks for sanding)

- Avoiding contamination (e.g. keeping filler containers sealed, not touching adhesive surfaces)

- Lifting and transporting items using manual handling best practices

- Preventing exposure to dust, fumes, or direct skin contact

2. Storage Principles for Different Types of Consumables

| Consumable | Storage Guidelines |
| --- | --- |
| Adhesives (PVA, contact glue) | Keep containers sealed, store upright, avoid direct sunlight, do not freeze |
| Edge banding rolls | Store flat or on a dispenser, away from heat, label by type/thickness |
| Fillers and putties | Seal tightly after use, store in a cool, dry place |
| Abrasives (sandpaper, pads) | Store flat or rolled in dry conditions, avoid crushing |
| Fasteners (screws, dowels) | Use divided containers, label clearly, store in closed drawers or bins |
| Spray cans or pressurised containers | Store upright in ventilated space, away from heat sources or sparks |

3. Safety and Labelling Practices

- Always read manufacturer instructions and follow storage temperature or humidity recommendations

- Label all opened containers and repackaged consumables with name, type, and date of opening

- Use clear signage and maintain inventory rotation (first in, first out)

- Dispose of expired or unusable materials according to workplace safety policies

Facilitator Demonstration Tip

Set up a correct vs incorrect storage display in the classroom or workshop. Include:

- Properly labelled and sealed adhesives

- Organised fastener bins

- Crushed or moisture-damaged sandpaper (example of incorrect storage)

- Open filler containers showing hardened contents

Use this display to prompt discussion and learner observation.

Activity Suggestion: Storage Station Assessment

Provide learners with a tray of mixed consumables. Ask them to:

- Identify which items are stored correctly and which are not

- Propose corrections for the mismanaged items

- Suggest an appropriate location or storage method within the workshop

Case Study: Edge Banding Contaminated in Storage

A furniture workshop stored PVC edge banding rolls near a warm window and left them partially unrolled. The heat caused the adhesive layer to dry out and curl. When used, the edge banding did not bond properly, resulting in product returns from customers.

Facilitator Prompts:

- What storage rules were violated?

- What are the cost and reputational impacts of using poorly stored consumables?

- What alternative storage method could be implemented?

Critical Thinking Questions

- Why is it important to rotate stock when storing consumables like adhesives or fillers?

- What workplace risks arise from leaving spray cans or solvents near heat sources?

- What simple labelling or shelving systems can help improve the organisation of consumables in small workshops?

- How does poor storage of consumables impact product quality and workshop productivity?

- What are the key safety checks before using a consumable that has been in storage for several months?

## Applied Knowledge

### AK0301 – Types of Consumables, Accessories, Their Use and Characteristics

Facilitator Purpose

The aim of this session is to ensure learners have a solid theoretical understanding of the range, function, and physical properties of both consumables and accessories used in furniture manufacturing. By understanding the characteristics and appropriate applications of these materials, learners will be better prepared to select and use them effectively during machining, assembling, finishing, and fitting processes.

This applied knowledge underpins the ability to interpret job card specifications, avoid material misuse, and contribute to overall quality assurance.

Key Concepts to Cover

1. Definition of Consumables and Accessories

| Term | Definition |
| --- | --- |
| Consumables | Items that are used up or exhausted during the production process |
| Accessories | Items that are fitted to furniture to enhance functionality or appearance |

2. Common Types and Categories

A. Consumables

| Category | Examples | Primary Use | Key Characteristics |
| --- | --- | --- | --- |
| Adhesives | PVA glue, epoxy, contact adhesive | Bonding wood, boards, laminates | Viscosity, curing time, moisture resistance |
| Fasteners | Screws, nails, confirmat screws, staples | Mechanical joining of components | Size, thread type, coating (zinc, brass) |
| Abrasives | Sandpaper, sanding pads | Surface preparation before finishing | Grit number (coarseness), durability |
| Fillers and putties | Wood filler, wax sticks | Filling surface defects, joints | Drying time, sandability, colour matching |
| Edge banding | PVC, ABS, veneer tape | Covering exposed board edges | Width, thickness, glue compatibility |
| Cleaning agents | Thinners, alcohol-based sprays | Tool cleaning, removing excess adhesive or dirt | Volatility, safety rating, flammability |

B. Accessories

| Accessory | Common Types | Use in Furniture | Key Characteristics |
| --- | --- | --- | --- |
| Hinges | Butt hinge, concealed hinge, piano hinge | Cabinet doors, wardrobes | Opening angle, self-closing, mounting method |
| Drawer runners | Roller, ball-bearing, soft-close | Smooth drawer movement | Load rating, travel length, motion quality |
| Handles and knobs | Pull handles, bar handles, finger grips | Opening drawers and doors | Fixing centres, shape, finish (chrome, matte) |
| Brackets and supports | Angle brackets, shelf pins, L-braces | Support structural integrity or hold shelves | Load-bearing capacity, size, finish |
| Locks and catches | Cam locks, magnetic catches, latch bolts | Security or closure systems for doors/drawers | Keyed/alignment mechanism, housing durability |
| Feet and leg adjusters | Plastic, metal, rubber with thread bases | Levelling and stability of furniture | Height range, non-slip, thread size |

3. Material Compatibility and Application Tips

- Use PVA glue for solid wood joints and contact adhesive for laminates and edge banding

- Choose confirmat screws for melamine-faced chipboard carcasses

- Use wax sticks or wood filler that matches the timber colour for seamless finishing

- Select concealed hinges for modern designs and brass butt hinges for traditional furniture

- Ensure drawer runners match the load capacity of the drawer (e.g. office files vs. clothing)

Facilitator Demonstration Tip

Create a material identification tray with labelled and unlabelled items. Include:

- A variety of screws, adhesives, hinges, edge banding samples, drawer runners, etc.

Ask learners to:

- Group the items into “consumables” and “accessories”

- Identify the function of each

- Match them to a job card example or furniture design

Case Study: Material Misapplication at a Shopfitting Site

A team of shopfitters fitted office drawers with lightweight plastic runners instead of steel ball-bearing runners specified in the design. Within two weeks, several drawers jammed or fell off their tracks. Investigation revealed that the accessories were mislabelled and improperly verified.

Discussion Prompts:

- What material characteristics were ignored or misunderstood?

- How can technical data sheets and job cards support accurate selection?

- What are the implications for the customer and manufacturer?

Critical Thinking Questions

- What is the main difference between a consumable and an accessory in furniture production?

- Why is it important to understand the load-bearing capacity of drawer runners or hinges?

- How do finish options (e.g. chrome, matte black, brass) influence accessory selection?

- What happens if incompatible adhesives are used with certain materials like PVC or MDF?

- Why should a furniture maker understand both the functional and aesthetic aspects of accessories?

## Integrated Assessment Task

Assessment Type: Practical Knowledge Integration

Duration: 60 minutes

NQF Level: 2 Credits: 20

Assessment Context: Practical Simulation Based on Job Card

Case Study: "FormCraft Joinery – Bedside Unit Order"

You are working as a furniture assembler at FormCraft Joinery. You are tasked with preparing all materials required to manufacture 20 bedside units. Each unit includes:

- A melamine-faced chipboard carcass

- Two drawers (with runners)

- One cabinet door (with concealed hinges and a soft-close function)

- One handle per drawer and door

You have received a job card listing the specifications:

- Board: 2750 x 1830 x 16 mm white melamine

- Edge banding: 0.8 mm × 22 mm PVC, white

- Screws: Confirmat screws, 5 × 50 mm

- Drawer runners: 400 mm ball-bearing type

- Handles: 128 mm chrome handles

- Hinges: 110° concealed hinges with soft-close

You are responsible for:

- Selecting and checking the consumables and accessories

- Handling and storing them safely

- Choosing the correct tools to fit the accessories

Assessment Questions

Question 1
Refer to the job card specifications. Identify four consumables and four accessories required for this task, and briefly describe the purpose of each.

Question 2
Describe three safe handling or storage procedures for consumables (e.g. adhesives, edge banding, screws) that you must follow in the workshop.

Question 3
Explain how you would select drawer runners and hinges to match the design and style of the bedside unit.

Question 4
List the correct tools you would use to fit the following accessories, and explain their purpose:
a) Concealed hinges
b) Drawer runners
c) Handles

✅ Model Answers

Answer 1

Consumables:

- Edge banding – seals exposed board edges, improves durability and finish

- Confirmat screws – join panels securely during carcass assembly

- Adhesive – secures edge banding to melamine board

- Abrasives – smooths surfaces before finishing

Accessories:

- Concealed hinges – allows cabinet doors to open smoothly, soft-close feature

- Ball-bearing drawer runners – enables drawers to slide in and out with ease

- Chrome handles – allows for drawer and door operation

- Magnetic catches (optional) – keeps doors closed firmly

Answer 2

- Store adhesives and edge banding away from heat or sunlight to prevent deterioration

- Label all containers and storage bins clearly

- Keep screws in sealed, compartmentalised containers to prevent mixing and loss

Answer 3

- Select drawer runners based on drawer length and weight; 400 mm ball-bearing runners offer smooth movement and durability

- Hinges should match the board thickness (16 mm), allow full 110° opening, and support the modern design aesthetic with a concealed look and soft-close feature

Answer 4

a) Concealed hinges – cordless drill with hinge jig, screwdriver: to drill cup holes and secure hinges
b) Drawer runners – drill with guide template, pozi screwdriver: for precise alignment and mounting
c) Handles – template jig, measuring tape, cordless drill: for correct hole spacing and neat installation

📝 MARKING MEMO

| Question | Criteria | Marks |
| --- | --- | --- |
| Q1 | 4 correct consumables (1 mark each) and 4 correct accessories (1 mark each) | 8 |
| Q2 | 3 correct procedures, 2 marks each | 6 |
| Q3 | Appropriate hinge and runner matched to function and style | 5 |
| Q4 | 3 correct tool selections with explanations (2 marks each) | 6 |
|  | Total Marks | 25 |

📊 ASSESSMENT RUBRIC

| Criteria | Outstanding (4) | Competent (3) | Developing (2) | Not Yet Competent (1) |
| --- | --- | --- | --- | --- |
| IAC0301 – Identify and select consumables and accessories | Correctly identifies all materials with full relevance to job card. | Identifies most items and matches majority to use. | Some items misidentified or incompletely explained. | Fails to identify or explain most items. |
| IAC0302 – Safe handling and storage | Demonstrates strong awareness of safety and storage for all consumables. | Applies basic safety principles; minor gaps in procedure. | Incomplete or inconsistent understanding of safety and storage. | Unsafe practices or lacks understanding of proper procedures. |
| IAC0303 – Select accessories by design | Selects all accessories with clear link to design and function. | Selects appropriate items; rationale is clear. | Selection is partially suitable or lacks explanation. | Inappropriate or incorrect accessory choices. |
| IAC0304 – Correct tools for fitting | Tools are correctly selected and matched to tasks with clear justification. | Tools are mostly appropriate with some detail. | Limited explanation or tool mismatches. | Incorrect tools or vague/uninformed responses. |

### Facilitator Assessment Briefing

Practical Module: PM-01 – Operate a Range of Machines in the Wood Machine Shop to Cut Components for Furniture Manufacturing

Sub-task: PM-01-PS03 – Identify Consumables and Accessories Used in Furniture Manufacturing

Assessment Type: Integrated Practical Knowledge Assessment

Internal Assessment Criteria:

- IAC0301: Different types of consumables and accessories are identified and selected according to the job card specifications

- IAC0302: Consumables are handled and stored according to health and safety specifications

- IAC0303: Accessories are selected according to their design and characteristics

- IAC0304: Correct tools are used when fitting accessories (hinges, runners, handles)

Purpose of the Assessment

The purpose of this assessment is to evaluate the learner’s ability to identify, handle, and apply consumables and accessories effectively within a practical workshop context. The learner will demonstrate their ability to follow job card specifications, apply correct health and safety procedures, and select the appropriate tools and materials for a given assembly task. This assessment forms part of the internal competency evidence required for progression to the External Integrated Summative Assessment (EISA).

Assessment Context

The assessment is based on a real-world job card scenario involving the preparation of materials for manufacturing bedside units. The learner will be expected to interpret product specifications, select suitable consumables and accessories, demonstrate safe handling practices, and indicate correct tooling procedures for fitting operations.

Facilitator Instructions

- Introduce the case study and confirm learners’ understanding of the scenario.

- Ensure learners have access to relevant catalogues, tools, or demonstration samples where applicable.

- Allow learners to complete the questions individually under supervised, classroom-based conditions.

- Use the provided model answers, marking memo, and assessment rubric to mark the assessment.

- Provide clear, constructive feedback, and offer additional support to learners who do not meet the required standard.

## PM-01-PS04: Identify a Range of Machines, Machine Parts, Machine Attachments and Tools in the Furniture Machine Shop

1. Introduction to the Practical Skill

This practical skill module introduces learners to the core machinery and related components used in a wood machining workshop. The focus is on identifying a variety of machines, their key parts, attachments, and tools, as well as understanding their operational control systems, colour coding, pneumatic features, and built-in safety mechanisms.

A competent furniture maker must understand how to recognise, interpret, and work with machinery commonly used in breakout, planing, sanding, and laminating operations. Equally important is the ability to interpret panel indicators, alarms, control switches, and to assess whether safety features are functional and properly engaged before use.

This foundational knowledge supports safe and efficient production processes and prepares the learner for machine set-up, routine maintenance, and quality machining in future tasks.

2. Scope of Practical Skill

Given access to a range of machines and tools used in the wood machine shop, the learner must be able to:

- PA0401 Identify the machines, parts, attachments and tools used in the break-out operation

- PA0402 Identify the machines, parts, attachments and tools used in the planing operation

- PA0403 Identify the machines, parts, attachments and tools used in the sanding operation

- PA0404 Identify the machines, parts, attachments and tools used in the laminating operation

- PA0405 Identify the safety mechanisms applicable to various machines

- PA0406 Identify the control systems for operating the machine

- PA0407 Identify and explain different colour coding used on the machines

- PA0408 Identify the pneumatic machines and the required pressures

3. Applied Knowledge

- AK0401 Machines in the wood workshop

- AK0402 Meaning of signals, switches, alarms, guides and gauges

- AK0403 Safety when using machines, equipment and tools

4. Internal Assessment Criteria

- IAC0401 The different machines operating in the machine shop are correctly identified along with their parts and their functions

- IAC0402 All switches, lights and signals on the panel board or control system are correctly identified and interpreted

- IAC0403 The safety mechanisms on the various machines in the machine shop are correctly identified in order to ensure they are functioning properly

### PA0401 – Identify the Machines, Parts, Attachments and Tools Used in the Break-out Operation

Facilitator Purpose

The purpose of this session is to enable learners to correctly identify the machines, machine parts, attachments, and tools used in the break-out stage of the furniture manufacturing process. The break-out operation is the first phase in machining, where large sheets or planks are cut to manageable sizes before being processed further.

Understanding the machines used during this stage is vital to preparing material safely and efficiently for planing, joining, and final shaping. The facilitator should emphasise the purpose of each machine, the components that enable cutting and feeding, and the tools or jigs that support precision and user safety.

Key Concepts to Cover

1. Purpose of the Break-out Operation

- Reduces large sheet or timber stock to sizes appropriate for machining

- Involves initial cross-cutting, ripping, and trimming

- Forms the first step in preparing parts for cabinetry or furniture frames

2. Common Machines Used in the Break-out Operation

| Machine | Function | Typical Application |
| --- | --- | --- |
| Panel saw | Cuts sheet materials along straight lines | Breaking down chipboard, MDF, plywood |
| Cross-cut saw | Cuts wood across the grain (short lengths) | Trimming ends of solid wood |
| Rip saw | Cuts wood along the grain | Ripping planks into narrower pieces |
| Radial arm saw | Makes accurate cross cuts, angles, mitres | Versatile cross-cutting and trenching |
| Band saw | Used for irregular or curved cuts (if needed) | Less common in initial break-out, but possible |

3. Key Machine Parts and Attachments

| Machine Part | Function |
| --- | --- |
| Fence or guide rail | Keeps cuts straight and aligned |
| Riving knife | Prevents material from pinching the blade |
| Blade guard | Protects operator from direct blade exposure |
| Blade height/depth adjustment | Controls how deep the blade cuts into the material |
| Emergency stop button | Instantly halts the machine in case of danger |
| Clamping mechanism | Secures workpiece to prevent movement during cutting |

4. Tools and Jigs Used

| Tool or Jig | Purpose |
| --- | --- |
| Push stick/push block | Keeps hands safe while feeding narrow stock |
| Measuring tape | Measuring before positioning cuts |
| Pencil or chalk | Marking cut lines on material |
| Adjustable stops | Repeating consistent cuts on multiple boards |
| Digital or manual angle gauge | Ensuring accurate angled or bevelled cuts |

Facilitator Demonstration Tip

Conduct a walkthrough of the break-out area in your workshop (or use high-resolution visuals if machinery is not physically accessible). Demonstrate:

- How each machine is named and identified

- Where the controls and guards are located

- What each part does and how it contributes to safety and accuracy

Encourage learners to label machine diagrams or complete a matching worksheet that pairs machines, parts, and functions.

Activity Suggestion: Identification Circuit

Create rotating stations with:

- A machine name card

- Photographs of parts

- A tray of accessories (e.g. push sticks, clamps)

Ask learners to:

- Match the items to the correct machine

- Explain the function of at least one safety mechanism on each

Case Study: Misuse of the Rip Saw

An apprentice misidentified a rip saw as a panel saw and used it to cut melamine-faced board. The blade chipped the surface, and the cut edge was rough and jagged. Additionally, the riving knife was removed, increasing kickback risk.

Discussion Prompts:

- What went wrong in machine selection and setup?

- Why is it essential to match the machine and blade to the material type?

- What could the workshop have done to avoid this?

Critical Thinking Questions

- Why is it important to identify a riving knife and ensure it is installed correctly?

- What is the purpose of the blade guard on a panel saw, and why must it never be removed?

- How does the fence assist in achieving safe and accurate break-out cuts?

- What risks arise from using a cross-cut saw for ripping solid timber?

- What role does a push stick play in learner safety, and when must it be used?

### PA0402 – Identify the Machines, Parts, Attachments and Tools Used in the Planing Operation

Facilitator Purpose

This session introduces learners to the machines and tools used in the planing operation, a critical stage in furniture manufacturing where timber and board materials are smoothed and dimensioned to required thicknesses. The focus is on identifying the correct machines, understanding their structure and function, recognising key safety mechanisms, and selecting the appropriate tools and attachments for efficient and accurate surface preparation.

Planing ensures that workpieces are uniformly flat, square, and ready for assembly or further processing. It also supports the proper bonding of laminates and reduces the risk of dimensional errors during cutting and joining.

Key Concepts to Cover

1. Purpose of Planing Operations

- Removes surface irregularities and warping from rough timber

- Reduces thickness to specified dimensions

- Prepares a smooth surface for joining, edge-gluing, or finishing

2. Common Machines Used in Planing

| Machine | Function | Application |
| --- | --- | --- |
| Surface planer (jointer) | Flattens one face of a board to produce a reference surface | First-stage flattening of timber |
| Thickness planer | Reduces the board to a specific, even thickness | Ensures uniform thickness across entire batch |
| Combination planer | Performs both jointing and thicknessing in one unit | Used in smaller shops or mobile training units |

3. Machine Parts and Attachments

| Component | Function |
| --- | --- |
| Infeed table | Supports material before it reaches the cutting blades |
| Outfeed table | Receives material post-cut, ensuring smooth exit |
| Cutter head/blades | Rotating blades that remove material |
| Height adjustment wheel | Adjusts the cutter head or table to control cutting depth |
| Fence | Guides timber for accurate edge planing |
| Pressure rollers | Feed the timber through the machine in a thickness planer |
| Dust extraction port | Connects to vacuum system to remove chips |

4. Tools Used with Planing Operations

| Tool | Purpose |
| --- | --- |
| Featherboards or pressure pads | Keep timber flat against fence and table |
| Calipers or ruler | Check final thickness of timber after planing |
| Push blocks | Assist in feeding short stock while keeping hands safe |
| Moisture meter | Ensure wood is properly dried before planing |
| Marking tools | Indicate high or low spots before additional passes |

Facilitator Demonstration Tip

If available, conduct a live demonstration or video walkthrough using:

- A surface planer to flatten one side of a rough timber plank

- A thickness planer to reduce to a precise measurement

- Highlight infeed/outfeed roles, blade position, and safety features such as blade guards and emergency stops

Ask learners to label a diagram of the planer machines and identify each part’s function.

Activity Suggestion: Matching Game

Provide printed cards or slides with:

- Machine parts

- Machine names

- Functions

Ask learners to match three components correctly per machine (e.g. "Cutter head – Surface Planer – Slices top surface").

Case Study: Uneven Timber After Incorrect Planer Use

An apprentice was asked to prepare timber for kitchen carcasses. They used the thickness planer without first flattening one face on the surface planer. As a result, the timber bowed during cutting, leading to gaps in joinery and poor glue bonding.

Facilitator Prompts:

- What mistake occurred in the sequence of operations?

- Why must the reference surface be prepared first?

- What impact did this have on the assembly stage?

Critical Thinking Questions

- Why must one face be flattened on a surface planer before using a thickness planer?

- What is the function of pressure rollers in a thickness planer?

- Why should a moisture meter be used before planing?

- What safety risk is associated with planing very short pieces of timber?

- How can inaccurate height adjustment lead to material wastage or machine overload?

### PA0403 – Identify the Machines, Parts, Attachments and Tools Used in the Sanding Operation

Facilitator Purpose

This session is designed to familiarise learners with the machines, parts, attachments, and tools used during the sanding stage of furniture production. Sanding is a critical step in achieving smooth, defect-free surfaces before applying finishes such as paint, stain, or varnish. It contributes to the overall appearance, feel, and quality of the finished product.

Learners will gain insight into both manual and powered sanding methods, including the use of wide belt sanders, orbital sanders, edge sanders, and related safety and setup considerations.

Key Concepts to Cover

1. Purpose of the Sanding Operation

- Smooths surfaces after machining or joining

- Removes saw marks, surface blemishes, and glue residue

- Prepares panels or solid timber for finishing

- Evens out slight thickness variations

2. Common Machines Used in the Sanding Operation

| Machine | Function | Application |
| --- | --- | --- |
| Wide belt sander | Removes material evenly from panel surfaces | Used for flat, large boards or veneered panels |
| Edge sander | Sands edges of panels or solid components | Straight edge finishing for carcasses, doors |
| Spindle sander | Sands internal curves or rounded parts | Craft or decorative component sanding |
| Orbital/Random orbit sander | Handheld; finishes flat surfaces and removes minor defects | For finer sanding before finishing |
| Drum sander | Used for narrow, thick, or profiled solid wood | Smaller batch or high-precision sanding |

3. Machine Parts and Attachments

| Part or Attachment | Function |
| --- | --- |
| Sanding belt/drum/pad | Abrasive surface used to remove material |
| Conveyor feed belt | Moves the panel through the wide belt sander evenly |
| Table height adjuster | Controls sanding depth or thickness |
| Dust extraction port | Removes fine dust to improve safety and finish quality |
| Safety guard/shield | Protects operator from moving parts and debris |
| Emergency stop button | Provides immediate shutdown in case of malfunction |

4. Tools and Accessories Used in Sanding

| Tool | Purpose |
| --- | --- |
| Abrasive pads and blocks | Manual sanding for fine finishing or awkward areas |
| Sandpaper (various grits) | For progressing from coarse to fine finish |
| Tack cloth or brush | Removes dust between sanding passes |
| Calipers or micrometer | Measure uniformity in sanding thickness |
| Template or jig | Guides sanding for consistent shapes or profiles |

Facilitator Demonstration Tip

Use an actual edge sander or orbital sander to:

- Show how different grits of abrasives feel and function

- Explain feed rate, pressure application, and stopping points

- Emphasise dust management (PPE, ventilation, dust extraction systems)

Display samples of sanded wood from coarse (80 grit) to fine (220+ grit), and let learners compare finishes by touch and sight.

Activity Suggestion: Grit Progression Board

Provide learners with small timber panels and sandpaper in three grits (e.g. 80, 120, 220). Ask them to:

- Sand one area with each grit

- Label the grit used

- Reflect on the smoothness and intended application

Case Study: Surface Damage Due to Incorrect Sanding

In a recent production run, a team used a coarse grit belt on a veneered panel in the wide belt sander. The belt was worn and the machine was incorrectly adjusted. The result was sanding through the veneer, damaging expensive material.

Facilitator Prompts:

- What should have been checked before starting the operation?

- How could the veneer damage have been avoided?

- What is the role of grit selection and machine calibration in sanding?

Critical Thinking Questions

- Why is it important to use progressively finer grits when sanding a surface?

- What safety hazards are associated with sanding operations, particularly with large machines?

- How does the sanding process differ when working with veneered panels versus solid wood?

- What can happen if a sanding belt is worn, loose, or clogged with dust?

- Why is dust extraction essential in the sanding area, both for safety and finish quality?

### PA0404 – Identify the Machines, Parts, Attachments and Tools Used in the Laminating Operation

Facilitator Purpose

This session enables learners to identify and describe the machines, parts, attachments, and tools used in the laminating process, a critical operation in modern furniture manufacturing. Laminating involves bonding two or more materials (usually a decorative surface onto a board or timber substrate) to enhance aesthetics, durability, and function.

Learners will explore both manual and mechanical laminating methods, and gain familiarity with tools and machines used for surface preparation, adhesive application, pressing, and curing. This foundation supports efficient, safe, and high-quality laminating procedures aligned to industry standards.

Key Concepts to Cover

1. Purpose of Laminating in Furniture Manufacturing

- Enhances the appearance of cost-effective core materials

- Adds durability, scratch and moisture resistance

- Reduces the need for extensive finishing

- Supports mass production of uniform surfaces (e.g. cabinet doors, countertops)

2. Common Machines Used in Laminating Operations

| Machine | Function | Typical Application |
| --- | --- | --- |
| Glue spreader | Evenly applies adhesive to board surfaces | Preparing panels for laminating |
| Cold press | Applies uniform pressure over a long period | Bonding laminates to substrates using PVA glue |
| Hot press | Uses heat and pressure to cure glue quickly | Laminating with heat-activated adhesives |
| Edge bander | Applies edge strip to raw board edges | Sealing and finishing melamine or MDF panels |
| Vacuum press | Presses curved or complex surfaces evenly using vacuum | Forming laminated curves, specialty surfaces |

3. Machine Parts and Attachments

| Machine Part | Function |
| --- | --- |
| Rollers | Distribute adhesive or press laminate to board |
| Pressure plates or frames | Apply pressure across the panel during curing |
| Temperature and pressure gauges | Monitor and control machine performance |
| Conveyor feed belts | Move boards through hot presses or edge banders |
| Edge trimming units | Trim excess laminate or edge banding material |

4. Tools and Consumables Used in Laminating

| Tool or Item | Purpose |
| --- | --- |
| Hand roller | Manually apply pressure to small or irregular laminates |
| Contact adhesive / PVA glue | Bonds laminate to board or curved surfaces |
| Laminate shears or trimmer | Cut high-pressure laminate to size |
| Cleaning cloths and thinners | Remove glue squeeze-out or surface dirt |
| Measuring tape, ruler, and templates | Ensure accurate sizing before laminating |

Facilitator Demonstration Tip

Demonstrate or display:

- A glue spreading station

- Cold or hot press controls (or images/diagrams)

- Edge banding machine and its stages (glue pot, pressure rollers, trimming)

If possible, show laminate sheets and let learners:

- Feel the surface

- Cut sample pieces

- Apply by hand using contact adhesive and a roller

Activity Suggestion: Laminating Process Walkthrough

Provide a step-by-step visual guide or printed handout showing:

- Surface cleaning

- Adhesive application

- Pressing or clamping

- Trimming and edge finishing

Ask learners to place the steps in correct sequence, and link each step to the corresponding machine/tool.

Case Study: Incomplete Bonding in Laminated Panels

A batch of office desks laminated using a cold press began peeling at the edges after a few weeks. Investigation showed that adhesive was unevenly applied, and the pressure applied was insufficient. The operator also failed to allow for full curing time.

Facilitator Prompts:

- What process or machine settings may have been incorrect?

- Why is curing time critical in cold press laminating?

- How can machine calibration prevent bonding failures?

Critical Thinking Questions

- What are the advantages and disadvantages of hot press vs cold press laminating?

- Why is even adhesive application critical in laminating operations?

- What risks can arise from using an incorrectly set edge banding machine?

- How does laminate orientation (grain or pattern) affect the visual outcome of furniture panels?

- What checks must be completed before pressing to ensure the laminated panel will cure correctly?

### PA0405 – Identify the Safety Mechanisms Applicable to Various Machines

Facilitator Purpose

This session introduces learners to the safety mechanisms installed on woodworking machinery, with the aim of promoting safe operation, reducing the risk of injury, and ensuring compliance with occupational health and safety regulations. Learners will be able to recognise, describe, and explain the function of standard safety features fitted to machines used in break-out, planing, sanding, and laminating operations.

This knowledge underpins every machine-related practical activity and contributes to the learner’s ability to perform pre-use checks, report faults, and respond to mechanical hazards effectively.

Key Concepts to Cover

1. Purpose of Machine Safety Mechanisms

- Protect the operator from injury

- Prevent accidental start-up

- Limit access to dangerous moving parts

- Support safe emergency response

- Ensure consistent operational control

2. Common Safety Mechanisms and Their Functions

| Safety Mechanism | Function | Machine Examples |
| --- | --- | --- |
| Blade guard | Covers saw blade while in operation to prevent contact | Table saw, panel saw, cross-cut saw |
| Riving knife | Prevents timber from closing on the saw blade, reducing kickback | Rip saw, panel saw |
| Emergency stop button | Instantly cuts power to the machine in case of emergency | Standard on all major stationary machines |
| Brake system | Brings moving parts (e.g. cutters, belts) to a stop quickly | Surface planer, wide belt sander |
| Limit switches | Stops machine if guard is removed or if door/panel is open | Presses, enclosed sanders |
| Start-up warning light or buzzer | Alerts nearby workers that a machine is starting up | Larger presses, CNC machinery |
| Pressure sensors or cut-off valves | Prevents operation without proper pressure (pneumatic) | Pneumatic clamping or pressing systems |
| Interlock systems | Locks controls until machine setup or safe conditions are met | Cold press, laminators, CNC routers |

3. Visual Indicators of Safety

- Colour Coding (often aligned to ISO or local standards):

  - Red – emergency stop or hazard

  - Yellow – caution zones or guards

  - Green – safe operation or start-up controls

- Safety Labels and Signage: “Do not operate without guard”, “Eye protection required”, etc.

- Alarms and Indicators: Flashing lights, beeping sounds, digital readouts warning of overload

Facilitator Demonstration Tip

During a workshop tour or using machine images:

- Point out the location of each safety mechanism

- Demonstrate an emergency stop activation and reset

- Remove and reattach a blade guard (where safely possible) to show interlock in action

- Highlight where signage or labels should appear and discuss their meanings

Encourage learners to create a safety checklist for machine use that includes these mechanisms.

Activity Suggestion: Machine Safety Scavenger Hunt

In small groups, learners move between machines and locate:

- The emergency stop

- A safety guard or riving knife

- A label or warning sign

- A start-up indicator

They record the name of the machine, what the mechanism does, and what risk it prevents.

Case Study: Injury Caused by Bypassed Safety Guard

A junior operator in a woodshop removed the blade guard from a cross-cut saw to make repeated cuts faster. During use, a piece of timber kicked back and the blade grazed his hand. The supervisor discovered that multiple operators were bypassing safety guards for convenience.

Facilitator Prompts:

- What safety mechanisms were ignored?

- What responsibilities lie with the operator, supervisor, and employer?

- How can this type of incident be prevented in future?

Critical Thinking Questions

- Why is it important to never operate a woodworking machine without safety guards in place?

- How does an emergency stop button improve workshop safety, and where should it be located?

- What are the risks of disabling or bypassing limit switches or interlocks?

- How do colour-coded components support safe operation in a busy machine shop?

- What routine checks should be performed before operating a machine to ensure all safety mechanisms are in working order?

### PA0406 – Identify the Control Systems for Operating the Machine

Facilitator Purpose

This session is designed to ensure that learners can identify, describe, and correctly interpret the control systems used to operate a variety of woodworking machines in the furniture manufacturing environment. Understanding control interfaces is essential for safe operation, troubleshooting, and consistent machine output.

Learners will be introduced to control panels, buttons, switches, and digital displays, and will develop the ability to interpret their functions according to machine type and workshop protocols.

Key Concepts to Cover

1. Purpose of Machine Control Systems

- Initiate and stop machine operations

- Regulate machine functions (e.g. speed, feed rate, temperature, pressure)

- Ensure operator control and feedback during production

- Display error codes, alerts, and operational statuses

2. Types of Machine Control Interfaces

| Control Element | Function | Examples of Machines |
| --- | --- | --- |
| Start/Stop buttons | Powers the machine on or off | Panel saw, thickness planer |
| Emergency stop (E-stop) | Instantly cuts power in emergencies | All fixed machines |
| Speed/Feed rate dials | Adjusts rotation speed or material feed | Wide belt sander, spindle moulder |
| Digital display screen | Shows parameters such as thickness, timer, pressure | CNC router, hot press, programmable planer |
| Mode selector switch | Chooses between automatic/manual, pre-set modes | Edge bander, multi-boring machine |
| Pressure gauges | Monitors pneumatic or hydraulic pressure | Cold press, pneumatic clamps |
| Sensor or indicator lights | Indicate power status, overload, errors, or cycle end | Found across all modern woodworking machinery |

3. Control System Colour Coding and Symbols

| Colour | Meaning |
| --- | --- |
| Green | Start, operational, safe |
| Red | Stop, fault, emergency |
| Yellow | Caution, warning |
| Blue | Information, programming modes |

Common symbols:

- Circle with line: power

- Arrow: feed direction

- Exclamation mark: caution/error

- Flame/thermometer: temperature controls or overheating alert

Facilitator Demonstration Tip

Provide a demonstration using a machine with a visible control panel (or projected photos of one), and walk learners through:

- The start-up sequence

- Setting operational parameters

- How to respond to indicator lights or alarms

- Proper shutdown procedures

Have learners create a simple control flow diagram based on their observations.

Activity Suggestion: Control Panel Simulation

Using a printed or mock-up machine control panel:

- Give learners specific scenarios (e.g. “Machine is jammed – what indicator shows this?”)

- Ask them to point out the relevant button, switch, or light

- Discuss what action should follow (e.g. E-stop, fault report, system reset)

Case Study: Misuse of Digital Control Panel

An operator used a programmable planer to reduce board thickness. However, they skipped inputting the final thickness and used the last saved setting by mistake. This resulted in over-planing, material waste, and rework. No system reset was done before beginning the job.

Facilitator Prompts:

- What control system was neglected?

- What procedure should be followed when starting a new job?

- How can digital displays prevent errors if used correctly?

Critical Thinking Questions

- Why is it important to reset digital controls or check settings before each machining task?

- How do visual control indicators support safe and efficient workflow in the machine shop?

- What are the consequences of ignoring error lights or alarms during machine operation?

- Why should the operator be trained in both manual and automated control settings?

- What steps should be included in a machine pre-start control system checklist?

### PA0407 – Identify and Explain Different Colour Coding Used on the Machines

Facilitator Purpose

The purpose of this session is to enable learners to recognise and interpret standard colour coding used on woodworking machinery. Colour coding enhances visibility, supports intuitive operation, and is an essential component of occupational health and safety in the workshop. Learners will learn how colours relate to machine controls, safety features, hazard zones, and maintenance points, and how this knowledge supports safe, compliant machine use.

Understanding these visual systems empowers operators to make fast and accurate decisions under pressure, reduce accidents, and communicate more effectively with fellow workers and supervisors.

Key Concepts to Cover

1. Why Colour Coding is Important

- Provides instant recognition of risk levels, actions, and safe zones

- Supports international safety standards and organisational protocols

- Aids communication in noisy environments where verbal instructions are limited

- Reduces reliance on written language – suitable for diverse teams and multilingual environments

2. Common Colour Codes on Woodworking Machinery (Aligned to ISO/ANSI/SABS Guidelines)

| Colour | Meaning / Application | Examples |
| --- | --- | --- |
| Red | Emergency stop, fire hazard, danger | Emergency stop buttons, fire extinguishers |
| Green | Safe to start, normal operation, safety confirmation | Start buttons, main power switches, access points |
| Yellow | Caution, potential hazard, moving parts | Guards, adjustable fences, exposed blade zones |
| Blue | Mandatory action or specific instructions | PPE signs, reset buttons, lockout systems |
| Orange | Risk of mechanical or pinch hazards | Rotating cutters, gearboxes, drive belts |
| White/Black | Neutral operational zones or functional markings | Height scales, dial labels, measurement markings |
| Grey | Structural or non-hazardous machine parts | Machine bases or panels |

🛈 Colour codes may also be supplemented by symbols or pictograms to improve clarity.

3. Where Colour Coding Appears

- Control panels (start/stop buttons, fault indicators)

- Safety zones (marked areas on the floor or machine perimeter)

- Moving parts (guards, fences, spindles)

- Instructional signs and labels (PPE requirements, machine status)

- Maintenance zones (lubrication points, electrical access panels)

Facilitator Demonstration Tip

Using actual machines or labelled photographs:

- Point out where each colour appears and explain its purpose

- Ask learners to role-play identifying machine status using colour alone (e.g. “Machine is ready for use” = green button illuminated)

Encourage learners to document the colours used on at least three machines and interpret their meanings.

Activity Suggestion: Safety Colour Code Mapping

Prepare a colour-coded key and give learners a blank machine diagram. They must:

- Use coloured markers or labels to mark where each code should appear

- Annotate with the function (e.g. "Red = Emergency Stop")

- Present their diagrams to the class or small groups

Case Study: Confusion Over Unmarked Controls

In a small joinery shop, a new machine was installed with unlabelled buttons. An operator pressed a red button believing it was the start button, inadvertently activating the emergency shutdown and halting production for 30 minutes. A follow-up audit revealed that colour coding and signage had not been standardised across machines.

Facilitator Prompts:

- What went wrong from a colour coding perspective?

- How could standardised colour usage have prevented confusion?

- What procedures can be implemented during machine commissioning to avoid this?

Critical Thinking Questions

- Why is it dangerous to use colours on control systems that do not follow standard coding conventions?

- How does colour coding contribute to workshop safety in multilingual or fast-paced environments?

- What is the risk of relying only on symbols or text labels without colour differentiation?

- How can learners verify the meaning of a colour or symbol if they are unsure during operation?

- Should organisations be required to document their colour coding systems in SOPs or training manuals? Why or why not?

### PA0408 – Identify the Pneumatic Machines and the Required Pressures

Facilitator Purpose

This session introduces learners to the use of pneumatic (air-powered) machines and tools in the furniture machine shop. Learners will identify commonly used pneumatic equipment, understand how compressed air is delivered and regulated, and recognise the typical operating pressures required for each machine or tool to function effectively and safely.

This competency enables learners to operate pneumatic tools with greater confidence and to interpret gauge readings, pressure ratings, and air supply requirements as part of their workshop routine.

Key Concepts to Cover

1. What is Pneumatics?

- Pneumatics refers to the use of compressed air to drive mechanical motion

- Common in tools and machines that require rapid, repetitive movement

- Compressed air is typically supplied by a central compressor and delivered via hoses, valves, and regulators

2. Common Pneumatic Machines and Tools in Furniture Manufacturing

| Pneumatic Tool or Machine | Function | Typical Operating Pressure |
| --- | --- | --- |
| Nail gun or brad nailer | Fires small nails or brads into timber or panels | 4.5 – 6.0 bar (65 – 90 psi) |
| Staple gun | Drives staples for upholstery or assembly | 5.0 – 7.0 bar (70 – 100 psi) |
| Pneumatic edge banding press | Applies clamping pressure to bond edge strips | 6.0 – 8.0 bar (85 – 115 psi) |
| Clamping systems (presses) | Secures workpieces during laminating or gluing | 6.5 – 8.5 bar (95 – 125 psi) |
| Dust cleaning gun (air blower) | Blows dust off surfaces, machines, tools | 3.0 – 6.0 bar (45 – 85 psi) |
| Random orbital sander (pneumatic) | Used for light to medium surface finishing | 5.5 – 6.5 bar (80 – 95 psi) |

🛈 Note: Pressures may vary by tool and manufacturer. Always check specifications on the label or data sheet.

3. Key Pneumatic System Components

| Component | Function |
| --- | --- |
| Compressor | Generates and stores compressed air |
| Air hose | Delivers compressed air from source to tool |
| Regulator | Controls air pressure going to each tool |
| Gauge | Displays the pressure in the system or line |
| Filter and lubricator | Removes moisture/debris; adds lubrication to extend tool life |
| Quick coupler | Allows tools to be connected or disconnected easily |

Facilitator Demonstration Tip

If available, demonstrate:

- How to connect a pneumatic tool to a hose using a quick coupler

- How to read the pressure gauge and adjust the regulator

- The audible and tactile signs of too high or too low pressure during use

If not available, use photographs or printed diagrams of a pneumatic setup and typical tools.

Activity Suggestion: Pressure Matching Task

Provide learners with a set of laminated tool cards and a chart of operating pressures. Ask them to:

- Match the tool to its correct pressure range

- State what might happen if the pressure is too low or too high

- Identify safety steps before connecting a pneumatic tool

Case Study: Air Leak and Undetected Over-Pressurisation

At a training centre, a staple gun was connected to a compressor running at 9 bar. The regulator was bypassed, causing the staple gun to misfire and jam repeatedly. An instructor later found the hose had a small leak and the gauge was faulty.

Facilitator Prompts:

- What safety and maintenance checks were missed?

- What risks are associated with exceeding a tool’s rated pressure?

- What procedures can ensure pressure settings are always correct?

Critical Thinking Questions

- Why must pneumatic tools never be connected or disconnected while the compressor is under pressure?

- How can incorrect pressure settings impact tool performance and operator safety?

- What routine checks should be performed before and after using a pneumatic machine?

- What are the benefits of using air tools over electric tools in furniture manufacturing?

- What precautions should be taken when using compressed air to clean surfaces or machines?

## Applied Knowledge

Introduction to Applied Knowledge

The applied knowledge associated with this sub-task equips learners with essential theoretical understanding that supports safe, competent, and confident machine operation in the wood machining workshop. It lays the groundwork for identifying and interpreting the purpose, structure, and behaviour of woodworking machines and tools used in operations such as break-out, planing, sanding, and laminating.

A clear understanding of machine types, safety systems, and operational signals ensures that learners not only function effectively within a team-based production environment, but also develop habits that promote precision, responsibility, and injury prevention.

AK0401 – Machines in the Wood Workshop

Learners must be familiar with the range of machines used in the machining department, including stationary and portable equipment. This knowledge includes each machine’s primary function, its core parts and attachments, and its application within the broader furniture manufacturing process.

Learners will also explore the differences between machines used for material preparation (e.g. panel saws, planers), shaping (e.g. routers, spindle moulders), surfacing (e.g. sanders), and assembly preparation (e.g. presses and laminators).

AK0402 – Meaning of Signals, Switches, Alarms, Guides and Gauges

This section ensures learners understand how to interpret the controls and feedback systems integrated into modern woodworking machinery. These include indicator lights, warning alarms, pressure gauges, temperature settings, and digital displays, all of which provide critical information for safe and efficient operation.

The ability to read and respond appropriately to signals and control panel indicators is essential for preventing errors, identifying faults early, and maintaining machine performance.

AK0403 – Safety When Using Machines, Equipment and Tools

This knowledge area reinforces the principles of personal safety, operational safety, and machine safety in the wood machining workshop. It includes:

- Safe handling of sharp tools and moving parts

- The correct use of PPE (personal protective equipment)

- The importance of guards, emergency stops, and proper housekeeping

- Lockout and isolation procedures during maintenance

This applied knowledge supports the learner’s capacity to act responsibly and confidently within a high-risk workshop environment, while also preparing them for further operational training in tool setting, troubleshooting, and production monitoring.

### AK0401 – Machines in the Wood Workshop

Facilitator Purpose

This session provides learners with a broad overview of the key machines used in a wood machining workshop, supporting their ability to recognise, classify, and describe the purpose and function of each type. It enables learners to connect theoretical knowledge of machinery with the practical skills required for cutting, shaping, planing, sanding, and laminating operations.

By the end of this session, learners should be able to name common woodworking machines, explain what each machine does, and understand how they are grouped within the production process.

Key Concepts to Cover

1. Classification of Woodworking Machines by Function

| Function | Machines |
| --- | --- |
| Break-out/Cutting | Panel saw, table saw, radial arm saw, rip saw, cross-cut saw |
| Dimensioning | Surface planer (jointer), thickness planer, combination planer |
| Shaping | Spindle moulder, router, tenoner, mortiser |
| Sanding/Surfacing | Wide belt sander, edge sander, orbital sander, disc sander |
| Laminating/Pressing | Cold press, hot press, edge banding machine, vacuum press |
| Assembly and Joining | Boring machine, dowel inserter, pneumatic clamp systems |
| Finishing and Cleaning | Air blower, dust extractor, spray booth |

2. Descriptions of Key Machines

| Machine | Primary Use |
| --- | --- |
| Panel saw | Breaking down large boards into panels |
| Thickness planer | Reducing boards to consistent thickness |
| Spindle moulder | Creating shaped profiles, rebates, grooves |
| Wide belt sander | Smoothing large flat surfaces evenly |
| Edge bander | Applying and trimming edge tape or strips |
| Cold press | Pressing laminated materials to core boards |
| Boring machine | Drilling precise holes for dowels or cam fittings |
| Mortiser | Cutting rectangular mortises for traditional joinery |

3. Machine Layout and Workflow in the Workshop

- Understand the logical flow: from material preparation to surface finishing

- Machines are often positioned to reduce movement of raw and semi-finished materials

- Consider dust extraction and ventilation points as part of layout planning

- Machinery should be grouped by noise, function, and dust output for safety and efficiency

Facilitator Demonstration Tip

Use printed diagrams or workshop walkthroughs to help learners:

- Identify at least two machines per operation type

- Understand the workflow layout in a typical wood machining area

- Link specific furniture components (e.g. drawer sides, shelves, carcasses) to the machines that shape or finish them

Activity Suggestion: Machine Matching Exercise

Provide learners with a list of furniture parts (e.g. "cabinet side panel," "drawer front," "curved table leg") and a list of machine names. Ask them to:

- Match each part to the appropriate machine

- Briefly explain what the machine would do to that part

Case Study: Poor Machine Selection in Small-Scale Workshop

In a startup workshop, a team attempted to shape a batch of curved chair legs using only a table saw and hand tools. The result was inconsistent, and rework increased due to poor cuts. After investing in a spindle moulder with appropriate tooling, accuracy and speed improved significantly.

Facilitator Prompts:

- Why was the table saw unsuitable for shaping curves?

- How did the use of the correct machine improve product quality?

- What would be the risks of forcing a machine to do a job it was not designed for?

Critical Thinking Questions

- Why is it important to match the machine to the material and job requirements?

- How can the layout of machines in a workshop influence productivity and safety?

- What are the advantages of combination machines in small-scale manufacturing environments?

- Why is machine specialisation (e.g. sanding vs shaping) important in a professional production line?

- How can a learner or junior operator ensure they understand the correct use of each machine before operation?

### AK0402 – Meaning of Signals, Switches, Alarms, Guides and Gauges

Facilitator Purpose

This session is aimed at building learners’ understanding of the control and communication elements on modern woodworking machines. These include signals (lights and sounds), switches (manual and electronic), alarms (warnings and faults), mechanical guides (alignment tools), and gauges (pressure, temperature, depth, or thickness). Mastery of these features is critical for safe, accurate, and efficient operation in a busy machine shop.

Learners will develop the ability to interpret indicators and react appropriately, contributing to improved quality control, reduced downtime, and a strong culture of preventative maintenance.

Key Concepts to Cover

1. Switches and Their Functions

| Type of Switch | Purpose | Where Found |
| --- | --- | --- |
| Start/Stop button | Activates or shuts off the machine | Panel saw, planer, sander, press |
| Emergency stop (E-stop) | Cuts all power immediately in emergency | All machines; must be clearly visible and accessible |
| Mode selector switch | Changes machine between manual, automatic, or set functions | Edge bander, CNC router, presses |
| Reset switch | Clears fault condition or reinitialises a system | Programmable or computerised machines |

2. Signals and Alarms

| Type | Meaning | Example |
| --- | --- | --- |
| Flashing red light | Critical error or machine malfunction | CNC alarm, overheating, jamming |
| Flashing amber/yellow light | Caution – low air pressure, guard open, overheating | Pneumatic systems, presses |
| Green light | Machine is powered and safe to operate | General machine-ready indicator |
| Audible alarm or buzzer | Startup warning or fault condition | Hot press or automated machines |

3. Guides and Their Functions

| Type of Guide | Purpose | Associated Machine |
| --- | --- | --- |
| Fence or guide rail | Keeps workpiece aligned during cutting | Panel saw, rip saw, jointer |
| Mitre guide | Supports angled or cross-cutting | Table saw, cross-cut saw |
| Featherboard or hold-down | Maintains pressure and safety during feeding | Spindle moulder, router table |
| Depth stop | Controls maximum depth of cut or bore | Drill press, mortiser |

4. Gauges and What They Measure

| Type of Gauge | What It Measures | Found On |
| --- | --- | --- |
| Pressure gauge | Air pressure level (typically bar or psi) | Pneumatic clamps, compressors |
| Thickness gauge | Final dimension of planed or sanded material | Thickness planer, wide belt sander |
| Temperature gauge | Surface or internal temperature | Hot presses, varnishing ovens |
| Speed/RPM indicator | Cutting or sanding speed (rotation per minute) | Spindle moulder, drill press, lathe |

Facilitator Demonstration Tip

Set up a machine control panel walk-through with learners:

- Identify and interpret colour-coded indicator lights

- Simulate a fault condition and demonstrate alarm acknowledgement/reset

- Discuss how gauges are monitored during production (e.g. compressor pressure)

- Highlight correct responses to unusual readings or alerts

If machines are not accessible, use photographic or digital diagrams with labels and colour codes.

Activity Suggestion: “Decode the Dashboard” Exercise

Provide a worksheet with a simulated control panel showing:

- A green light, an amber flashing light, and a pressure gauge reading below 4 bar

Ask learners:

- What is the status of the machine?

- Is it safe to operate? Why or why not?

- What action should be taken before proceeding?

Case Study: Ignoring a Panel Warning

An operator noticed a flashing yellow warning on the edge bander indicating low glue pot temperature. Instead of waiting, they fed panels through, resulting in failed edge adhesion and customer complaints. The issue led to a delay in delivery and product rework.

Facilitator Prompts:

- What warning was ignored, and what was the consequence?

- How could proper interpretation of machine signals have prevented the problem?

- What system could be put in place to ensure warnings are always reported?

Critical Thinking Questions

- Why should signals and alarms never be ignored, even if the machine still appears to function?

- What are the risks of misinterpreting a pressure gauge reading on a pneumatic system?

- How do guides and fences contribute to both accuracy and safety?

- What are the advantages of digital over analogue gauges on modern machines?

- Why is it important for all team members to be trained in recognising and responding to control panel signals?

### AK0403 – Safety When Using Machines, Equipment and Tools

Facilitator Purpose

This session provides learners with essential safety principles and best practices for using woodworking machines, handheld tools, and workshop equipment. Emphasising both personal safety and operational safety, the session aims to cultivate an understanding of hazards, the correct use of safety mechanisms, and the importance of personal protective equipment (PPE) and responsible behaviour.

By the end of the session, learners should be able to identify risks, apply preventative measures, and demonstrate consistent safe practices across a range of workshop situations.

Key Concepts to Cover

1. Categories of Safety in the Woodworking Workshop

| Category | Examples |
| --- | --- |
| Personal safety | Wearing PPE, tying back hair, removing jewellery |
| Machine safety | Using guards, emergency stops, lockout/tagout procedures |
| Tool safety | Inspecting before use, using sharp tools correctly, returning tools properly |
| Environmental safety | Keeping walkways clear, good lighting, dust extraction |
| Chemical/material safety | Handling adhesives and finishes correctly, proper storage |

2. Personal Protective Equipment (PPE)

| PPE Item | Purpose |
| --- | --- |
| Safety goggles | Protects eyes from dust, debris, and splinters |
| Dust mask or respirator | Prevents inhalation of wood dust and fumes |
| Hearing protection | Shields ears from high machine noise levels |
| Protective gloves | Protects hands during non-rotating tool handling (avoid near moving blades) |
| Steel-toe safety boots | Protects feet from falling materials or dropped tools |
| Apron or overalls | Keeps clothing close to the body, prevents entanglement |

3. General Machine and Equipment Safety Rules

- Always complete pre-use inspections (blades, guards, switches, wiring)

- Never operate machines without proper training or supervision

- Use push sticks, jigs, or featherboards where needed

- Ensure guards are correctly fitted and never bypassed

- Use machines only for their intended purpose

- Keep hands, clothing, and accessories clear of moving parts

- Do not distract or crowd operators during machine use

- Report all malfunctions or near misses immediately

- Maintain good housekeeping – clean as you go

Facilitator Demonstration Tip

Lead a demonstration (or use visual aids) showing:

- Correct PPE and clothing

- A workstation with a clear vs cluttered layout

- How to use a push stick on a table saw

- Where to find safety signage, emergency stops, and first aid stations

Discuss what constitutes unsafe behaviour, and allow learners to identify hazards in sample workshop photos or staged mock-ups.

Activity Suggestion: "Spot the Hazard" Exercise

Provide printed or projected images of a busy workshop. Ask learners to:

- Identify at least five safety violations or risks

- Explain why they are dangerous

- Suggest the correct behaviour or corrective action

Case Study: Injury Due to Overconfidence and Distraction

A senior learner, confident in using the spindle moulder, began working without a guard to save time and ignored a classmate asking a question mid-cut. The timber snagged, kicked back, and the operator suffered a hand injury. Investigation revealed multiple safety protocols were bypassed.

Facilitator Prompts:

- What critical mistakes led to the injury?

- Why must even experienced operators follow all safety protocols?

- How does distraction affect risk in the machine shop?

Critical Thinking Questions

- Why is it important to wear PPE even for "quick" or "routine" machine tasks?

- What role does mental focus and attentiveness play in machine safety?

- How can unsafe workshop behaviour affect not only the individual but the team?

- What systems should be in place for learners to report unsafe tools or machines?

- Why is good housekeeping a fundamental part of machine and equipment safety?

## 🛠️ Integrated Assessment Task

Assessment Type: Practical Knowledge Integration

NQF Level: 2 Credits: 20

Duration: 60 minutes

Assessment Context: Workshop Simulation or Visual Scenario-Based Assessment

Case Study: Safety and Setup at "Precision Woodworks"

You are completing a work readiness assessment at Precision Woodworks, a training workshop that manufactures modular storage units and study desks. Before you may operate any machinery, your supervisor requires you to conduct a full machine readiness check, including identifying key machine types, control systems, and safety mechanisms.

You are asked to inspect the following:

- A panel saw

- A thickness planer

- A wide belt sander

You must identify the machine types, parts, safety mechanisms, and interpret the control system indicators (lights, switches, and alarms) for each.

Assessment Questions

Question 1
For each of the three machines listed, name the machine, identify two main parts or attachments, and describe the function of each part.

Question 2
List and describe three control system components (e.g. switches, lights, signals) that you may find on the machines listed above. Explain the purpose of each.

Question 3
Identify and describe the purpose of three safety mechanisms found on woodworking machines. Provide one example of how each supports safe operation in the workshop.

✅ Model Answers

Answer 1

Panel Saw

- Blade guard – Covers the blade to prevent operator contact

- Rip fence – Guides the timber along a straight path during cutting

Thickness Planer

- Cutter head – Contains blades that remove material from timber surface

- Height adjustment wheel – Sets the desired thickness by raising or lowering the table

Wide Belt Sander

- Sanding belt – Smooths and finishes the surface of panels

- Conveyor feed belt – Moves the panel through the sanding zone evenly

Answer 2

- Start/Stop button (green/red) – Used to activate or halt machine operation

- Emergency stop button (E-stop) – Cuts all power instantly during emergencies

- Warning light (amber) – Indicates low air pressure, open guard, or fault condition

Answer 3

- Riving knife (panel saw) – Prevents kickback by keeping the cut gap open

- Blade guard (planer, saw) – Prevents accidental contact with moving blades

- Emergency stop button – Allows quick shutdown in dangerous situations

Each mechanism reduces the chance of injury and allows the operator to respond quickly to unexpected machine behaviour.

📝 MARKING MEMO

| Question | Criteria | Marks |
| --- | --- | --- |
| Q1 | 3 machines × (2 parts + 2 functions × 1 mark each) | 12 |
| Q2 | 3 control elements correctly named and described (2 marks each) | 6 |
| Q3 | 3 safety mechanisms identified and explained (2 marks each) | 6 |
|  | Total | 24 |

📊 ASSESSMENT RUBRIC

| Criteria | Outstanding (4) | Competent (3) | Developing (2) | Not Yet Competent (1) |
| --- | --- | --- | --- | --- |
| IAC0401 – Machine parts and function | All machines and parts identified accurately with detailed function descriptions | Most machines and parts identified, functions generally correct | Some errors in part names or unclear functional descriptions | Incorrect machine or part names and functions missing |
| IAC0402 – Control system interpretation | All controls correctly identified with accurate purpose explained | Most controls and purposes correct, minor interpretation errors | Incomplete or partially correct descriptions of control system elements | Unable to identify or explain basic controls and indicators |
| IAC0403 – Safety mechanisms | All mechanisms clearly identified with examples of how they prevent injury | Most mechanisms and examples relevant | Limited understanding of how mechanisms function or protect users | Lacks understanding of common safety systems and their purpose |

### Facilitator Assessment Briefing

Practical Module: PM-01 – Operate a Range of Machines in the Wood Machine Shop to Cut Components for Furniture Manufacturing

Sub-task: PM-01-PS04 – Identify a Range of Machines, Machine Parts, Machine Attachments and Tools in the Furniture Machine Shop

Assessment Type: Integrated Practical Knowledge Assessment

Internal Assessment Criteria:

- IAC0401: The different machines operating in the machine shop are correctly identified along with their parts and their functions

- IAC0402: All switches, lights and signals on the panel board or control system are correctly identified and interpreted

- IAC0403: The safety mechanisms on the various machines in the machine shop are correctly identified in order to ensure they are functioning properly

Purpose of the Assessment

The purpose of this integrated assessment is to evaluate the learner’s ability to identify machines and their parts, interpret operational signals and controls, and understand the safety mechanisms essential for safe and effective use of woodworking equipment. The learner’s understanding of these aspects is foundational for subsequent machining tasks, tool setup, and workshop safety.

This assessment also builds toward readiness for the External Integrated Summative Assessment (EISA).

Assessment Context

This assessment is based on a realistic machine readiness check in a furniture manufacturing workshop. The learner must demonstrate an understanding of machine functions, parts, control systems, and safety features across three types of equipment commonly found in the machining department.

The task supports both theory and practical interpretation, aligned to the learning environment and operational procedures of South African wood machining workshops.

Facilitator Instructions

- Read through the case study and confirm learner understanding

- Ensure visual or physical access to machine control panels and safety mechanisms where possible (images or practical workshop)

- Learners must complete the task individually under classroom conditions

- Use the model answers, marking memo, and rubric provided to assess learner performance

- Provide written or verbal feedback, and allow for remediation where gaps are identified

## PM-01-PS05: Apply Safety Measures Related to the Machine Operation and Work Area

1. Introduction to the Practical Skill

This sub-task is designed to instil in learners the importance of workplace safety as an ongoing, active responsibility. Learners will learn how to set up machines and work areas safely, make use of appropriate personal protective clothing (PPC) and personal protective equipment (PPE), and identify potential hazards and risks associated with machine operation in a furniture manufacturing environment.

This unit reinforces the principle that safety is not an isolated activity, but one that is embedded in all machine-related tasks. Learners will be taught to recognise workplace safety notices and hazard signs, operate within marked zones, and maintain a tidy, organised, and risk-aware environment.

It supports both individual safety and collective responsibility for the safety of others in the workshop.

2. Scope of Practical Skill

Given access to a range of machines and tools in the machine shop, the learner must be able to:

- PA0501 Set up the machine to ensure that the work area will be safe and efficient

- PA0502 Use the correct PPC and PPE for the given situation and machine

- PA0503 Identify hazards and risks related to the operation and machine

3. Applied Knowledge

- AK0501 Understanding of safety notices, colour coding and demarcation lines

- AK0502 Personal protective equipment

4. Internal Assessment Criteria

- IAC0501 Different notices in the work area are identified and adhered to

- IAC0502 Work is performed within the demarcated area

- IAC0503 Work is performed without creating hazards for self and that of others and safety rules and practices are adhered to at all times

### PA0501 – Set Up the Machine to Ensure That the Work Area Will Be Safe and Efficient

Facilitator Purpose

This session enables learners to understand and apply the principles of safe and efficient machine setup. Learners are introduced to a structured checklist approach to machine preparation, including checks for machine readiness, area cleanliness, proper tool mounting, safety mechanisms, and material positioning.

A correctly prepared machine and workspace reduce the likelihood of injury, tool damage, or production errors, and reinforce professional conduct within the shared workshop environment.

Key Concepts to Cover

1. What Is Meant by “Machine Setup” in a Safety Context?

- Preparing the machine to operate correctly and safely

- Ensuring safety mechanisms are in place and functional

- Verifying that tools, blades, and accessories are installed securely

- Checking alignment, fences, cutting depth, and feed systems

- Clearing the area of offcuts, spills, or obstructions

- Confirming access to emergency stop controls

- Ensuring that dust extraction systems are active

2. Step-by-Step Machine Setup for Safety and Efficiency

| Step | Purpose |
| --- | --- |
| Inspect machine and surroundings | Ensure machine is clean, undamaged, and workspace is clear |
| Check power source and cables | Avoid tripping or electrical hazards |
| Confirm guards and safety features | Ensure riving knife, blade guard, emergency stop are in place |
| Set fences, guides, and stops | Align for accurate and safe material feed |
| Mount tool bits/blades securely | Prevent dislodgement or imbalance during use |
| Test operation without material | Confirm smooth operation and correct feed settings |

3. Efficient Layout of the Work Area

- Materials should be within reach but not on the machine table

- Toolboxes and accessories must be neatly arranged and away from paths

- Offcuts should be placed in designated bins, not on the floor

- Ensure clear entry/exit around large machines such as panel saws and presses

- Good lighting and visibility should be prioritised

Facilitator Demonstration Tip

Perform a live or simulated demonstration of:

- A machine setup checklist

- A pre-use inspection, including loose part detection

- Setting up fences or guides for a standard cut

- What a poor setup looks like (e.g. clutter, misalignment, missing guard)

Encourage learners to perform a mock setup using a checklist and evaluate one another in pairs.

Activity Suggestion: Machine Setup Readiness Audit

Divide learners into small groups. Assign each a machine or workstation and ask them to:

- Complete a setup readiness checklist

- Identify any hazards or inefficiencies

- Present their findings and proposed corrections to the class

Case Study: Productivity Loss Due to Unsafe Setup

A learner in a production training session forgot to secure the fence on a panel saw before use. During the first cut, the board shifted, resulting in a poor-quality cut and minor kickback. The machine had to be shut down for inspection, halting production for 30 minutes.

Facilitator Prompts:

- What setup steps were missed?

- What safety risks arose?

- How did this impact productivity and workshop flow?

Critical Thinking Questions

- Why is it important to run a machine briefly before introducing any material?

- What might happen if the blade or bit is not secured properly before operation?

- How can poor work area layout contribute to accidents, even if the machine is correctly set up?

- What checklist items would you include in a daily machine setup form?

- How does an efficient work area improve not just safety, but also productivity and accuracy?

### PA0502 – Use the Correct PPC and PPE for the Given Situation and Machine

Facilitator Purpose

This session equips learners with the ability to select and correctly use personal protective clothing (PPC) and personal protective equipment (PPE) based on the nature of the task, the machine involved, and the potential hazards present. A key objective is to promote a safety-first mindset and to ensure that all learners understand why different items of protective gear are required for specific machines and materials.

Learners will also be taught how to inspect, maintain, and store PPE to ensure it remains effective and compliant with health and safety regulations.

Key Concepts to Cover

1. Difference Between PPC and PPE

| PPC – Personal Protective Clothing | PPE – Personal Protective Equipment |
| --- | --- |
| Clothing that is worn to protect the body | Equipment that protects specific parts of the body |
| Includes overalls, safety boots, gloves | Includes goggles, hearing protection, respirators |
| Often prevents entanglement or exposure | Designed to shield against mechanical, chemical or airborne hazards |

2. Typical PPC and PPE for Woodworking Machines

| Machine | Required PPC and PPE |
| --- | --- |
| Panel saw | Safety boots, overalls, hearing protection, safety glasses |
| Spindle moulder | Dust mask, safety goggles, non-loose clothing, push sticks |
| Thickness planer | Safety boots, ear protection, push blocks, overalls |
| Edge bander | Heat-resistant gloves (if near hot glue system), safety glasses, apron |
| Wide belt sander | Dust mask or respirator, ear plugs, safety shoes, goggles |
| Air-powered nailer | Eye protection, gloves, ear protection, secure footwear |

🛈 Always remove rings, watches, scarves, or other accessories that could be caught in moving parts.

3. Selection of PPE Based on Risk Assessment

Learners must understand how to:

- Identify the hazard (e.g. dust, noise, heat, sharp blades)

- Match the correct PPE to protect against that hazard

- Check whether PPE is in good working condition and fits correctly

- Ensure PPE is stored in a clean, dry location when not in use

Facilitator Demonstration Tip

Display a full PPC and PPE kit at the front of the class. Include:

- Different types of gloves (rubber, heat-resistant, cut-resistant)

- Types of safety glasses (impact-resistant, dust-sealed)

- Examples of clean vs damaged PPE (scratched goggles, worn gloves)

Demonstrate correct fitting and allow learners to practise donning and doffing PPE safely.

Activity Suggestion: Match the Machine to the PPE

Provide a worksheet or cards showing different machines and separate cards showing PPE items. Learners must:

- Match each machine to the required PPC and PPE

- Justify their choices based on identified risks

- Present in small groups for discussion

Case Study: Injury from Inappropriate Footwear

A learner operating a thickness planer wore slip-on shoes without steel toe protection. When a board fell off the outfeed table, it struck the learner’s foot, causing a minor injury. The workshop supervisor found that the learner had not checked the PPE list on the wall.

Facilitator Prompts:

- What PPE was required, and why?

- How could the injury have been prevented?

- What system should be in place to remind learners of PPE requirements?

Critical Thinking Questions

- Why is hearing protection essential when working near multiple operating machines?

- What are the dangers of wearing loose clothing or jewellery in a machine shop?

- How can poorly maintained PPE become a safety risk in itself?

- What steps should you take if the required PPE for a task is missing or damaged?

- Why is it important to match PPE not just to the machine, but also to the specific material being processed (e.g. dusty chipboard vs clean timber)?

### PA0503 – Identify Hazards and Risks Related to the Operation and Machine

Facilitator Purpose

This session enables learners to develop situational awareness and the ability to identify potential hazards and risks associated with woodworking machinery, tools, and processes. By learning to assess their environment and actions, learners will be better prepared to prevent incidents, respond to unsafe conditions, and maintain a culture of accountability and caution in the workshop.

This competency also supports learners in making sound decisions about machine readiness, workspace layout, and operational behaviour.

Key Concepts to Cover

1. Definitions

| Term | Explanation |
| --- | --- |
| Hazard | A source of potential harm or adverse health effect (e.g. exposed blade) |
| Risk | The likelihood that a person may be harmed by a hazard and the severity of harm |

2. Types of Hazards in the Machine Shop

| Hazard Type | Examples |
| --- | --- |
| Mechanical hazards | Moving blades, rotating parts, unguarded cutters |
| Electrical hazards | Damaged cords, uninsulated wiring, overloaded circuits |
| Dust and fume hazards | Fine dust from sanding, adhesive fumes, spray booth vapours |
| Noise hazards | Exposure to loud machinery without protection |
| Ergonomic hazards | Repetitive motion, awkward postures, heavy lifting without assistance |
| Slip/trip hazards | Sawdust buildup, oil spills, offcuts left on the floor |
| Sharp object hazards | Chisels, broken blades, exposed screws or nails |

3. How to Identify Hazards and Assess Risks

Learners should be taught to:

- Conduct visual inspections of the machine and surrounding area

- Check for missing guards, leaks, damaged tools, or unlabelled switches

- Use a hazard checklist when setting up the work area

- Rate the likelihood and severity of each risk using a simple colour-coded or numeric scale

- Understand the hierarchy of controls (eliminate, substitute, isolate, engineer, administrate, PPE)

Facilitator Demonstration Tip

Use real examples or images from your own workshop or catalogue:

- Highlight a machine with the guard removed or PPE missing

- Present two photos: one of a safe workstation, one with obvious hazards

- Ask learners to compare and list all possible risks in the unsafe example

Activity Suggestion: Hazard Identification Challenge

Divide learners into teams and assign each a different workshop zone (e.g. cutting area, sanding area, glue station). Ask them to:

- List potential hazards in that area

- Suggest what could be done to reduce or eliminate each hazard

- Present their findings with a basic risk matrix

Case Study: Ignored Trip Hazard Causes Injury

During a busy shift in a college workshop, a power cable was left trailing across the sanding station. A learner carrying a board tripped, dropped the board onto another machine, and sprained their wrist in the fall. Investigation revealed that the hazard had been noted earlier but not reported.

Facilitator Prompts:

- What type of hazard is this?

- Who was responsible for correcting it?

- How could reporting and communication procedures be improved?

Critical Thinking Questions

- Why is it important to identify both visible and hidden hazards before starting work?

- How can good housekeeping reduce both physical and ergonomic risks?

- Why should hazards be reported immediately, even if no one has yet been hurt?

- What is the role of peer accountability in maintaining a safe working environment?

- How can risk assessment be used as a planning tool, not just a compliance task?

## Applied Knowledge

Introduction to Applied Knowledge

The applied knowledge linked to this sub-task reinforces the learner’s understanding of workplace safety principles, particularly in relation to visual safety communication systems and the correct use of personal protective equipment (PPE) in the furniture manufacturing environment. This theoretical grounding is essential for preparing learners to identify, interpret, and respond appropriately to safety-related instructions and environmental indicators.

Together, these knowledge components support proactive decision-making, hazard prevention, and full alignment with industry safety protocols and regulatory compliance expectations.

AK0501 – Understanding of Safety Notices, Colour Coding and Demarcation Lines

Learners must be able to recognise and interpret standard safety signage, colour codes, and floor demarcation lines used throughout the machine shop to communicate hazard areas, machine zones, safety instructions, and emergency controls. These systems form the visual language of workshop safety and are often the first layer of risk mitigation.

Learners will explore the meaning and correct responses to:

- Mandatory signs (blue): “Wear hearing protection,” “Safety goggles required”

- Warning signs (yellow): “Caution – moving machinery,” “Trip hazard”

- Prohibition signs (red): “No entry,” “Do not use”

- Demarcation lines on floors or around machines to indicate safe working distances, isolation zones, or storage areas

This knowledge enables learners to operate confidently and responsibly in visually coded environments.

AK0502 – Personal Protective Equipment

This section covers the types, functions, and proper use of PPE in the woodworking context. Learners will gain an understanding of when and how to use safety glasses, gloves, masks, hearing protection, protective footwear, and other essential items based on task risk assessment and machine type.

Key focus areas include:

- Matching PPE to the task and identified hazard (e.g. goggles for flying debris, dust masks for sanding)

- Ensuring correct fit and condition of PPE

- Understanding limitations of PPE (e.g. gloves are not always safe near rotating blades)

- Responsibility for care, storage, and reporting of damaged PPE

Through this knowledge, learners are empowered to take personal responsibility for their health and safety, and to contribute to a culture of shared safety in the workplace.

### AK0501 – Understanding of Safety Notices, Colour Coding and Demarcation Lines

Facilitator Purpose

This session introduces learners to the standardised safety symbols, colours, signage, and demarcation practices used in machine shops and manufacturing environments. These visual elements form a critical part of health and safety systems, enabling both quick recognition of risks and prompt compliance with safety instructions.

Understanding and correctly responding to these visual cues is essential for ensuring personal safety, preventing incidents, and maintaining a safe and orderly workplace.

Key Concepts to Cover

1. Safety Notices and Their Classifications

| Type of Notice | Colour | Meaning | Examples |
| --- | --- | --- | --- |
| Mandatory Signs | Blue | Actions that must be taken | "Wear safety glasses", "Use ear protection" |
| Warning Signs | Yellow | Hazards that may cause injury or danger | "Caution: rotating blade", "Slippery when wet" |
| Prohibition Signs | Red | Actions that are not allowed | "Do not use machine", "No unauthorised access" |
| Emergency Signs | Green | Indicates emergency exits or equipment | "First aid", "Emergency stop", "Fire exit" |

All signage must use clear symbols, be visible at eye level, and be positioned close to the relevant hazard or action zone.

2. Colour Coding on Machines and in Workspaces

| Colour | Meaning |
| --- | --- |
| Red | Emergency stop, fire equipment, danger |
| Green | Safe conditions, normal operation, emergency exits |
| Yellow | Caution, moving parts, pinch points |
| Blue | Mandatory actions (e.g. PPE required) |
| Orange | High-risk rotating components |
| Black/White | General instructional or layout markings |

Colour coding enhances visibility and reduces reliance on written text, making it inclusive for multilingual workforces.

3. Demarcation Lines in the Workshop

| Demarcation | Purpose |
| --- | --- |
| Floor markings (yellow) | Define safe walking paths, caution zones around machines |
| Red tape or paint | Denotes fire equipment access zones – must be kept clear |
| Striped tape (black/yellow) | Highlights hazardous areas or moving machinery boundaries |
| Blue areas | PPE zones or mandatory instruction areas |
| Green lines | Emergency routes or safe escape paths |

These markings are part of 5S and OHS visual management systems.

Facilitator Demonstration Tip

Display real-life workshop photos or visit the actual shop floor. Ask learners to:

- Identify the signs or markings

- State what each one indicates

- Explain the correct behaviour or action in response

Bring printed examples of each sign for tactile learning. You can also create a floor map poster showing demarcation lines and safety zones.

Activity Suggestion: Safety Sign Identification Quiz

Create a set of flashcards or a digital slideshow:

- Show a symbol (e.g. yellow triangle with exclamation mark)

- Ask learners to name it, explain what it means, and state the appropriate response

- Bonus round: Learners draw their own sign based on a described risk scenario

Case Study: Ignored Safety Sign Results in Minor Injury

In a training centre, a learner entered a no-access zone to retrieve a tool from behind a panel saw. A "Do Not Enter – Machine in Operation" sign was clearly posted, but ignored. The saw operator had to stop mid-cut, and the learner’s presence caused confusion, leading to a dropped board and a bruised hand.

Facilitator Prompts:

- What type of sign was ignored?

- What risks were introduced by this behaviour?

- How can workshops reinforce compliance with posted signage?

Critical Thinking Questions

- Why is colour coding especially important in loud or fast-paced environments?

- How do demarcation lines help prevent both accidents and production delays?

- What steps can a workshop take to ensure signage remains visible and effective?

- What should a worker do if they notice damaged or missing safety signage?

- Why is it important that all workers, regardless of language or reading level, understand safety signals and markings?

### AK0502 – Personal Protective Equipment

Facilitator Purpose

This session develops learners’ understanding of the types, functions, limitations, and responsibilities related to personal protective equipment (PPE) in the furniture manufacturing workshop. By acquiring this knowledge, learners will be able to make informed choices about which PPE to use for different machines and operations, ensure correct usage and maintenance, and comply with health and safety regulations.

This knowledge component is closely aligned with the learner’s practical responsibilities in operating safely and preventing both personal injury and workplace incidents.

Key Concepts to Cover

1. What is Personal Protective Equipment (PPE)?

PPE refers to equipment and clothing specifically designed to protect the wearer from injury or exposure to hazards in the workplace. It is a last line of defence when risks cannot be fully eliminated through engineering or administrative controls.

2. Types of PPE in the Woodworking Workshop

| PPE Item | Protects Against | Typical Use |
| --- | --- | --- |
| Safety goggles | Flying debris, dust, splinters | Cutting, sanding, routing |
| Dust mask or respirator | Inhalation of fine dust, fumes from adhesives | Sanding, spray finishing, board processing |
| Hearing protection | High noise levels from machines | Use of saws, planers, presses, and edge banders |
| Protective gloves | Splinters, sharp edges, contact with chemicals | Handling raw timber, cleaning, glue application |
| Steel-toe safety boots | Foot injuries from falling tools or materials | General use throughout workshop |
| Overalls/aprons | Clothing entanglement, minor abrasions | All machine-related activities |

🛈 Note: Gloves should not be worn when operating machines with rotating parts unless specifically designed for the task.

3. Proper Use and Limitations of PPE

- PPE must be correctly fitted, adjusted, and worn throughout the task

- Learners should be taught to inspect PPE before each use for damage or wear

- PPE must be cleaned and stored properly after use to ensure hygiene and longevity

- PPE is not a substitute for unsafe behaviour – it must be used in conjunction with safe practices

- Learners must report missing or damaged PPE immediately to a supervisor

Facilitator Demonstration Tip

Lay out a complete PPE station with:

- Clean and damaged items side by side

- Demonstrate proper wearing techniques (e.g. sealing a mask, adjusting goggles)

- Ask learners to identify the PPE that would be appropriate for:

  - Cutting a melamine board

  - Using a spray adhesive

  - Operating a spindle moulder

Activity Suggestion: PPE Scenario Matching

Present learners with a variety of workshop scenarios. For each one, they must:

- Identify the risks involved

- Select the PPE required

- Briefly explain how each item offers protection

Example scenario: "You are sanding MDF panels for a cabinet project."
Expected PPE: Dust mask, safety goggles, ear plugs, protective clothing.

Case Study: Consequence of Improper PPE Use

During a routine day, a learner chose not to wear ear plugs while using a wide belt sander. Over time, the learner began experiencing ringing in the ears and difficulty focusing. A medical check-up confirmed early signs of noise-induced hearing loss. The workshop had posted signage and provided ear protection, but it was not enforced.

Facilitator Prompts:

- What PPE was required, and why?

- Who bears responsibility – the learner or the supervisor?

- How can workshops promote PPE compliance without policing behaviour?

Critical Thinking Questions

- What are the consequences of wearing the wrong type of PPE for a specific hazard?

- Why is PPE considered a “last line of defence” in the hierarchy of hazard control?

- What procedures should be followed if a learner notices that PPE is damaged or missing?

- How can workshops create a culture where wearing PPE becomes second nature?

- What are the limitations of PPE, and how should workers compensate for them through behaviour and awareness?

## Integrated Assessment Task

Assessment Type: Integrated Practical Knowledge Assessment

NQF Level: 2

Credits: 20

Assessment Context: Practical Simulation Based on Workshop Safety Protocols

Case Study: Morning Setup at Cedar Designs Workshop

You are beginning your shift in the machining area at Cedar Designs, where your responsibilities include operating a panel saw and supporting the setup of a wide belt sander. Before starting work, you are required to complete a standard safety walk-through and machine readiness check.

The workshop includes:

- Demarcated machine zones with yellow lines

- Blue PPE signage posted at various stations

- Red prohibition signs at restricted areas

- Fire equipment and emergency exits marked in green and red zones

During your checks, you observe:

- One co-worker is working outside a marked area

- A warning sign is partially covered by a jacket

- Offcuts are left on the floor beside the sander

You are asked to report and correct the situation using standard workshop procedures.

Assessment Questions

Question 1
List and describe three different types of safety notices or signs you observed or would expect to see in a woodworking machine shop. Explain how each sign supports workplace safety.

Question 2
What is the purpose of demarcated areas in the workshop, and how should a machine operator behave within them?

Question 3
Based on the case study, describe three safety violations that could lead to hazards. Explain how each should be corrected to maintain a safe working environment.

✅ MODEL ANSWERS

Answer 1

- Blue mandatory sign – "Wear hearing protection": Reminds users of required PPE before operating loud machines

- Red prohibition sign – "No unauthorised access": Prevents entry into high-risk or restricted zones

- Yellow warning sign – "Caution: moving machinery": Alerts operators and others to potential mechanical hazards

Answer 2

Demarcated areas define safe working zones around machines. They ensure that:

- Operators have adequate space to work safely

- Other workers remain at a safe distance from moving machinery

- Materials and tools are kept clear of walkways and operating zones

Operators must stay within the lines, keep the area tidy, and monitor for obstructions.

Answer 3

- Working outside marked area – May lead to interference with machine operation or injury. Correction: Reposition the workstation or alert the co-worker and supervisor.

- Covered safety sign – Prevents others from seeing critical information. Correction: Remove the obstruction and report it to maintenance if signage is faded or damaged.

- Offcuts on floor – Slip/trip hazard near machine. Correction: Clear immediately and use designated offcut bins.

📝 Marking Memo

| Question | Criteria | Marks |
| --- | --- | --- |
| Q1 | 3 correct types of signs + explanation of purpose (2 marks each) | 6 |
| Q2 | Clear explanation of demarcation purpose and correct behaviour | 6 |
| Q3 | 3 violations correctly identified and addressed (2 marks each) | 6 |
|  | Total | 18 |

📊 Assessment Rubric

| Criteria | Outstanding (4) | Competent (3) | Developing (2) | Not Yet Competent (1) |
| --- | --- | --- | --- | --- |
| IAC0501 – Safety Notices | Identifies all signs accurately with clear explanations of their function | Most signs identified with general understanding | Limited understanding; some sign types confused | Fails to identify sign types or interpret their meaning |
| IAC0502 – Demarcated Areas | Fully understands function and models correct in-zone behaviour | Understands basic rules and boundaries | Aware of zones but unclear on best practices | No awareness or incorrect assumptions about marked areas |
| IAC0503 – Workplace Hazards | Identifies and explains multiple risks with solutions | Recognises most hazards and proposes reasonable corrections | Identifies basic risks; lacks depth in recommendations | Fails to identify hazards or misinterprets basic safety concepts |

### Facilitator Assessment Briefing

Practical Module: PM-01 – Operate a Range of Machines in the Wood Machine Shop to Cut Components for Furniture Manufacturing

Sub-task: PM-01-PS05 – Apply Safety Measures Related to the Machine Operation and Work Area

Assessment Type: Integrated Practical Knowledge Assessment

Internal Assessment Criteria:

- IAC0501: Different notices in the work area are identified and adhered to

- IAC0502: Work is performed within the demarcated area

- IAC0503: Work is performed without creating hazards for self and that of others and safety rules and practices are adhered to at all times

Purpose of the Assessment

The purpose of this assessment is to determine the learner’s ability to operate safely within a wood machining environment by demonstrating knowledge of visual safety communication, physical boundaries, and acceptable behaviour in high-risk areas. Learners must show that they understand the function of safety signage and demarcation systems, and that they can apply best practices when working near and with machinery.

This competency supports compliance with occupational health and safety (OHS) regulations and underpins every other practical operation in the furniture manufacturing process.

Assessment Context

The assessment is based on a practical case study involving a standard daily setup in a real-world workshop scenario. Learners will be required to interpret signage, assess and correct safety violations, and demonstrate a responsible approach to working within designated machine zones.

Facilitator Instructions

- Present the case study and confirm learner understanding of the scenario

- Encourage discussion and clarification of terms such as signage, demarcation, and risk

- Learners must complete the task individually and in writing

- Assess learner responses using the provided model answers, marking memo, and assessment rubric

- Provide feedback and remediation if learners do not fully meet the requirements

## PM-01-PS06: Prepare for Machine Operations

1. Introduction to the Practical Skill

This sub-task prepares learners to carry out all preliminary activities required to operate woodworking machines safely and accurately. It focuses on equipping learners with the competencies to interpret cutting lists, select materials and tooling, adjust machine settings, conduct safety and operational checks, and carry out minor tool maintenance such as changing blades or belts.

By mastering these preparatory steps, learners will ensure that machines are correctly set up, materials are handled responsibly, and safety protocols are observed. This task is foundational to efficient machining operations and helps minimise production errors, equipment wear, and workplace hazards.

2. Scope of Practical Skill

Given a cutting list/job card, material samples, timber, and access to a range of woodworking machines, the learner must be able to:

- PA0601 Read and understand the cutting list/job card and sample

- PA0602 Select the correct timber indicated on the cutting list/job card

- PA0603 Select knives, saws, blades, cutter heads, cams, bits, or belts according to the workpiece, machine function, or product specifications

- PA0604 Fit the correct tool to the machine or verify that the correct tooling and sanding belts are already installed

- PA0605 Set machine speeds (blade or tool rotation) based on the type of material

- PA0606 Conduct pre-start-up checks, including sound tests, guard inspections, and test cuts

- PA0607 Conduct safety checks

- PA0608 Inspect the machine to confirm it is operational

- PA0609 Inspect blades and cutting tools for sharpness and correct fitting

- PA0610 Replace blades or belts after a specified number of components are completed

3. Applied Knowledge

- AK0601 Different measuring equipment

- AK0602 Angles and degrees

- AK0603 Basic calculations

4. Internal Assessment Criteria

- IAC0601 Different measuring equipment are used to measure timber, such as measuring tapes and vernier callipers

- IAC0602 The machine is set and ready for operation and all foreign objects are removed from the machine

- IAC0603 The raw material is inspected for grain direction, type (board or solid), and defects

- IAC0604 Waste control is exercised while cutting material to eliminate fire hazards

- IAC0605 Basic calculations are applied in order to obtain the right number and size of components

- IAC0606 Machine problems are identified and minor problems are resolved while those outside the operator's control are reported via the correct communication channels

### PA0601 – Read and Understand the Cutting List/Job Card and Sample

Facilitator Purpose

This session introduces learners to the critical first step in any machining task: reading and interpreting a cutting list or job card and comparing it to a physical sample, if provided. This task ensures that learners understand how to extract and apply production specifications, such as dimensions, material type, quantities, grain direction, and machining requirements, before setting up or operating any equipment.

This competency supports effective planning, material optimisation, and the prevention of errors, thereby laying the foundation for high-quality furniture production.

Key Concepts to Cover

1. What is a Cutting List / Job Card?

- A document that specifies the components required to build a product

- Includes dimensions (length × width × thickness), material type, quantity, and machine instructions

- Often includes special notes such as edge banding, grain direction, or laminate requirements

- May be accompanied by a sample component or drawing for reference

2. Key Elements Learners Must Identify

| Information to Extract | Why It Matters |
| --- | --- |
| Component names | Clarifies the purpose (e.g. "shelf", "drawer side") |
| Dimensions | Ensures correct sizing for machine setup |
| Material type | Informs correct tool selection (e.g. pine vs MDF) |
| Quantity required | Affects board usage and batch cutting strategy |
| Grain direction | Important for aesthetics and structural integrity |
| Special notes | May affect speed, tooling, or additional processes |

Facilitator Demonstration Tip

Show learners:

- A sample cutting list and job card, real or simulated

- A panel or timber piece labelled with a sticker referencing the job card

- How to highlight key instructions (e.g. a different blade needed for chipboard vs solid wood)

You may use a printed sample to explain:

- How to cross-reference dimensions with a tape measure

- What happens when the wrong material is selected or grain direction is ignored

Activity Suggestion: Cutting List Decoding Exercise

Provide learners with a simplified cutting list and a mock timber rack containing:

- Several labelled pieces of board/timber with dimensions and types

Ask them to:

- Identify the correct timber based on the job card

- Measure and confirm that the sizes match

- Check grain direction and note any additional requirements

Case Study: Mistake Due to Misreading the Cutting List

A learner read the job card and selected 18 mm chipboard instead of 16 mm melamine for a set of drawer bottoms. This caused the assembled drawers to jam in the cabinet carcass. The material had to be re-cut, and the workshop fell behind on delivery.

Facilitator Prompts:

- What key instruction was missed?

- How could the mistake have been avoided?

- What effect did this error have on cost, time, and customer satisfaction?

Critical Thinking Questions

- What should you do if you do not understand an abbreviation or instruction on the job card?

- How does accurate interpretation of grain direction support both aesthetics and strength in furniture?

- Why is it important to cross-check the number of pieces before starting machine setup?

- What risks are introduced if the wrong material is selected?

- How can using a sample component help you verify accuracy before machining all parts?

### PA0602 – Select the Correct Timber Indicated on the Cutting List/Job Card

Facilitator Purpose

This session teaches learners how to accurately select timber or board materials based on a given cutting list or job card. Material selection affects everything from tool wear and machine settings to furniture durability, appearance, and cost-efficiency. Learners must be able to identify timber species, board types, and sizes, and cross-check this information against specifications before proceeding with machine setup or cutting.

Correct selection ensures that the right material is used for the right component, preventing mismatches, material wastage, and assembly issues.

Key Concepts to Cover

1. Types of Timber and Board Used in Furniture Manufacturing

| Category | Examples | Characteristics |
| --- | --- | --- |
| Solid Timber | Pine, Meranti, Kiaat, Oak | Strong, used for frames, tops, legs |
| Composite Boards | MDF, chipboard, melamine-faced chipboard | Uniform thickness, affordable, used for carcasses, panels |
| Plywood | Laminated veneers | Durable, stable, used for drawer bottoms, panels |
| Veneer Boards | MDF or chipboard with wood veneer | Combines surface appeal with cost-efficiency |

2. Material Properties That Influence Selection

| Property | Why It Matters |
| --- | --- |
| Thickness | Affects cutting list accuracy, edge treatment, joinery fit |
| Board type | Impacts blade selection, tool wear, and finish quality |
| Grain direction | Affects aesthetics, machining direction, and structural integrity |
| Surface finish | Determines whether sealing, painting, or edge banding is required |
| Defects (for solid wood) | Cracks, warping, knots – must be avoided for strength |

3. Material Selection Procedures

- Read the job card carefully to identify material name, thickness, and quantity

- Inspect timber rack or board storage area for correct labels and markings

- Measure dimensions using a measuring tape or calliper

- Check the surface for defects (splits, bubbles, moisture damage)

- Confirm that grain direction matches job card or sample

- Record or tag selected material as part of production tracking (where applicable)

Facilitator Demonstration Tip

Provide examples of:

- Correct and incorrect material choices for specific components

- Real samples of pine, chipboard, MDF, and veneer board

- A job card with different materials listed and ask learners to “go fetch” the correct timber from a mock storage setup

Demonstrate how to:

- Identify grain direction

- Match surface finishes

- Use visual labels and physical measurements to confirm accuracy

Activity Suggestion: Timber Selection Task

Set up a simulated timber rack with:

- A mix of labelled and unlabelled timber/board

- A cutting list for a small cabinet

Ask learners to:

- Select the correct material for each component

- Identify the matching board/timber

- Explain how they confirmed their selection

Case Study: Material Misuse in Drawer Construction

In a training session, a learner selected MDF instead of plywood for the base of a drawer unit. During assembly, the base flexed under load and detached. The error was traced back to a rushed selection process where the learner had not cross-referenced the material name on the job card.

Facilitator Prompts:

- Why was MDF a poor choice for this application?

- What simple check could have prevented this error?

- How would the error impact the end-user and product warranty?

Critical Thinking Questions

- What should you do if the correct material is not available on the shelf?

- Why is it risky to use thicker or thinner boards than those specified?

- How can incorrect grain direction affect machining and product strength?

- What are the potential cost implications of using the wrong timber or board?

- How can quality control systems help prevent material selection errors?

### PA0603 – Select Knives, Saws, Blades, Cutter Heads, Cams, Bits, or Belts According to the Workpiece, Machine Function, or Product Specifications

Facilitator Purpose

This session equips learners with the knowledge and skills to identify and select the appropriate cutting or sanding tool for a given task. Tool selection depends on several factors, including the machine being used, the material being processed, and the desired final product. Correct tool selection improves surface finish, minimises machine wear, ensures safety, and aligns with the product's design specifications.

Learners will be introduced to the main types of cutting and abrasive tools used in woodworking, and guided through how to match them to different machines and materials.

Key Concepts to Cover

1. Overview of Tooling Types

| Tooling Category | Examples | Typical Machine |
| --- | --- | --- |
| Saw blades | Crosscut, rip, combination, melamine blade | Panel saw, table saw |
| Cutter heads | Straight knives, profile cutters, rebate heads | Spindle moulder, surface planer |
| Router bits | Straight, round-over, dovetail | Handheld or table-mounted routers |
| Drill bits / boring heads | Brad point, Forstner, dowel boring bits | Drill press, multi-boring machine |
| Knives | Thicknesser or planer knives | Thickness planer, jointer |
| Sanding belts | 80–240 grit belts, open vs closed coat | Wide belt sander, edge sander |
| Cams and form tools | Specialised shaping attachments for repetition | CNC or shaping machines |

2. Factors Affecting Tool Selection

| Factor | Why It Matters |
| --- | --- |
| Material type | Hard vs soft wood, composite board – affects sharpness, wear, tooth design |
| Machine function | Sawing, planing, profiling, boring – each requires different mounting and geometry |
| Finish requirements | Fine finishing needs finer grit or sharp profile cutters |
| Safety considerations | Wrong tool can jam, break, or cause kickback |
| Production volume | Carbide-tipped tools may be selected for longer runs |

3. Tool Selection Procedures

- Review the job card for specifications

- Identify the machine and material type

- Consult tool catalogue or workshop chart if uncertain

- Inspect tool condition (sharpness, wear, correct size)

- Confirm mounting type and compatibility with the machine

- Request supervisor authorisation for specialised or high-risk tooling

Facilitator Demonstration Tip

Display a range of:

- Blades, knives, bits, and sanding belts

- Label them and describe their appropriate application

- Pass around dull vs sharp tools for learners to physically inspect

Show how the wrong tool (e.g. a rip blade on a melamine board) causes chipping, overheating, or poor cut quality.

Activity Suggestion: Tooling Match-Up

Provide task cards with short machining scenarios:

- “Edge profiling MDF board for cabinet doors”

- “Boring 5 mm dowel holes for shelf support”

- “Planing pine to 22 mm thickness”

Ask learners to:

- Choose the correct tool from a set of images or actual tools

- Justify their choice by explaining the tool’s function and suitability

Case Study: Tooling Mismatch Leads to Safety Incident

A learner selected a fine-tooth blade designed for cross-cutting melamine to cut through a solid oak plank. The blade began to bind, overheated, and ultimately warped during the cut. The machine had to be shut down and the blade replaced. Investigation revealed the blade had been selected without checking the job card.

Facilitator Prompts:

- What were the technical reasons this blade failed?

- What visual or audible signs indicated a problem?

- What should the learner have done before installation?

Critical Thinking Questions

- What are the risks of using a dull blade or bit during high-speed cutting?

- How does the tool type influence surface finish and machining accuracy?

- Why is it important to match the sanding belt grit to both the material and the stage of finishing?

- What steps should be taken if the required tooling is missing or damaged?

- How can a workshop’s tooling reference chart or system assist with rapid, correct selections?

### PA0604 – Fit the Correct Tool to the Machine or Check If the Correct Tool and/or Sanding Belts Are Installed

Facilitator Purpose

This session equips learners with the practical skills and knowledge to fit or verify the correct installation of tooling and sanding belts on woodworking machines. Safe and accurate tool installation is essential to protect the operator, maintain machine performance, and ensure the quality of the machined components.

Learners must be able to follow the correct procedures when mounting blades, knives, belts, cutter heads, or bits, and also be trained to visually and physically check that the installed tooling matches the job requirements, is in good condition, and is correctly aligned and secured.

Key Concepts to Cover

1. Types of Tooling to Be Fitted or Checked

| Tooling/Component | Associated Machine | Mounting Considerations |
| --- | --- | --- |
| Saw blade | Panel saw, table saw | Direction of rotation, locking nut torque, tooth type |
| Cutter head | Spindle moulder, surface planer | Secure seating, knife alignment, correct cutter profile |
| Router bit | Router table or handheld router | Shank depth, collet size, proper tightening |
| Planer/thicknesser knives | Thickness planer, jointer | Even blade projection, balancing, safety blocks |
| Sanding belts | Wide belt sander, edge sander | Belt tracking, tension, grit specification |
| Drill/boring bit | Drill press, boring machine | Centring, depth stop setting, clamping |

2. Fitting Procedure (General Steps)

- Isolate the machine using lock-out procedure (power off and tagged)

- Remove the existing tool if necessary, using appropriate spanners or tool keys

- Clean mounting surfaces to remove dust and debris

- Insert the new tool or belt, aligning with arrows/rotation direction

- Secure fasteners (e.g. tightening flange nut or locking bolts)

- Check alignment and clearance from fences, guards, or tables

- Reattach all guards and safety covers before restoring power

- Perform a dry run to ensure the tool is secure and runs smoothly

🛈 Where tools are pre-installed (e.g. sanders in production mode), learners must verify that tooling type, grit, and condition match the job card.

3. Visual and Operational Checks for Installed Tooling

| Check | Why It’s Important |
| --- | --- |
| Rotation arrow matches machine | Prevents cutting against grain or kickback |
| Blade is clean and undamaged | Dull or chipped tools reduce quality and safety |
| Belt tension and tracking | Prevents belt slippage or side wear |
| Fasteners are properly torqued | Reduces risk of tool ejection during use |
| Tool matches job card spec | Avoids mismatched cuts, overcuts, or product rejection |

Facilitator Demonstration Tip

Using decommissioned machines or demo kits:

- Demonstrate how to safely remove and replace a saw blade or sanding belt

- Show how to align the blade with rotation markings

- Highlight common fitting errors, such as over-tightening or misaligned inserts

- Emphasise safe use of hand tools when working on blades and cutter heads

Activity Suggestion: Tool Inspection and Verification Drill

Present learners with:

- A job card specifying tooling type

- A selection of installed machines or tool trays
Ask them to:

- Verify if the installed tool matches the job card

- Inspect for defects or incorrect fitment

- Record their findings on a “Tool Fitment Checklist”

Case Study: Loose Router Bit Causes Machine Damage

A learner failed to fully insert a router bit into the collet of a handheld router. The bit became loose during operation, causing vibration, damaging the board, and leaving a gouge on the router table. The supervisor noted the absence of a pre-check before operation.

Facilitator Prompts:

- What step was missed in the fitting process?

- How could the learner have confirmed correct tool installation?

- What are the safety implications of a loose or unbalanced tool?

Critical Thinking Questions

- Why must power always be isolated before changing tooling or belts?

- What signs might indicate a poorly mounted or unbalanced blade or belt during startup?

- What safety risks arise if a belt or bit is used beyond its wear limit?

- What should you do if a tool appears to be the wrong type for the job card?

- How can a workshop track the number of cuts or hours on a tool to know when to replace it?

### PA0605 – Set Machine Speeds (Rotation of the Blade) According to the Type of Material

Facilitator Purpose

This session teaches learners how to correctly adjust machine speed settings—specifically the rotational speed of blades, cutters, or sanding belts—based on the type and condition of material being processed. Correct speed settings help prevent burning, chipping, tear-out, premature tool wear, and safety risks. Learners must be able to interpret job card specifications, understand the machine’s speed adjustment mechanisms, and make appropriate adjustments in accordance with manufacturer guidelines.

Key Concepts to Cover

1. What Is Meant by Blade or Cutter Speed?

- Speed is usually measured in revolutions per minute (RPM)

- Affects how fast the tool rotates and interacts with the material

- Impacts cutting quality, surface finish, tool life, and safety

2. Factors That Influence the Required Speed Setting

| Factor | Recommended Action |
| --- | --- |
| Material type | Hardwoods = slower speed; Softwoods = moderate speed; MDF = adjusted carefully to avoid burn or fraying |
| Tool type and diameter | Larger blades or cutters = lower RPM; small bits = higher RPM |
| Feed rate and depth of cut | Deeper cuts = lower speed or multiple passes |
| Surface finish required | High finish = correct balance between speed and feed rate |
| Heat sensitivity | Composite boards may burn/melt if speed is too high |

3. Machine Examples and Speed Controls

| Machine | Speed Control Method | Notes |
| --- | --- | --- |
| Spindle moulder | Manual pulley adjustment or variable speed drive | Must match cutter diameter to spindle speed |
| Router (handheld/table) | Adjustable dial or electronic setting | Bit size must be considered when adjusting |
| Wide belt sander | Feed speed + belt rotation speed control | Must align with grit and board material |
| Panel saw | Often fixed, but some models have gear settings | Match blade to material rather than speed |
| Drill press | Pulley-driven adjustment | Slower for hardwoods or large bits |

🛈 Learners should always refer to tooling charts, machine labels, or supervisor guidance before changing speed settings.

Facilitator Demonstration Tip

Use a speed chart for common woodworking machines. Demonstrate:

- Adjusting spindle or router speed for hardwood vs softwood

- The sound and behaviour of an under-speed or over-speed tool

- Burn marks on wood from incorrect speed settings

- Proper use of a test piece to confirm adjustment before full production

Activity Suggestion: Speed Setting Chart Application

Provide learners with:

- A chart showing recommended RPM for various tools/materials

- A set of job cards with details like “Cutting melamine-faced chipboard with a 300 mm blade”
Ask learners to:

- Select the correct RPM range

- Explain their reasoning

- Identify which machine controls would be used to set that speed

Case Study: Burn Marks on Veneered Panel

During a production run, a learner set the feed speed too slowly and the spindle speed too high when routing a veneered MDF panel. The heat caused scorching and surface bubbling. Several panels were damaged before the cause was identified.

Facilitator Prompts:

- What combination of factors led to the burn?

- What changes could be made to resolve it?

- Why is it important to run a test piece before batch machining?

Critical Thinking Questions

- What are the risks of setting the machine speed too high for the material?

- How can incorrect speeds affect the quality and consistency of components?

- What could happen to the machine or tooling if a large diameter cutter is run too fast?

- How does the speed setting relate to safety, especially when using older or worn tools?

- Why is it important to record or log speed settings for recurring jobs in a production environment?

### PA0606 – Conduct Pre-Start-Up Checks

Facilitator Purpose

This session equips learners with the knowledge and habits required to carry out structured safety and operational checks before starting any machine. Pre-start-up checks are essential for identifying potential hazards, confirming that the machine is correctly set, and ensuring that safety systems are in place and functioning.

Learners will be introduced to a standardised checklist approach, and will practise confirming machine condition, tooling alignment, safety features, and readiness through test runs before starting production.

Key Concepts to Cover

1. Why Are Pre-Start-Up Checks Necessary?

- Prevents accidents or damage due to loose tools, missing guards, or faulty wiring

- Ensures that machine adjustments and speeds are correct for the material

- Confirms safety mechanisms are in working order

- Detects early signs of mechanical or electrical failure

- Verifies a clean, clear, and safe work area

2. Typical Pre-Start-Up Checklist Items

| Check Item | What to Look For |
| --- | --- |
| Visual inspection | No visible damage, wear, or loose parts |
| Clean work area | No offcuts, spills, or tools near the machine base |
| Blade or tool alignment and tightness | Secure fitment, correct height/angle for cut |
| Guard and riving knife in place | Blade fully enclosed, no removed covers |
| Emergency stop function | Press to test; machine should cut power instantly |
| Noise test | No unusual vibrations, whines, or grinding sounds on startup |
| Trial run with test piece | Confirm cut depth, finish quality, speed settings |
| Dust extraction engaged | Confirm suction is active and correctly positioned |

3. When and How to Perform Checks

- Before every shift and after tool changes or machine adjustments

- Use a printed or laminated machine-specific checklist

- Involve a second person or supervisor for new operators or critical jobs

- Log and report any issues that are outside the operator’s ability to resolve

Facilitator Demonstration Tip

Perform a live walk-through at a machine (or use a large poster/photo if machinery is unavailable). Demonstrate:

- The difference between a machine that is “ready” vs one that is not

- How to test an emergency stop

- The purpose of a test piece (use offcut boards for realism)

- How to listen for unusual sounds and what they might indicate

Distribute a sample pre-start checklist that learners can use in their future assessments.

Activity Suggestion: Pre-Start Checklist Simulation

Assign learners to groups and give each:

- A mock machine inspection form

- A case scenario (e.g. tool was just changed, new operator on duty)
Ask them to:

- Conduct a simulated pre-start-up inspection

- Record their findings

- Decide whether the machine is safe to start or not

Case Study: Injury Due to Missed Pre-Start Check

A learner failed to run a test piece after changing the blade on a table saw. The new blade was incorrectly tightened, causing it to wobble and kick the first workpiece back toward the operator. No one was injured, but the material and blade were damaged.

Facilitator Prompts:

- What pre-start check would have revealed this problem?

- How could a test piece have helped prevent damage?

- Why is it important to never assume a machine is safe after maintenance?

Critical Thinking Questions

- Why is it risky to skip the noise or vibration test before production begins?

- How does a simple visual check contribute to preventing serious injury?

- What steps can a workshop take to ensure learners do not forget pre-start checks?

- How does a test piece help confirm correct machine setup?

- Who is responsible for identifying and reporting problems found during pre-start checks?

### PA0607 – Conduct Safety Checks

Facilitator Purpose

This session teaches learners how to systematically inspect and confirm safety conditions before and during machine operation. Unlike pre-start-up checks which focus on operational readiness, safety checks are broader and ongoing, ensuring that the work environment, tools, materials, and operator conduct remain compliant with health and safety regulations throughout the work session.

Learners will develop the habit of conducting routine safety checks that help to identify and eliminate potential hazards before they cause harm.

Key Concepts to Cover

1. What Are Safety Checks?

Safety checks are inspections conducted to:

- Confirm safety mechanisms are working correctly

- Ensure all protective equipment and guards are in use

- Assess the work area, machine, and operator behaviour for risks

- Identify trip hazards, fire hazards, sharp objects, or exposed electricals

2. Common Safety Checkpoints in a Machine Shop

| Safety Check Area | What to Check |
| --- | --- |
| Machine safeguards | Blade guards, riving knives, cutter head enclosures, interlocks |
| Emergency controls | Emergency stop button clearly marked and functioning |
| PPE compliance | Learner and team wearing appropriate PPE (goggles, masks, etc.) |
| Cables and power supply | No exposed wires, cords secured away from walkways |
| Dust extraction | Active and unobstructed, bags emptied if full |
| Fire safety | Fire extinguisher accessible and zone kept clear |
| Floor and pathways | Free of spills, sawdust, offcuts, and clutter |
| Lighting and visibility | Adequate lighting at all workstations |

3. Frequency and Responsibility

- Safety checks should be done:

  - Before using a machine

  - After long pauses or material changes

  - When a potential risk is noticed

- Learners should be taught that safety is everyone's responsibility – issues must be reported, even if they seem minor

Facilitator Demonstration Tip

Prepare a “safe” vs “unsafe” station setup. Show learners:

- A properly guarded machine with tidy work area vs one with cables, spills, or open blades

- How to simulate a functional safety check using a laminated checklist

- How to test an emergency stop or shut-off valve

- Encourage discussion around what may appear safe but is actually risky (e.g. loose clothing, blocked e-stop)

Activity Suggestion: Hazard Flagging Exercise

Create a workshop mock-up or image set with 10+ safety scenarios (some correct, some unsafe). Ask learners to:

- Identify at least five safety risks

- Record them on a safety report form

- Propose a corrective action for each

Case Study: Slipping Incident Due to Ignored Safety Check

During a sanding operation, a learner slipped on a patch of sawdust left under the edge sander. The machine had been running for several hours, but no one had swept the area or checked underfoot. The learner twisted their ankle and was unable to continue working for two weeks.

Facilitator Prompts:

- What safety checks should have been in place?

- How can cleanliness and visibility affect safety?

- What system could be used to ensure these risks are caught early?

Critical Thinking Questions

- What are the potential risks of ignoring minor issues like a partially blocked dust extraction hose?

- How do regular safety checks protect both the operator and the machine?

- What actions should be taken if safety issues are discovered during operation?

- Why is it important for safety checks to be documented and communicated clearly?

- How can safety checks be embedded into daily workshop routines without slowing down production?

Facilitator Notes: PA0608 – Inspect the Machine is Operational

Facilitator Purpose

This session teaches learners how to confirm that a woodworking machine is fully operational before, during, and immediately after startup. The focus is on recognising the indicators of machine readiness, identifying abnormalities early, and applying logical steps to either resolve or report issues.

This forms part of a broader culture of preventative maintenance and operational safety, contributing to longer machine lifespan, consistent production quality, and reduced downtime.

Key Concepts to Cover

1. What Does “Operational” Mean in this Context?

A machine is considered operational when:

- It starts, runs, and shuts down correctly and safely

- No error indicators or unusual sounds are present

- All functions and movements perform as intended

- Tooling is secure, and no vibrations or resistance are observed

- Safety mechanisms are intact and functioning

2. Key Indicators That a Machine Is Operational

| Inspection Point | What to Check |
| --- | --- |
| Startup sequence | Machine powers on smoothly; control lights are green or steady |
| Running sound | Smooth, consistent hum; no rattling, screeching, or grinding |
| Movement and feed | Material moves cleanly through the machine without jamming |
| Dust extraction | Suction is active and aligned; no dust build-up or clogging |
| Tooling stability | No wobbling, rattling, or flexing from blades or cutters |
| Control response | Speed, height, or direction controls work as expected |
| Emergency system | Emergency stop button immediately halts operation when pressed |

3. Actions if the Machine Is Not Operational

- Do not continue operation if a fault is suspected

- Log the issue in a maintenance report form

- Inform the supervisor or technical personnel immediately

- Place a “Do Not Use” tag on the machine where applicable

- Never attempt internal repairs unless trained and authorised

Facilitator Demonstration Tip

Show two conditions side by side:

- A “ready” machine: starts up cleanly, aligned, all guards in place

- A “faulty” machine: unplugged hose, wobbling cutter head, flickering control panel

Let learners practise:

- Identifying signs of proper function

- Describing “what’s wrong” when faults are present

- Completing a sample operational inspection checklist

Activity Suggestion: Operational Checklist Simulation

Provide each group of learners with:

- A visual (photo or actual machine)

- A mock inspection sheet

- A task to evaluate whether the machine is operational and what to do if it is not

They must:

- Mark “Pass” or “Fail” per category

- Describe any corrective or reporting actions needed

Case Study: Production Delay Due to Ignored Operational Fault

A wide belt sander began producing uneven sanding results. A slight belt misalignment was visible, but the operator ignored it. After a few boards were damaged, the machine was stopped, revealing the belt was nearly torn. Maintenance was called, and the machine was out of service for two days.

Facilitator Prompts:

- What were the early warning signs?

- What step should have been taken as soon as the fault was noticed?

- How might a quick inspection have saved time and material?

Critical Thinking Questions

- Why should even small operational abnormalities (e.g. noise, belt drift) be investigated immediately?

- What are the consequences of continuing production on a machine that is not fully functional?

- What signs indicate that a machine may be unsafe to operate, even if it starts?

- Why should learners never attempt to ‘fix’ machines themselves unless qualified?

- What systems should be in place to track and respond to operational faults?

### PA0609 – Inspect Blade and Cutting Tools for Sharpness and Correct Blade and Belts

Facilitator Purpose

This session teaches learners how to conduct a thorough inspection of cutting blades, knives, belts, and sanding tools to determine whether they are sharp, safe, and suitable for the task at hand. Maintaining sharp, correctly installed tools is essential for accurate machining, operator safety, efficient workflow, and material conservation.

Learners will be guided through the process of identifying dull or damaged tooling, understanding the consequences of using incorrect or worn tools, and reporting or replacing them as part of standard operational procedure.

Key Concepts to Cover

1. Why Blade and Belt Inspections Matter

- Sharp tools ensure smooth cuts, reduce material damage, and minimise strain on machines

- Dull or damaged blades can burn wood, cause kickback, tear material, and create inconsistent finishes

- Incorrect or worn belts can affect sanding quality, tracking, and increase the risk of tearing

- Routine inspection helps prevent accidents, rework, and downtime

2. What to Look for During Inspection

| Tool Type | What to Inspect |
| --- | --- |
| Saw blades | Missing or chipped teeth, warping, build-up of resin or dust |
| Knives and cutters | Dull edges, nicks, uneven wear, loose mounting screws |
| Router bits | Blunt edges, rust, incorrect shank size or depth |
| Sanding belts | Worn abrasive, tears, fraying edges, tracking issues |
| Belts (drive belts) | Cracking, stretching, frayed or delaminated edges |

3. How to Conduct the Inspection

- Isolate the machine – power off, lock out if necessary

- Remove guards safely and expose tooling area

- Use gloves and a torch to check condition without direct hand contact

- Rotate tooling slowly by hand (if applicable) to inspect full edge

- Check that the installed blade or belt type matches the job card

- Record findings in a machine inspection log

- Report damaged or dull tools immediately or replace if authorised

🛈 Always use a test piece after blade inspection to confirm smooth operation and cut quality.

Facilitator Demonstration Tip

Display actual or simulated:

- Sharp vs dull blades

- Used vs fresh sanding belts

- Use magnifiers or high-quality close-up photos to help learners visualise wear and damage

Allow learners to feel the difference (safely) and practice rotating tooling slowly to check for defects. Emphasise the importance of lighting and attention to detail.

Activity Suggestion: Blade and Belt Fault Identification

Set up a display board or tool tray with:

- A mix of correctly maintained and worn blades/belts
Ask learners to:

- Sort the tools into “ready to use” vs “requires replacement”

- Justify their reasoning for each choice

- Suggest what should be done with the worn item (e.g. sharpen, discard, log)

Case Study: Cabinet Door Chipping Due to Worn Blade

A batch of melamine-faced doors was cut using a dull combination blade that hadn’t been replaced in time. The result was chipped edges and visible surface tearing. The problem was only discovered during quality control, leading to expensive rework and material loss.

Facilitator Prompts:

- What signs of wear might have been detected during inspection?

- What should the operator have done before using the blade?

- How can blade replacement be planned more proactively?

Critical Thinking Questions

- Why is using a dull or damaged blade a safety hazard as well as a quality concern?

- What could happen if sanding belts are worn or incorrectly tensioned during use?

- How often should blades and belts be inspected – and by whom?

- What systems can help workshops monitor the life cycle of cutting tools?

- What is the relationship between tool sharpness and fire risk in woodworking machines?

### PA0610 – Replace the Blade or Belts After Specific Number of Components Are Completed

Facilitator Purpose

This session enables learners to understand when and how to replace worn blades or belts based on usage tracking, component count, and visible tool wear. Learners will explore how the tool’s lifespan correlates with production volume, material type, and machine workload, and how replacing tools at the correct time prevents damage to both the machine and the product.

This practical skill is an important part of workshop routines, ensuring that the cutting or sanding tools perform optimally, that finished products meet quality standards, and that safety risks are minimised.

Key Concepts to Cover

1. Why Scheduled Replacement Matters

- Maintains cutting/sanding quality and consistency

- Reduces the risk of tool breakage or machine strain

- Prevents damage to high-value materials or components

- Ensures that tool wear does not compromise production targets or deadlines

- Supports fire prevention and machine health

2. Determining When Replacement Is Required

| Trigger for Replacement | Explanation |
| --- | --- |
| Number of components produced | Tooling manufacturers or workshop standards define maximum usage (e.g. after 500 cuts) |
| Visual inspection | Dull edges, burning marks, frayed belts, excessive dust build-up |
| Sound and performance indicators | Vibration, squealing, reduced feed speed, tearing or chipping |
| Scheduled maintenance logs | Each machine should have a tracking sheet or digital log for tool changes |

3. Replacement Procedure Overview

- Power off and isolate the machine using the lockout procedure

- Remove the worn blade or belt using appropriate spanners or tools

- Inspect the tool mount for dust, resin build-up, or signs of damage

- Install the new blade or belt, ensuring correct orientation and tension

- Check that guards are replaced and tooling is secure

- Run a test cut or sanding operation to confirm correct function

- Record the replacement in the maintenance logbook or digital system

Facilitator Demonstration Tip

Use a board or slideshow to show:

- A blade or belt “before and after” a full production cycle

- Manufacturer guidelines (e.g. “this blade is rated for 1 000 linear metres of board”)

- Demonstrate logging replacement using a tracking sheet

If possible, show how a fresh blade cuts more smoothly and with less resistance than a worn one.

Activity Suggestion: Tool Lifespan Scenario Exercise

Give each learner or group:

- A task card with: "Cutting 300 cabinet sides from MDF using a 60-tooth TCT blade"

- Blade lifespan info (e.g. “Good for 600–800 cuts depending on density”)
Ask learners to:

- Estimate when the blade should be changed

- Explain what signs might prompt an earlier change

- Describe the correct replacement and logging procedure

Case Study: Production Halt Due to Belt Failure

A belt on the wide belt sander was not replaced after 900 boards, despite the manufacturer recommending replacement at 800. During a large batch run, the belt tore, damaging the panel mid-sanding and halting production. The incident delayed delivery by two days and increased scrap material costs.

Facilitator Prompts:

- What could have been done differently?

- How can workshops keep track of tool lifespan more effectively?

- What is the cost-benefit of replacing tooling before it fails?

Critical Thinking Questions

- What are the consequences of running a blade or sanding belt beyond its intended lifespan?

- How can a component-counting system be used to trigger preventative maintenance?

- What safety risks increase when a blade or belt is not replaced in time?

- How can learners ensure accurate recordkeeping for tool replacements?

- Why is it important to confirm tool performance with a test piece after replacement?

## Applied Knowledge

This applied knowledge supports the practical skill of preparing for machine operations. It focuses on developing a learner’s ability to use precision measurement tools, understand angles and degrees as they relate to component shaping, and apply basic calculations to interpret cutting lists, determine quantities, and ensure dimensional accuracy. These foundational skills are essential for ensuring product consistency, material efficiency, and quality control in a woodworking machine shop environment.

AK0601 – Different Measuring Equipment

Learners must understand the purpose and correct usage of various measuring tools used in furniture manufacturing. These include:

- Measuring tapes: For general length and width measurements

- Steel rules: For straight, short measurements with greater accuracy

- Set squares and combination squares: For marking and checking 90° and 45° angles

- Calipers (vernier and digital): For precise thickness or internal/external measurements

- Marking gauges: For scoring repeatable lines along or across the grain

Competence in selecting and using these tools ensures that all machine setup and component cutting adheres to specified dimensions and tolerances.

AK0602 – Angles and Degrees

Understanding angles and degrees is crucial when preparing machines for:

- Bevelled cuts, mitres, or angled joints

- Adjusting fences, tilting tables, and cutter heads

- Ensuring visual symmetry and structural integrity in finished products

Learners must be able to read angle indicators on machines and tools, such as mitre gauges, angle finders, and bevel protractors, and apply this information during both setup and inspection.

AK0603 – Basic Calculations

Basic arithmetic is essential for:

- Converting units (e.g. mm to cm)

- Calculating quantities (e.g. total components from a board)

- Determining allowances for blade kerf or sanding losses

- Working with fractions and decimals on cutting lists

- Ensuring material optimisation and waste reduction

Calculations may include simple addition, subtraction, multiplication, and division, as well as understanding percentages for tolerance or ratios for scaled drawings.

This applied knowledge enables learners to interpret technical information accurately and perform confidently in precision-based machining tasks.

### AK0601 – Different Measuring Equipment

Facilitator Purpose

This session develops learners’ familiarity with the range of measuring tools used in a wood machining workshop, and builds the competency to select the correct equipment for specific measurements during preparation, machine setup, and verification of component dimensions.

Learners must understand how to use, read, and care for these tools to ensure consistent accuracy, quality, and safety in all operations.

Key Concepts to Cover

1. Common Measuring Tools in the Workshop

| Measuring Tool | Purpose | Typical Application |
| --- | --- | --- |
| Measuring tape | General measurement of length and width | Sizing timber, panels, verifying cut dimensions |
| Steel rule | Straight, short, precise measurements | Marking lines, setting depths |
| Set square / try square | Checking or marking 90° angles | Ensuring square edges and joints |
| Combination square | Measuring and marking both 90° and 45° angles | Mitres, framing components |
| Vernier calliper (or digital) | Measuring thickness, diameters, depth | Blade thickness, board calibration, internal gaps |
| Marking gauge | Scribing consistent parallel lines along timber grain | Dado cuts, grooves, edge positioning |
| Measuring wheel | For longer distances or curved components | Large frame layouts or templates |

2. Best Practices for Measuring

- Zero the tool before use (especially vernier callipers)

- Always measure from the same reference face (datum)

- Use firm but gentle pressure – avoid compressing soft materials

- Double-check critical measurements

- Record measurements neatly and consistently

- Clean measuring tools after use and store in a dry, protected place

3. Reading Scales and Increments

- Emphasise millimetre precision, as most cutting lists in woodworking use mm

- Demonstrate how to read metric vernier callipers and digital equivalents

- Explain when to use fractions vs decimals, depending on machine setting formats

- Teach learners to identify kerf allowance (blade thickness) in length calculations

Facilitator Demonstration Tip

Display real or mock versions of:

- Measuring tapes, rules, set squares, and callipers

- Show learners how to:

  - Calibrate and read vernier callipers

  - Check whether a component is square

  - Measure board thickness and length precisely

  - Scribe lines for cutting or drilling

Let learners handle each tool and practise reading or marking with guidance.

Activity Suggestion: Tool Selection and Accuracy Task

Create a mini practical challenge:

- Provide various materials (e.g. board offcuts, metal bar, dowels)

- Give learners measurement tasks (e.g. measure diameter, mark a 45° mitre)

- Ask learners to:

  - Select the correct tool

  - Perform the measurement

  - Record the result and explain their tool choice

Case Study: Incorrect Board Fit Due to Measuring Error

A learner cut four cabinet dividers using a measuring tape and incorrectly read the 580 mm line as 560 mm. The boards were too short to fit into the pre-drilled carcass and could not be used.

Facilitator Prompts:

- What tool could have prevented this error?

- How can the learner ensure accuracy before cutting?

- Why is consistent measurement essential in mass production?

Critical Thinking Questions

- What measuring tool would you use to check the depth of a groove cut into a shelf?

- Why is it important to measure both the material and the sample before starting a cut?

- What are the risks of using a damaged or stretched measuring tape?

- How can a marking gauge help improve consistency in repeated cuts?

- When is it appropriate to use a calliper rather than a tape measure?

### AK0602 – Angles and Degrees

Facilitator Purpose

This session introduces learners to the concepts of angles and degrees, which are essential in preparing components for mitres, bevels, chamfers, joints, and other geometrically defined operations. Understanding how to measure and apply angles accurately ensures that components fit correctly and align as designed, both structurally and aesthetically.

Learners will explore how angles relate to machine adjustments, cutting layouts, and drawing interpretation, enabling them to set machines and mark workpieces with greater precision and confidence.

Key Concepts to Cover

1. What Is an Angle?

- An angle is the space between two intersecting lines, measured in degrees (°)

- In woodworking, common angles include:

  - 90° (right angle)

  - 45° (common for mitre joints)

  - 30°, 60°, and 120° for decorative or structural purposes

2. Common Applications of Angles in Furniture Making

| Application | Angle Used | Purpose |
| --- | --- | --- |
| Mitre joints | 45° | Used for picture frames, carcass corners, plinths |
| Bevelled edges | Variable (15°–60°) | Softens edges, adds style or reduces sharp corners |
| Compound angles | Two angles simultaneously | For angled cabinet fronts or custom joinery |
| Chamfers and tapers | Often 30°–60° | Applied to legs, frames, trims |
| Shelving joints | Can use 60°/120° for hexagonal layouts | Speciality furniture or modular shelving |

3. Measuring and Marking Angles

| Tool | Use |
| --- | --- |
| Protractor | Measures and marks specific angles on timber |
| Combination square | Allows for quick 45° and 90° marking |
| Sliding bevel (bevel gauge) | Transfers existing angles from a sample or drawing |
| Mitre gauge (machine accessory) | Guides timber through saws at specific angles |
| Digital angle finder | Used for precise machine setup and blade tilt adjustments |

🛈 Most machines (e.g. mitre saws, spindle moulders, panel saws) have angle indicators that must be read and adjusted accurately.

Facilitator Demonstration Tip

Use a whiteboard or angle blocks to:

- Show the difference between common angles (e.g. 30°, 45°, 60°, 90°)

- Demonstrate how a sliding bevel can capture and transfer a non-standard angle

- Show learners how to set a machine mitre gauge to a specific angle

- Provide physical offcuts or templates for learners to compare and measure

Activity Suggestion: Angle Layout and Matching

Give each learner:

- A drawing with 3–4 angles marked (e.g. frame corner, shelf brace, chamfer edge)

- Offcut pieces of board
Ask them to:

- Measure and mark the angle on the timber using the correct tool

- Label the angle (e.g. “45° mitre”)

- Match or transfer an angle from one piece to another using a bevel gauge

Case Study: Inaccurate Mitre Causes Visible Gap

During assembly of a veneered cabinet frame, a mitre corner left a 3 mm gap. The cut was made using a table saw set at 47°, instead of the correct 45°, due to a misread dial. The frame had to be recut, and the incorrect piece was scrapped.

Facilitator Prompts:

- What tool or method could have verified the correct angle setting?

- How would a test cut have prevented the error?

- Why is even a small angular error visually noticeable in mitres?

Critical Thinking Questions

- Why must a saw blade or fence be set at the exact angle specified on the job card?

- What tool would you use to copy an angle from a sample and apply it to a new board?

- How can understanding degrees help in both machine setup and quality inspection?

- What could happen if angles are measured in inches or fractions instead of degrees in a metric system workshop?

- Why is consistency across all angles important in batch production (e.g. making six identical drawer fronts)?

### AK0603 – Basic Calculations

Facilitator Purpose

This session introduces learners to the essential mathematical skills required in wood machining and component preparation. While woodworking often relies on hands-on accuracy, effective planning, waste reduction, and compliance with specifications all depend on the learner’s ability to perform basic arithmetic, unit conversions, and practical reasoning related to quantities, sizes, and tolerances.

Mastering these calculations supports confident decision-making in reading job cards, setting out components, preparing material quantities, and troubleshooting measurement discrepancies.

Key Concepts to Cover

1. Arithmetic for Furniture Machining

| Calculation Type | Example | Application |
| --- | --- | --- |
| Addition/Subtraction | 450 mm + 550 mm = 1000 mm | Total component lengths; working within board size |
| Multiplication/Division | 8 shelves × 500 mm = 4000 mm total | Material required per job or number of cuts per sheet |
| Unit Conversion | 2.4 m = 2400 mm | Interpreting job cards and tool settings |
| Allowances | Subtracting kerf (e.g. 3 mm per cut) | Accurate layout on boards |
| Percentage/Waste | 10% trimming loss on 1000 mm = 100 mm | Factoring in offcuts and tolerance in yield planning |

2. Workshop Examples Where Calculations Are Required

- Working out how many components can be cut from a board

- Determining how much edging or laminate is needed for a unit

- Calculating spacing for bore holes or dowels

- Estimating time or cost per component in planning stages

- Converting fractions to decimals (e.g. ½ inch = 12.7 mm) when tools or guides are in different systems

3. Decimal and Fraction Usage

| Decimal | Fraction | Common Application |
| --- | --- | --- |
| 0.5 | ½ | Thickness settings, blade height |
| 0.25 | ¼ | Groove width, tolerance on edge fitting |
| 0.75 | ¾ | Board widths, panel overlays |

🛈 Learners should be taught to round to the nearest whole mm unless the machine or tool allows for finer calibration.

Facilitator Demonstration Tip

- Use a cutting list and sample board size (e.g. 2750 mm × 1830 mm melamine) to calculate how many parts of a certain size can be cut

- Demonstrate using a calculator or layout sheet to plan cuts

- Show how ignoring kerf width can cause sizing errors in mass production

Activity Suggestion: Workshop Calculation Task

Give learners a worksheet with:

- A list of components (e.g. “12 × 450 mm × 300 mm drawer fronts”)

- A board size

- A task to:

  - Calculate how many parts fit on the board

  - Determine leftover material or number of boards required

  - Convert between mm and cm as needed

Case Study: Inaccurate Yield Estimate Causes Material Shortage

During preparation for a small production batch, a learner miscalculated the number of shelves that could be cut from a sheet of melamine by failing to account for the 3 mm saw blade kerf. The result was one fewer shelf per board than expected. The batch was delayed while more material was sourced.

Facilitator Prompts:

- What was the mathematical error?

- How could it have been avoided?

- What does this tell us about the importance of including blade width in planning?

Critical Thinking Questions

- How can incorrect decimal rounding affect the fit of machine-cut components?

- Why is it important to calculate waste percentages in production planning?

- How can you estimate the number of cuts a blade will make based on component length and board size?

- What is the risk of failing to convert measurements correctly between metres and millimetres?

- Why is mathematical accuracy just as important as manual skill in the machining department?

## Integrated Assessment Task

Assessment Type: Practical Knowledge Application

NQF Level: 2 Credits: 20

Assessment Context: Simulated or real workshop environment using job card, tools, and machinery

Case Study: Preparing for Production at Woodline Designs

You are working in the machining department of Woodline Designs, preparing materials for a batch of bedside cabinets. You receive a cutting list and job card that includes dimensions, quantities, and timber specifications. Your responsibility is to prepare and inspect the material, complete machine setup, and perform test cuts safely and efficiently.

The materials include:

- 16 mm melamine-faced chipboard for carcass panels

- 22 mm solid pine for drawer fronts

- The board size is 2750 mm × 1830 mm

- The blade kerf is 3 mm

- 20 cabinet sides measuring 600 mm × 400 mm are required

Assessment Questions

Question 1
Name two different measuring tools you would use to inspect and measure the timber for this task. Briefly explain the purpose of each.

Question 2
List three steps you would take to ensure the machine is correctly set and safe for use before starting production.

Question 3
Describe how you would inspect the solid pine and the chipboard to ensure they are suitable for cutting. Mention grain direction, board type, or any visible defects.

Question 4
Explain two ways you can control or reduce waste while cutting the material. Include one safety reason for managing waste properly.

Question 5
Using the board dimensions and component size given in the case study, calculate:
a) How many full cabinet sides (600 mm × 400 mm) can be cut from one sheet of 2750 mm × 1830 mm chipboard, allowing for 3 mm kerf between cuts
b) How many full sheets are required to make 20 sides

Question 6
List two minor problems that could occur when setting or operating the machine, and explain how you would resolve or report them correctly.

✅ MODEL ANSWERS

Answer 1

- Measuring tape: Used to measure the board and check if the required dimensions fit

- Vernier calliper: Used to measure the board thickness or tool depth with high accuracy

Answer 2

- Remove all foreign objects and clean the table

- Check the blade or tool is correctly mounted and tight

- Confirm that guards are in place and run a test piece

Answer 3

- For chipboard: Check for a flat surface, consistent laminate, no bubbling

- For pine: Inspect for cracks, knots, grain alignment, and moisture warping

Answer 4

- Plan the cutting layout to minimise offcuts

- Stack offcuts neatly and clear sawdust regularly to reduce fire risk

Answer 5

a)

- Board length: 2750 mm ÷ (600 mm + 3 mm kerf) ≈ 4 pieces per row

- Board width: 1830 mm ÷ (400 mm + 3 mm kerf) ≈ 4 pieces per column

- Total per sheet: 4 × 4 = 16 cabinet sides per board

b)

- 20 required ÷ 16 per board = 2 full boards required

Answer 6

- Problem 1: Blade wobble – stop machine, tighten flange nut, test before restarting

- Problem 2: Dust suction not working – report to supervisor and mark machine “Not in Use” if unsafe

📝 Marking Memo

| Question | Criteria | Marks |
| --- | --- | --- |
| Q1 | 2 tools with accurate explanation | 4 |
| Q2 | 3 correct safety steps | 6 |
| Q3 | Both materials described with correct inspection points | 6 |
| Q4 | 2 waste control measures (incl. 1 safety rationale) | 4 |
| Q5 | Correct step-by-step calculation + result | 6 |
| Q6 | 2 minor problems + correct action/reporting | 4 |
|  | Total | 30 |

📊 Assessment Rubric

| Criteria | Outstanding (4) | Competent (3) | Developing (2) | Not Yet Competent (1) |
| --- | --- | --- | --- | --- |
| IAC0601 – Measuring tools used | Correct tools selected and accurately described | Tools appropriate; descriptions generally correct | Partial understanding or limited tool variety | Incorrect or no tools mentioned |
| IAC0602 – Machine is safe and clear | All setup steps clearly identified and sequenced | Most correct steps provided; logical reasoning | Basic awareness; unclear sequence or omissions | Missed key safety steps or setup errors |
| IAC0603 – Raw material inspection | Accurate comparison of board and timber, defects and suitability | Inspection areas correctly stated but lacks detail | Limited recognition of defects or types | Misidentifies materials or skips inspection altogether |
| IAC0604 – Waste control | Practical and safety-focused suggestions given | Correct waste reduction suggestions, may lack rationale | Waste acknowledged but no method suggested | No reference to waste or hazard |
| IAC0605 – Calculations | Fully correct; steps shown and logical | Correct answer; minimal working shown | Attempted with errors or missing details | No attempt or incorrect methodology |
| IAC0606 – Machine problem response | Two problems clearly stated; appropriate resolution/reporting | One complete problem; other unclear | Incomplete or partially correct action | Problems unclear or actions unsafe |

### Facilitator Assessment Briefing

Practical Module: PM-01 – Operate a Range of Machines in the Wood Machine Shop to Cut Components for Furniture Manufacturing

Sub-task: PM-01-PS06 – Prepare for Machine Operations

Assessment Type: Integrated Practical Knowledge Assessment

Internal Assessment Criteria:

- IAC0601: Different measuring equipment are used to measure timber such as measuring tapes and vernier callipers

- IAC0602: The machine is set and ready for operation and all foreign objects are removed from the machine

- IAC0603: The raw material is inspected for grain direction, type (board or solid) and defects

- IAC0604: Waste control is exercised while cutting material to eliminate fire hazards

- IAC0605: Basic calculations are applied in order to obtain the right number and size of components

- IAC0606: Machine problems are identified and minor problems are resolved while those outside operator control are reported via the correct communication channels

Purpose of the Assessment

This integrated assessment measures the learner’s readiness to perform machine preparation activities that directly affect the quality, safety, and efficiency of production in the woodworking environment. It combines applied knowledge and practical interpretation of job cards, material inspection, tool setup, machine checking, and basic mathematical reasoning.

Successful completion demonstrates the learner’s ability to think critically, apply safety and quality standards, and prepare both tools and materials for cutting operations in a professional and compliant manner.

Assessment Context

This assessment is based on a realistic workshop case study. The learner is expected to interpret specifications from a job card, prepare and inspect material and machines, apply accurate measurement and calculation skills, and demonstrate responsibility in identifying and reporting any mechanical or operational issues.

Facilitator Instructions

- Read the case study with the learner to confirm understanding

- Provide access to cutting lists, mock job cards, and relevant tools or simulated resources

- Allow learners to complete the task individually

- Use the model answers, marking memo, and rubric to guide scoring

- Offer clear feedback and remediation if necessary to ensure competency

## PM-01-PS07: Operate Various Machines in the Machining Department in Laminating, Breakout, Planing and Sanding Operations to Produce Timber Components to Specifications

1. Introduction to the Practical Skill

This sub-task consolidates the learner’s ability to operate a range of machines used in the laminating, break-out, planing, and sanding stages of timber processing. These operations are fundamental to the transformation of raw materials into precision-cut components for furniture production.

The focus is on developing machine handling skills, material sensitivity, and operational awareness to ensure that timber is processed to exact specifications—safely, efficiently, and in alignment with product quality standards.

Learners are expected to demonstrate accurate machine control, tool setting, grain direction awareness, and product inspection techniques while managing real-time production activities and responding to routine interruptions.

2. Scope of Practical Skill

Given different types of machines in the workshop, the learner must be able to:

- PA0701 Start the machine according to starting procedures

- PA0702 Feed workpieces to the machine

- PA0703 Use helping aids such as push sticks or a helping fence where appropriate to ensure personal safety

- PA0704 Adjust the cutting tools to meet product specification

- PA0705 Observe the direction of the grain of the wood as cutting to ensure the pattern of grains is right

- PA0706 Check the concave and convex side of the wood when planing

- PA0707 Choose and use the correct laminating procedure

- PA0708 Perform the break-out operation using a radial arm/cross-cut saw or a rip saw

- PA0709 Use planing machines such as the surface planer or the thickness planer as per product specifications

- PA0710 Conduct sawing operations with a panel saw or a band saw as per product specifications

- PA0711 Perform sanding operations using machinery such as a stroke sander, drum sander and an edge sander

- PA0712 Observe the defects of timber such as knots and remove nails or foreign objects in the case of reclaimed timber

- PA0713 Replenish raw material as needed to ensure optimum production efficiency

- PA0714 Perform quality or style changes such as changing from solid wood to board or from softwood to hardwood, paying attention to settings such as speed and cleaning to prevent scratching

- PA0715 Optimise machine efficiencies and down-time, planned and unplanned interruptions such as breaks, power outages, running out of material, breakdowns

- PA0716 Stop the machine at the end of use or in case of an emergency

- PA0717 Dispose/store off-cuts safely

- PA0718 Store and label components according to specifications and size

- PA0719 Check samples at set intervals (spot checks) for correctness and consistency of cut components

3. Applied Knowledge

- AK0701 Understanding of material and defects

- AK0702 Material handling

4. Internal Assessment Criteria

- IAC0701 Materials and material defects are identified according to their uses, applications and the tolerance standards to which they are subject in order to identify quality raw materials and reject non-conforming materials

- IAC0702 Cutting lists and routing sheets are interpreted in order to ensure components are correct

- IAC0703 Organisational reporting procedures are followed

- IAC0704 Materials are accurately sorted, handled and stacked safely and securely

- IAC0705 Personal protective equipment is selected and used correctly according to Health and Safety regulations and requirements

### PA0701 – Start the Machine According to Starting Procedures

Facilitator Purpose

This session focuses on teaching learners the importance of adhering to machine-specific start-up procedures. Correct machine start-up is fundamental to both operator safety and machine integrity. Learners will be trained to recognise the start-up sequence, understand machine status indicators, and observe the surrounding environment before and during machine activation.

The learner will develop routine habits for initiating machines used in laminating, break-out, planing, and sanding operations, thereby promoting safe and effective operation aligned with industry standards.

Key Concepts to Cover

1. Why Start-Up Procedures Matter

- Prevents sudden tool movement or uncontrolled material feed

- Ensures all safety features and guards are active

- Allows time to observe warning indicators or startup delays

- Promotes consistency across all operators in the workshop

- Reduces the risk of mechanical failure or personal injury

2. Typical Start-Up Procedure Steps

| Step | Action |
| --- | --- |
| Step 1: Pre-check confirmation | Ensure tooling is secured, machine area is clean, and power cables are safe |
| Step 2: Power on and check signals | Switch on main power and observe machine control lights or indicators |
| Step 3: Safety lockout clearance | Remove any lockout tags if previously applied and confirmed safe to start |
| Step 4: Activate start mechanism | Use designated start button, switch, or foot pedal depending on the machine type |
| Step 5: Listen and observe | Watch for abnormal noise, vibration, or startup hesitation |
| Step 6: Confirm idle run | Let machine run unloaded for a few seconds to verify stability |

🛈 Always refer to the machine’s operating manual for manufacturer-specific instructions.

3. Key Safety Considerations

- Never start a machine while another person is inside the danger zone

- Ensure emergency stop buttons are functional before startup

- Wear all required PPE before approaching the machine

- Use dry hands when operating electrical components

- Notify a supervisor immediately if the machine does not start or emits unusual sounds

Facilitator Demonstration Tip

Conduct a step-by-step demonstration using:

- A panel saw, spindle moulder, or edge sander (or a diagram if machines are unavailable)

- Emphasise visual/auditory checks and the use of indicator lights

- Demonstrate dry run versus loaded operation

Encourage learners to repeat the steps aloud while observing or shadowing an instructor.

Activity Suggestion: Machine Start-Up Simulation

Assign each learner or small group to:

- Read a laminated start-up checklist

- Perform a simulated start-up at a demo station (or photo board)

- Identify potential risks (e.g. blade cover left open, unsecured material)

- Explain what they would do differently if a fault was detected

Case Study: Missed Step Leads to Machine Fault

A learner failed to inspect the dust extraction before starting the thickness planer. The machine operated for five minutes before jamming due to sawdust build-up. The planer overheated and needed to be shut down for repairs.

Facilitator Prompts:

- Which part of the start-up procedure was skipped?

- What impact did this have on production?

- How could the learner have identified the issue earlier?

Critical Thinking Questions

- Why is it necessary to let a machine run idle before inserting a workpiece?

- What are the risks of rushing the start-up process in a busy workshop?

- Why must startup procedures be standardised across all operators?

- What would you do if the machine control panel shows a flashing red indicator?

- How can workshops promote a culture of responsible machine start-up behaviour?

### PA0702 – Feed Workpieces to the Machine

Facilitator Purpose

This session develops the learner’s ability to feed materials into machines correctly, with attention to safety, grain direction, machine limitations, and support techniques. Feeding workpieces incorrectly can lead to inaccurate cuts, kickback, jamming, or injury. The goal is to ensure learners understand how to maintain control of the workpiece throughout the operation and match their actions to both machine and material characteristics.

Key Concepts to Cover

1. Purpose of Correct Feeding Technique

- Ensures precision of cut, shape, or finish

- Reduces material wastage due to misfeeds or deflection

- Minimises risk of kickback or tool binding

- Promotes correct posture and reduces fatigue or strain on the learner

- Improves workflow consistency and speed in production settings

2. Factors That Affect Feeding

| Factor | Explanation |
| --- | --- |
| Grain direction | Feeding against the grain can cause tear-out or blade chatter |
| Material type | Hardwoods and softwoods behave differently under pressure |
| Machine type | Feed speeds and methods differ (planer vs panel saw vs edge sander) |
| Component size | Small components may require jigs or push sticks |
| Machine feed system | Some machines are self-feeding (e.g. thickness planer); others are manual (e.g. table saw) |

3. General Feeding Guidelines by Machine Type

| Machine | Feeding Guidelines |
| --- | --- |
| Panel saw | Feed steadily with both hands, keeping workpiece flat and against the fence |
| Spindle moulder | Use pressure pads or push blocks; feed from right to left (against cutter rotation) |
| Planer (surface/thickness) | Flat face down, grain direction respected, use infeed/outfeed rollers |
| Edge sander | Keep workpiece moving, light pressure, avoid prolonged contact in one area |
| Drum sander | Centre the workpiece, ensure belt alignment, light consistent pressure |
| Rip/cross-cut saw | Material must be firmly held, hands clear of the blade, feed along designated track |

🛈 Never force the workpiece. The feed should be firm, controlled, and match machine speed and blade resistance.

Facilitator Demonstration Tip

Use a range of setups to demonstrate:

- Correct feeding direction based on grain

- What happens when pressure is uneven (e.g. taper cut, slipping)

- How to use push sticks, fences, and outfeed supports for longer boards

- Correct hand positioning to maintain control while avoiding danger zones

Encourage learners to practise feeding sample boards on machines that are either deactivated or using dummy setups.

Activity Suggestion: Feed Positioning and Posture Drill

Set up three stations with different machines or visuals. Ask learners to:

- Describe how the workpiece should be held and guided

- Point out the danger zones and how they will avoid them

- Demonstrate correct posture and body alignment while feeding material

Use a mirror or peer feedback for learners to observe their form.

Case Study: Tear-Out During Planing

A learner planed a batch of drawer fronts without checking grain direction. Several pieces splintered along the trailing edge. Inspection revealed they had been fed against the grain, leading to surface damage and additional sanding time.

Facilitator Prompts:

- What could the learner have looked for to prevent this?

- What tools or checks could have been used before feeding?

- How would a test piece have helped in this situation?

Critical Thinking Questions

- Why is it important to match the feed speed to the material and the machine?

- What safety tools can help reduce risk during feeding operations?

- How does incorrect feeding affect the quality and dimensions of the final component?

- What precautions should be taken when feeding narrow or short workpieces?

- Why is it important to stay focused and avoid distractions during feeding?

### PA0703 – Use Helping Aids Such as Push Sticks or a Helping Fence Where Appropriate to Ensure Personal Safety

Facilitator Purpose

This session aims to reinforce the learner’s ability to identify and correctly use helping aids—such as push sticks, push blocks, featherboards, and helping fences—to prevent injury and maintain control when feeding materials through machines. These aids are essential for maintaining safe hand distance, especially when working with small, narrow, or short components.

The learner will be trained to assess when helping aids are necessary, how to use them properly, and how they enhance both precision and safety during machining.

Key Concepts to Cover

1. What Are Helping Aids and Why Are They Used?

| Helping Aid | Purpose |
| --- | --- |
| Push stick | Keeps hands away from blade/cutter while pushing narrow or short pieces |
| Push block | Provides downward and forward pressure on workpiece across a flat surface |
| Featherboard | Applies side pressure to keep material against fence or table |
| Helping fence | Acts as a secondary guide or hand guard, especially for planing operations |
| Hold-down clamps | Secure workpieces during drilling or routing to prevent lifting or spinning |

🛈 Helping aids must be made from non-slip or sacrificial materials like hardwood or plastic, and should be kept clean and free of damage.

2. Situations Requiring Helping Aids

- Feeding narrow or short workpieces through table saws or planers

- Holding down thin or flexible materials on edge sanders or routers

- Working near rotating blades or cutters where hand proximity increases risk

- Supporting long boards with an additional helping fence to prevent tipping

- Performing repetitive tasks where operator fatigue may reduce control

Best Practice Guidelines

- Use push sticks for cut widths under 120 mm

- Replace damaged or missing helping aids immediately

- Never remove guards to compensate for poor workpiece control

- Store helping aids within reach of all operating stations

- Demonstrate use before assigning independent machine tasks

Facilitator Demonstration Tip

Use a table saw or mock setup to show:

- The danger zone near the blade

- How to grip and angle the push stick or push block for stable pressure

- The difference between safe feeding with vs without a helping aid

- Real-life examples of common mistakes (e.g. hands too close, pushing with bare fingers)

Create a helping aid rack display showing correct tool types and when each is used.

Activity Suggestion: Safety Zone and Helping Aid Roleplay

Set up:

- A visual layout with a mock saw station

- Learners must place themselves in the correct stance

- Select and demonstrate the appropriate helping aid

- Justify their selection and explain how it improves safety

Use a peer checklist to observe proper distance, grip, and motion.

Case Study: Hand Injury Due to Missing Push Stick

A junior operator used a panel saw to rip narrow strips without a push stick. While reaching to stabilise the board near the blade, their finger was grazed by the rotating saw. The workshop did not have a push stick within reach at the time.

Facilitator Prompts:

- What safety rule was broken?

- How could this have been prevented?

- What system should be in place to ensure helping aids are always available?

Critical Thinking Questions

- Why is it dangerous to rely only on hand control when machining small pieces?

- How do helping aids improve both safety and precision?

- What should you do if the correct helping aid is not available at your machine station?

- When might a helping fence be more appropriate than a push stick?

- Why must helping aids be included in machine start-up and safety checklists?

### PA0704 – Adjust the Cutting Tools to Meet Product Specification

Facilitator Purpose

This session enables learners to adjust machine-mounted cutting tools—including saw blades, cutter heads, planer knives, and sanding components—to ensure they align with the technical specifications of the job card or routing sheet. Tool adjustments are necessary to achieve correct cutting depth, width, angle, feed clearance, and profile accuracy, all of which affect product quality and operational safety.

Learners will be trained to interpret machining requirements, apply adjustment procedures correctly, and verify setup through test cuts and inspections.

Key Concepts to Cover

1. Why Adjustments Are Necessary

- Different components require different tooling positions and angles

- Incorrect settings can lead to incorrect dimensions, edge tear-out, or joint misalignment

- Proper adjustments reduce tool strain, overheating, and material damage

- Allows for style changes (e.g. bevel, groove, rebate) in a controlled manner

2. Types of Cutting Tool Adjustments

| Machine Type | Adjustable Features |
| --- | --- |
| Panel saw | Blade height, tilt angle, fence alignment |
| Spindle moulder | Cutter head height, spindle speed, fence depth, guide pressure |
| Thickness planer | Table height (to control finished thickness), cutter sharpness |
| Router table | Bit height, fence depth, cutting depth in multiple passes |
| Edge sander | Table height relative to sanding belt, contact pressure adjustments |

🛈 Tools must be adjusted while the machine is isolated (power off), and locked in position before use.

3. Adjustment Procedure Guidelines

- Consult the cutting list or drawing for target measurements and shape requirements

- Isolate the machine (power off and tagged out)

- Unlock the adjustment mechanisms (fence knobs, guide handles, table lifts)

- Adjust depth/angle/height settings using appropriate gauges or rulers

- Secure adjustments by tightening locks and bolts firmly

- Test run the setup with scrap material and measure the result

- Make fine adjustments if needed, and record settings if repeat cuts are required

Facilitator Demonstration Tip

Use a machine or visual model to demonstrate:

- Raising/lowering a planer table to reach a thickness target

- Tilting a panel saw blade to 45° for mitre cutting

- Adjusting a router bit height for groove or rebate cutting

- Emphasise safe body position, hand placement, and lockout procedures

Let learners perform hands-on setup tasks under supervision using dummy tooling or marked calibration blocks.

Activity Suggestion: Specification Alignment Exercise

Provide learners with:

- A drawing that specifies a 12 mm deep groove or 45° bevel

- Access to a marked training router table or panel saw
Ask them to:

- Perform the required tool adjustment

- Cut a test piece

- Measure and verify compliance with the specification

Encourage the use of steel rules, callipers, or depth gauges for inspection.

Case Study: Product Rework Due to Incorrect Cutter Height

A group of learners prepared door panels using a spindle moulder. The cutter was set 5 mm too high, causing a rebate that was deeper than intended. This created a visible step when the panels were fitted, requiring re-machining and delaying final assembly.

Facilitator Prompts:

- What should have been checked before full production began?

- How can test cuts prevent this kind of issue?

- Why is it important to lock adjustment handles and spindles after setting?

Critical Thinking Questions

- Why is it essential to isolate the machine before adjusting blades or tooling?

- What happens if a cutting tool is not tightened securely after adjustment?

- How can adjustment logs or visual indicators support faster setup in production?

- What tools help verify cutting depth or height before committing to production?

- What role does test cutting play in preventing errors during component preparation?

### PA0705 – Observe the Direction of the Grain of the Wood as Cutting to Ensure the Pattern of Grains is Right

Facilitator Purpose

This session equips learners with the ability to identify and work with the grain direction of timber during machining. Grain direction affects both the appearance and structural behaviour of wooden components. Cutting against the grain can cause tear-out, rough finishes, or weakened joints, while proper alignment enhances aesthetic consistency and preserves material integrity.

Learners will be guided to observe grain direction before cutting, determine the correct orientation for feeding, and adjust operations based on visual grain cues and product design requirements.

Key Concepts to Cover

1. What Is Wood Grain and Why It Matters

- Wood grain is the alignment of fibres in timber, visible as natural lines or patterns

- The grain direction indicates how wood will behave when cut, planed, or sanded

- Cutting with the grain produces smoother finishes and reduces resistance

- Cutting against the grain can result in splintering, surface tear-out, and tool wear

2. Grain Direction in Machining

| Machine Type | Grain Considerations |
| --- | --- |
| Planer/thicknesser | Always plane with the grain to avoid tear-out on the surface |
| Spindle moulder/router | Grain direction affects feed direction and cut smoothness |
| Saw (rip/cross-cut) | Less affected, but grain still determines tear-out on exit |
| Edge/belt sander | Sand with the grain to avoid scratches and patchy texture |

🛈 Grain can change direction in a single board—known as reversing grain—and should be assessed before each operation.

3. Visual Indicators of Grain Direction

- Raised fibres or a “fuzzy” edge: indicates cutting against the grain

- Smooth, even surfaces: indicates cutting with the grain

- Arrows drawn on boards in pencil or chalk: used to mark correct feed direction

- Curved or wavy lines: look at their direction in relation to the surface you are working on

Facilitator Demonstration Tip

Use real timber boards to show:

- Differences in feel and appearance when rubbing along vs against the grain

- Demonstrate planing with and against the grain (showing tear-out)

- Use chalk or arrows to guide learners in marking grain direction before feeding

Give learners offcut samples to inspect, feel, and test with hand planes or sanding blocks to experience resistance differences.

Activity Suggestion: Grain Orientation Exercise

- Present 3–4 boards with different grain patterns (straight, reversing, spiral)

- Ask learners to:

  - Identify and mark the feed direction for planing or sanding

  - Explain their choice

  - Predict what would happen if cut incorrectly

Follow with a short cut or sanding task to compare results based on orientation.

Case Study: Surface Tear-Out on Cabinet Panels

A learner planed veneered MDF panels in the wrong direction, assuming the surface was symmetrical. The veneer splintered at the exit edge, leading to visible surface damage and rework.

Facilitator Prompts:

- How could the grain have been assessed before planing?

- What should the learner have done to test the correct direction?

- How can workshop processes help prevent repeated tear-out?

Critical Thinking Questions

- How does grain direction affect tool wear and cutting quality?

- What are the visual or tactile signs that you are cutting against the grain?

- Why is grain direction important even on engineered boards with veneer surfaces?

- What steps can you take to avoid tear-out on highly figured or reversing grain timber?

- How can grain direction be included in production planning and marking procedures?

### Facilitator Notes: PA0706 – Check the Concave and Convex Side of the Wood When Planing

Facilitator Purpose

This session trains learners to identify and respond to the natural bowing or warping of timber prior to planing. Most timber exhibits some curvature—either concave (hollow) or convex (rounded)—due to drying processes or natural grain structure.

Understanding how to orient these boards during planing ensures stable feeding, even cutting, and safer machine operation. It also helps avoid sniping, jamming, or uneven thickness and contributes to the structural and aesthetic integrity of the final component.

Key Concepts to Cover

1. Concave vs Convex Sides

| Type | Description | Preferred Planing Face |
| --- | --- | --- |
| Concave | Hollow or cupped inward (edges higher than the centre) | Face down – stable support against cutter |
| Convex | Rounded or arched upward (centre higher than edges) | Face up – prevents rocking and poor contact |

🛈 The goal is to plane the most stable face first to create a reliable reference surface for thicknessing.

2. Why Orientation Matters When Planing

- Ensures stable contact with the planer table, reducing vibration

- Prevents material shifting that could cause sniping or uneven cuts

- Reduces the risk of blade contact bounce or incomplete surfacing

- Creates a flat reference face for further machining or assembly

3. Identifying Concave and Convex Boards

| Inspection Method | What to Look For |
| --- | --- |
| Visual check (hold at eye level) | Curve in the length or width of the board |
| Flat reference test (lay on known flat surface) | Rocking (convex) or gap underneath (concave) |
| Hand press check | If edges lift, it’s concave; if centre lifts, it’s convex |

Facilitator Demonstration Tip

Using timber samples:

- Show learners how to hold a board at eye level to spot curvature

- Place boards on a flat table to test for wobble (convex) or gapping (concave)

- Demonstrate planing a convex face down vs concave face down and show the difference in cut quality and safety

Let learners examine several boards, mark concave vs convex sides, and justify their planing orientation.

Activity Suggestion: Stability Orientation Task

Set up 5–6 warped timber boards with various curves. Ask learners to:

- Inspect each board

- Mark the concave and convex sides with chalk

- Indicate which side should be placed face-down on the planer for the first pass

- Justify their choice

Case Study: Wobbling Workpiece Causes Uneven Surfacing

A learner placed a convex board with its curved side facing down on a surface planer. As the rollers engaged the board, it rocked slightly, causing a gouged surface at the start and inconsistent thickness throughout.

Facilitator Prompts:

- What was the main issue in this situation?

- How could the learner have detected and corrected the orientation?

- What effect does this error have on later processes like jointing or edge banding?

Critical Thinking Questions

- What risks are introduced when planing a convex board with the wrong side down?

- How does proper board orientation support thickness accuracy and finish quality?

- Why should a learner always test board flatness before feeding it into the machine?

- What methods can workshops use to train new staff in grain and curvature recognition?

- How can board defects such as twist or cup be addressed before or during planing?

### Facilitator Notes: PA0707 – Choose and Use the Correct Laminating Procedure

Facilitator Purpose

This session introduces learners to the process of laminating timber and board materials, which involves bonding layers together using adhesive and pressure. Laminating enhances strength, stability, and visual appeal, and may be used in producing tabletops, doors, frames, and curved components.

The learner must be able to identify when laminating is required, choose the correct adhesive and method, and apply the appropriate pressure using clamps or laminating presses.

Key Concepts to Cover

1. What Is Laminating?

- Laminating is the process of bonding two or more layers of wood or board material

- It may involve solid timber lamination (e.g. finger-jointed panels), veneering, or plastic laminate application

- Proper lamination improves the dimensional stability, aesthetics, and strength of components

2. Types of Laminating Techniques

| Type | Typical Application | Tools/Equipment |
| --- | --- | --- |
| Flat lamination | Solid timber panels, carcasses, cabinet doors | Clamps, cold press, hot press |
| Edge lamination | Gluing multiple narrow boards to create wide panels | Clamps, dowels or biscuit joiners |
| Veneer lamination | Applying a thin wood veneer to board substrates | Vacuum press, glue roller, squeegee, roller |
| Plastic laminate (HPL) | Countertops, doors, shelving | Contact adhesive, press or roller, trimmer |
| Curved lamination | Chair backs, bowed panels | Moulds, vacuum bag, form press, flexible adhesives |

3. Steps in the Laminating Process

- Select materials – Ensure boards or veneers are flat, dry, and clean

- Choose appropriate adhesive – White glue (PVA), urea-formaldehyde, contact adhesive, etc.

- Apply adhesive evenly – Using a brush, roller, or glue spreader

- Align and clamp – Ensure consistent pressure across the full surface

- Cure/drying time – Leave clamped for the recommended duration based on adhesive type

- Trim and inspect – Remove excess glue and check for gaps, bubbles, or misalignment

🛈 Humidity, glue type, and surface preparation all affect bonding quality.

Facilitator Demonstration Tip

Demonstrate:

- How to apply glue evenly using a roller

- Correct clamp positioning to avoid bowing

- Veneer lamination using a sample board and vacuum bag or squeegee

- The difference between under-clamped and over-clamped joints

Let learners apply glue, set up a clamping jig, and label their laminated sample for testing after curing.

Activity Suggestion: Lamination Method Match-Up

Provide each group with:

- A material type (e.g. chipboard, solid oak, veneer)

- A product (e.g. door, shelf, tabletop)
Ask them to:

- Select a lamination method

- Choose the correct adhesive

- Describe the pressing or clamping method

- Justify their choices

Case Study: Delamination of a Laminated Worktop

A learner applied a plastic laminate to a chipboard base using contact adhesive. They failed to apply even pressure across the full surface. After installation, the laminate began lifting at the corners.

Facilitator Prompts:

- What caused the failure in this example?

- How could the learner have improved pressure distribution?

- Why is surface preparation critical before applying laminates?

Critical Thinking Questions

- What factors influence your choice of adhesive for different laminating jobs?

- Why is even pressure important during curing?

- What could happen if the surface is dusty or oily before gluing?

- How can a vacuum press improve consistency in veneer lamination?

- What role does time play in achieving a strong bond during lamination?

### Facilitator Notes: PA0708 – Perform the Break-Out Operation Using a Radial Arm/Cross-Cut Saw or a Rip Saw

Facilitator Purpose

This session introduces learners to the break-out operation, the process of cutting full-length boards or sheets into smaller, rough-sized pieces for further machining. This is often the first machine-based operation in furniture manufacturing and must be performed with a strong focus on accuracy, safety, and efficiency.

Learners will operate a radial arm saw, cross-cut saw, or rip saw, depending on the required cut direction, material size, and type. The focus is on correct setup, handling, feed alignment, and cut sequencing based on the cutting list.

Key Concepts to Cover

1. What is Break-Out?

- The initial separation of raw material into pieces that match rough dimensions from the cutting list

- Typically done before planing, edging, or profile cutting

- Also referred to as first-stage cutting or panel breakdown

- Often includes marking each piece for tracking through further machining

2. Machines Used for Break-Out

| Machine | Use |
| --- | --- |
| Radial arm saw | Cross-cutting timber to length; ideal for rough board stock |
| Cross-cut saw | For clean 90° cuts; useful for small batch production |
| Rip saw | Longitudinal cuts along the grain; used to break down boards width-wise |
| Panel saw (optional) | For sheet goods like chipboard or MDF |

🛈 Machine selection depends on material dimensions, grain direction, and production volume.

3. Key Safety and Operational Practices

- Mark material lengths clearly with pencil or chalk before cutting

- Always wear appropriate PPE: goggles, dust mask, ear protection

- Confirm cutting list dimensions before each cut

- Use fences and stops for repetitive cuts to ensure consistency

- Keep hands clear of the blade path and use clamps or hold-downs where necessary

- Check that boards are free of nails, screws, or staples (especially reclaimed wood)

- Never cut warped material unless safely supported

Facilitator Demonstration Tip

At the machine:

- Show correct setup and positioning of the fence and stops

- Demonstrate how to pull/push the saw through the material (radial arm vs rip saw)

- Explain blade selection for softwood vs hardwood

- Show how to safely dispose of offcuts and secure longer pieces before cutting

Use pre-cut labels or tags to reinforce component tracking after break-out.

Activity Suggestion: Break-Out Simulation Drill

Set up timber boards and assign cutting list dimensions. Have learners:

- Mark out the break-out sizes using a tape measure

- Cut material using a cross-cut saw or rip saw

- Stack and label each piece with the component name (e.g. “Leg – 450 mm”)

- Complete a tally sheet to track output

Case Study: Incorrect Cut Order Leads to Waste

A learner began cutting components from a full board without laying out the full cutting list. They cut four short pieces first, which prevented them from retrieving longer pieces later. As a result, 20% of the board was wasted.

Facilitator Prompts:

- What should have been done before cutting began?

- How can layout plans help minimise waste?

- What role does grain direction play in sequencing cuts?

Critical Thinking Questions

- What are the safety considerations when using a radial arm or rip saw for long material?

- How can pre-planning cut layout reduce offcuts and improve material yield?

- Why must reclaimed wood be checked thoroughly before break-out?

- What is the impact of an inaccurate break-out operation on subsequent machining processes?

- What systems can be used to ensure the correct dimensions are consistently cut in batch work?

### Facilitator Notes: PA0709 – Use Planing Machines Such as the Surface Planer or the Thickness Planer as per Product Specifications

Facilitator Purpose

This session provides learners with the skills and knowledge to operate both the surface planer (jointer) and thickness planer, which are essential for preparing straight, square, and uniformly thick timber components in furniture manufacturing.

Learners will learn to reference faces, follow the correct material flow, and monitor cutting depth to achieve accurate, repeatable results. Proper planing is critical for ensuring component fit, stability, and a clean surface finish prior to assembly or further machining.

Key Concepts to Cover

1. Surface Planer vs Thickness Planer

| Machine | Function | Key Use |
| --- | --- | --- |
| Surface planer | Flattens one face and one edge of the board | Creates a reference face and edge |
| Thickness planer | Cuts the opposite face to a uniform thickness | Makes the board parallel and consistent |

🛈 Always begin with the surface planer to create a flat reference face before using the thickness planer.

2. Operating Procedures for Each Machine

| Step | Surface Planer | Thickness Planer |
| --- | --- | --- |
| Pre-inspection | Check knives, fence, guard, grain direction | Check rollers, bed cleanliness, cutter head sharpness |
| Feed direction | With the grain (to prevent tear-out) | Reference face down, grain aligned |
| Setup | Set fence for 90° edge, adjust depth of cut | Adjust table height to match required thickness |
| Material handling | Steady, controlled pressure; use push blocks if needed | Allow rollers to draw in the material—do not force |
| Finishing | Use multiple light passes rather than one heavy cut | Use final pass for smoothing after reaching target thickness |

3. Safety Precautions

- Always check for nails or staples in the timber before planing

- Keep hands away from blades, use push blocks on shorter or narrow boards

- Wear ear protection—both machines are high-noise operations

- Ensure dust extraction is functioning to prevent buildup

- Use support tables or rollers for long boards to prevent tipping

Facilitator Demonstration Tip

Demonstrate both machines in succession:

- Show a warped board being surfaced flat

- Mark the reference face and explain how to position it in the thickness planer

- Perform test passes and measure thickness using a caliper or gauge

- Highlight common mistakes: planing against the grain, too deep a cut, poor feed alignment

Provide side-by-side comparisons of planed vs unplaned boards for tactile and visual inspection.

Activity Suggestion: Reference and Thickness Planing Task

Assign learners to:

- Surface-plane a board on one face and edge

- Mark the reference face/edge

- Thickness-plane the opposite face to a specified measurement (e.g. 19 mm)

- Measure with a steel rule or vernier calliper and record results

They must work in pairs to verify square and flatness using a try square and straight edge.

Case Study: Uneven Board Thickness Across Batch

During a production run, a learner failed to plane all boards from the same reference face. As a result, the boards were uneven in thickness, leading to fitting problems during assembly.

Facilitator Prompts:

- What is the purpose of marking a reference face?

- Why must the same orientation be maintained for all boards in a batch?

- How would the learner correct or prevent this in future?

Critical Thinking Questions

- Why is it necessary to surface one face before thicknessing a board?

- What are the risks of removing too much material in a single planing pass?

- How does grain direction influence planing quality?

- What signs indicate that planer knives need sharpening or adjustment?

- Why must operators monitor output thickness after each pass, not just the machine setting?

### Facilitator Notes: PA0710 – Conduct Sawing Operations with a Panel Saw or a Band Saw as per Product Specifications

Facilitator Purpose

This session builds learner competence in operating the panel saw and band saw, both of which are commonly used in the machining department for cutting timber and boards to shape, size, and design specification. Learners must demonstrate the ability to interpret the cutting list, adjust the machine correctly, and guide the material safely through the cutting process.

These machines are critical to dimensional accuracy, edge quality, and material optimisation in furniture manufacturing, especially for sizing sheet goods, trimming solid wood, and cutting curves or irregular shapes.

Key Concepts to Cover

1. Panel Saw vs Band Saw – Applications and Differences

| Machine | Function | Typical Use |
| --- | --- | --- |
| Panel saw | Accurate straight-line cutting, especially for sheet material | Sizing melamine, MDF, plywood, large solid panels |
| Band saw | Flexible curve and rip cutting with a continuous looped blade | Cutting arches, small components, or trimming irregular shapes |

🛈 Panel saws typically have a sliding table; band saws use a static table and a flexible guide.

2. Preparing for Sawing

| Preparation Task | Purpose |
| --- | --- |
| Read the cutting list | Identify exact sizes and grain orientation |
| Select the correct blade | Fine-tooth for melamine; wide for straight cuts; narrow for curves |
| Set up the fence or guide rail | Ensure alignment for repeatable and straight cuts |
| Mark the cutting lines on the material | Ensures cuts are accurate and avoid waste |
| Check the dust extraction system | Prevent sawdust build-up and visibility issues |

3. Operating Procedure and Safety

- Panel Saw:

  - Secure board flat on the sliding table

  - Use the rip fence and scoring blade for melamine to reduce chipping

  - Maintain constant pressure and straight feed through the blade

  - Support large sheets with a second person or table extension

- Band Saw:

  - Adjust blade guard height to just above the material

  - Use both hands to guide material, keeping fingers away from blade path

  - Feed material slowly and steadily, especially during curves

  - Use a push stick when needed for small parts

Facilitator Demonstration Tip

Demonstrate:

- Setting up both saws: fence, blade height, speed settings (where applicable)

- How to use a test cut to verify alignment before batch cutting

- Different results from fine vs coarse tooth blades

- Common cutting errors: drift, overcutting, rough edges — and how to avoid them

Let learners handle mock materials and guide them through safe feeding techniques.

Activity Suggestion: Cut-to-Size Task

Provide:

- A cutting list (e.g. 4 panels of 600 mm × 400 mm melamine)

- A panel saw with pre-set guide

- Learners must:

  - Measure and mark the board

  - Perform the cut

  - Measure the finished piece and verify against the specification

  - Stack and label correctly

Include a band saw task to cut a simple curve or shape template in softwood.

Case Study: Inaccurate Batch Cutting on Panel Saw

A learner neglected to use the scoring blade when cutting melamine boards. As a result, the boards chipped along the bottom face. Several units had to be re-cut, increasing material waste.

Facilitator Prompts:

- What caused the chipping in this case?

- What is the purpose of the scoring blade?

- How can this mistake be prevented through proper machine setup?

Critical Thinking Questions

- What is the difference between the type of cuts you would do on a panel saw versus a band saw?

- Why is it important to select the correct blade width for a band saw curve cut?

- What steps can be taken to ensure multiple panels are cut to the exact same size?

- What role does grain direction play in planning your cut layout on the panel saw?

- How does safety differ between straight ripping and curved cutting operations?

### Facilitator Notes: PA0711 – Perform Sanding Operations Using Machinery Such as a Stroke Sander, Drum Sander and an Edge Sander

Facilitator Purpose

This session focuses on enabling learners to operate powered sanding machinery used for finishing timber components. Sanding machines help to remove marks from machining, even out surface inconsistencies, and prepare components for coating or assembly.

Learners will be trained to distinguish between machine types, select the appropriate sanding method, and monitor surface finish and safety during operation.

Key Concepts to Cover

1. Overview of Sanding Machines and Functions

| Machine Type | Function | Typical Use |
| --- | --- | --- |
| Stroke sander | Back-and-forth sanding across a flat surface | Large flat panels, tabletops, doors |
| Drum sander | Material passes under a rotating drum with sandpaper | Consistent thickness sanding, surface smoothing |
| Edge sander | Sanding belt mounted vertically or horizontally along an edge plate | Smoothing straight and curved edges, bevels, and small surfaces |

🛈 Each machine requires a specific technique and approach to pressure, speed, and feed.

2. Machine Preparation and Operation

| Preparation Step | Why It Matters |
| --- | --- |
| Select correct grit | Coarse for rough surfaces; fine for finish preparation |
| Check belt or drum condition | Worn abrasive leads to burn marks, uneven sanding |
| Set table height and guides | Prevents gouging or uneven sanding |
| Confirm dust extraction is active | Minimises airborne dust and prevents clogging |
| Wear appropriate PPE | Protects against dust and noise exposure |

3. Operation Guidelines per Machine

- Stroke Sander:

  - Keep the workpiece moving to avoid grooves

  - Apply even downward pressure; do not force

  - Use the entire belt width to extend lifespan

- Drum Sander:

  - Feed workpiece steadily using infeed/outfeed rollers

  - Use multiple light passes rather than deep cuts

  - Stop immediately if burning or resistance is felt

- Edge Sander:

  - Hold workpiece flat and steady against the table

  - Sand with the grain

  - Keep fingers and hands away from moving belt edge

Facilitator Demonstration Tip

Using real or simulated machines:

- Show the difference in sanding results with various grits

- Demonstrate edge rounding, face flattening, and burn removal

- Let learners practise feeding scrap timber through each sander

- Emphasise how excessive pressure or staying too long in one area affects the surface

Activity Suggestion: Sanding Quality Check

Give each learner:

- A timber panel with machining marks

- A target finish level (e.g. prep for clear coat)

- Access to different sanding machines and grits

Learners will:

- Choose the appropriate sander

- Sand the board to specification

- Inspect surface finish using light reflection or touch

- Record their sanding sequence and grit progression

Case Study: Uneven Sanding on Drawer Fronts

A learner used a drum sander to prepare drawer fronts but applied inconsistent pressure and fed some pieces at an angle. The result was tapered edges and an uneven surface finish, leading to gaps once fitted into the cabinet frame.

Facilitator Prompts:

- What errors were made during sanding?

- How does feed angle affect surface uniformity?

- What could have been done to achieve a consistent finish?

Critical Thinking Questions

- Why is it important to choose the correct grit when starting a sanding task?

- What effect does staying too long in one area have when using a stroke sander?

- Why must sanding operations always follow the grain direction where possible?

- How can sanding errors impact final assembly or coating results?

- What routine checks should be made on the sanding belt or drum before operation?

### Facilitator Notes: PA0712 – Observe the Defects of Timber Such as Knots and Remove Nails or Foreign Objects in the Case of Reclaimed Timber

Facilitator Purpose

This session focuses on developing the learner’s ability to inspect timber for visible and hidden defects that could affect the structural quality, aesthetic finish, or safety of machining operations. Particular emphasis is placed on reclaimed timber, which may contain embedded hazards such as nails, screws, or staples, and is increasingly used in sustainable furniture production.

The learner must be able to identify when timber is suitable for use, when it must be rejected, and when corrective steps such as nail removal or defect trimming are necessary.

Key Concepts to Cover

1. Common Timber Defects and Foreign Objects

| Defect/Foreign Object | Description | Risk/Consequence |
| --- | --- | --- |
| Knots | Hard, circular areas where branches were attached | Can weaken the board or cause blade deflection during cutting |
| Splits and checks | Cracks along the grain, often due to drying | Reduce strength and visual quality |
| Warping or cupping | Twists or curves in the timber surface | Affects machine feeding and joinery alignment |
| Nails, screws, staples | Typically found in reclaimed wood | Can damage blades or cause injury; sparks may create fire hazard |
| Decay/fungal staining | Discolouration, soft spots, or spongy areas | Indicate rot or moisture issues; must be rejected |

2. Inspection Methods and Tools

| Method | Application |
| --- | --- |
| Visual inspection | Look for visible defects, holes, staining, or metal traces |
| Tactile inspection | Run fingers along the edge to feel for protruding objects |
| Metal detector wand | Used to identify embedded nails or screws in reclaimed timber |
| Light tap or knock test | Can reveal loose areas or hollow sounds indicating decay |

3. Foreign Object Removal and Defect Management

- Use claw hammers, nail pullers, or screwdrivers to extract nails or staples

- Cut out severely damaged or split sections if salvageable

- Mark areas with chalk or pencil for defect avoidance during cutting

- Store rejected timber separately to prevent contamination of usable stock

- Always perform metal detection before planing or sawing reclaimed material

🛈 Even small metal objects can severely damage high-speed cutter heads and compromise operator safety.

Facilitator Demonstration Tip

Bring in:

- Reclaimed boards with real or simulated defects

- A metal detector wand to demonstrate scanning technique

- A set of hand tools for safe nail removal

- Before-and-after examples of boards with knot trimming or defect isolation

Let learners practise scanning, marking, and removing foreign objects in groups.

Activity Suggestion: Timber Grading and Hazard Identification

Provide learners with:

- A set of reclaimed timber pieces

- A timber defect chart or checklist

Learners must:

- Inspect and record the type of defects present

- Mark the area to avoid or remove

- Identify whether the board is usable, requires trimming, or must be rejected

Use a class discussion to justify decisions and explore real-world constraints.

Case Study: Blade Damage Due to Missed Staple

A learner failed to scan a piece of reclaimed pine for staples. When feeding it through the planer, the blade struck a hidden staple, damaging the cutter head and halting production for two days.

Facilitator Prompts:

- What could have prevented this incident?

- What are the consequences beyond just the blade damage?

- How can quality checks for reclaimed wood be improved in the workshop?

Critical Thinking Questions

- Why is it important to inspect both sides of the timber before machining?

- What is the correct response if a nail is embedded too deep to be removed safely?

- How can defects like knots influence the aesthetic of the final product—positively or negatively?

- What is the impact of not separating rejected timber from the production stockpile?

- Why is reclaimed timber both an opportunity and a risk in furniture manufacturing?

### Facilitator Notes: PA0713 – Replenish Raw Material as Needed to Ensure Optimum Production Efficiency

Facilitator Purpose

This session introduces learners to the importance of raw material monitoring and timely replenishment in a production environment. Ensuring that material is available when needed helps avoid downtime, keeps workflow uninterrupted, and supports productivity targets. Learners will understand how to recognise when stock is running low, request or fetch additional materials, and handle them safely.

This unit reinforces both production responsibility and collaboration between operators and storepersons.

Key Concepts to Cover

1. Why Timely Replenishment Matters

- Prevents unnecessary machine downtime

- Ensures a steady production flow

- Supports batch consistency by avoiding last-minute material substitutions

- Prevents bottlenecks and backlog across downstream operations

- Reduces workshop frustration and confusion during high-volume output

2. Material Tracking and Monitoring

| Aspect | Example/Action |
| --- | --- |
| Cutting list awareness | Review quantity required and compare to available stock |
| Batch progress monitoring | Monitor how many pieces have been processed vs what is needed |
| Check for offcuts suitability | Use trimmed material from prior cuts where appropriate |
| Visual stock inspection | Assess remaining sheets, boards, or bundles during the shift |
| Communication log | Use whiteboards, tags, or verbal updates to notify store team |

3. Replenishment Process in the Workshop

- Monitor stock during production (as boards are used or batches complete)

- Notify supervisor or stores clerk when running low

- Request delivery or collect boards from the storage area

- Use a trolley or pallet jack for safe and efficient handling

- Stack new material correctly and label clearly if part of a specific order

- Record stock movement if a system is in place (manual or digital)

4. Safety Considerations

- Use proper lifting techniques and get assistance for large boards

- Always check for defects or damage when retrieving new material

- Store material on flat, stable surfaces in designated zones

- Do not stack material in walkways or block emergency routes

- Ensure batch tags or labels are transferred accurately

Facilitator Demonstration Tip

- Show how to check a job card against remaining material

- Demonstrate safe movement of boards using lifting techniques and trolleys

- Emphasise communication—e.g. placing a “Material Low” sign or making a request to stores

Invite learners to practise fetching and safely restocking material during a production simulation.

Activity Suggestion: Stock Awareness Simulation

In a mock production setting:

- Give learners a partial stack of material and a full cutting list

- Ask them to estimate when more material will be needed

- Let them simulate placing a material request or restocking from storage

- Evaluate if timing was accurate and efficient

Case Study: Downtime Due to Missed Material Reorder

A learner running a panel saw completed 75% of a cabinet side batch before realising they had no more melamine sheets. They had not alerted the supervisor in time. The delay affected the assembly line and caused the job to finish one day late.

Facilitator Prompts:

- What systems should be in place to track material use?

- How could the learner have estimated usage earlier?

- What communication methods work best for timely restocking?

Critical Thinking Questions

- Why is it important to monitor stock levels even if you are not the storeperson?

- What are the risks of continuing to cut or assemble with mismatched or low-grade material due to stock pressure?

- How does proactive replenishment contribute to teamwork and workflow efficiency?

- What information should you give when requesting more material from the store?

- How can material shortages be prevented during high-volume production runs?

### Facilitator Notes: PA0714 – Perform Quality or Style Changes such as Changing from Solid Wood to Board or from Soft Wood to Hard Wood, Paying Attention to Settings such as Speed and Cleaning to Prevent Scratching

Facilitator Purpose

This session supports learners in managing transitions between different material types or design specifications during machine operations. Changes in material (e.g. from pine to melamine, or softwood to hardwood) or style (e.g. from curved to straight edges, or panel to frame) require adjustments to machine settings, cutting speed, tooling, and work area cleanliness.

Learners will be trained to identify when a changeover is necessary, interpret relevant instructions, and apply procedures that preserve component quality, prevent surface damage, and maintain production consistency.

Key Concepts to Cover

1. Examples of Quality or Style Changes

| Change Scenario | Adjustment Required |
| --- | --- |
| Switching from solid pine to oak | Reduce feed speed; use sharper cutters to handle hardness |
| Switching from melamine to MDF | Change to a finer-tooth blade; reduce blade height to avoid chipping |
| From hardwood frame to veneered board | Clean all rollers and tables to prevent scratching veneer |
| Style change: flat edge to bevel | Adjust spindle profile cutter or router bit and test before production |
| Product variation: thicker to thinner material | Adjust planer or saw blade height accordingly |

2. Key Operational Adjustments to Consider

- Machine speed (spindle RPM, feed rate)

- Blade or bit type and sharpness

- Cutting depth or sanding pressure

- Dust removal and surface cleaning

- Clamp padding or protection for sensitive finishes

- Test cuts or sample checks before proceeding with new material

3. Cleaning and Preventing Surface Damage

- Use soft cloths or compressed air to clean machine surfaces

- Inspect rollers, guides, fences, and tables for embedded grit or wood fibres

- Replace scratched or sticky pressure pads

- Ensure work area is free of glue residue, sawdust, and tool debris

- Stack new materials on clean surfaces with padding or spacers

Facilitator Demonstration Tip

Demonstrate a material changeover:

- Switching from rough pine boards to white melamine panels

- Clean the saw table, adjust blade height, switch to a finer-tooth blade

- Show how a dirty table can scratch veneered panels

- Emphasise using test pieces to check chip-out or burn marks

Use labelled samples to show the impact of incorrect setup when changing material types.

Activity Suggestion: Material Transition Simulation

Set up two workstations:

- One configured for softwood machining

- The other for veneered MDF

Ask learners to:

- Identify all changes that must be made before switching material

- Perform the necessary adjustments

- Explain how they would prevent scratching or tear-out

- Complete a checklist to confirm transition readiness

Case Study: Surface Damage Due to Poor Changeover Practice

A learner moved from machining hardwood to high-gloss board without cleaning the edge sander. Dust and wood fragments on the table surface scratched the laminate as it passed through. The component had to be reprocessed, and material was lost.

Facilitator Prompts:

- What steps should have been taken before switching material?

- What tools or supplies could help with changeover cleaning?

- How can clean-down routines be embedded in daily production practice?

Critical Thinking Questions

- Why is it important to slow machine feed rates when moving from softwood to hardwood?

- What are the risks of using the same blade or bit when changing between different materials?

- How can a test cut help detect issues before full production?

- What consequences can arise from surface scratching on high-finish boards?

- How can production teams coordinate changeovers to reduce downtime and defects?

### Facilitator Notes: PA0715 – Optimise Machine Efficiencies and Down-Time, Planned and Unplanned Interruptions Such as Breaks, Power Outages, Running Out of Material, Breakdowns

Facilitator Purpose

This session builds learner competence in identifying and managing production interruptions—whether scheduled (like breaks or shift changes) or unexpected (such as material shortages or mechanical faults). Learners will be guided to adopt a proactive mindset focused on maximising machine uptime, reducing delays, and supporting team-based recovery plans during disruptions.

The aim is to embed a practical understanding of how downtime impacts productivity, quality, and workflow—and how operators can play a role in sustaining efficiency and accountability.

Key Concepts to Cover

1. Types of Interruptions in Machine Shop Operations

| Type | Examples |
| --- | --- |
| Planned | Breaks, lunch time, cleaning shifts, tooling changeovers |
| Unplanned – Mechanical | Blade breakage, machine malfunction, overheating, dust extraction issues |
| Unplanned – Resource-related | Running out of raw material, incorrect stock, missing PPE |
| Unplanned – External | Load-shedding, power failure, safety inspections, delivery delays |

2. Strategies to Optimise Efficiency During Interruptions

| Optimisation Action | Purpose |
| --- | --- |
| Preload material before breaks | Reduces setup time post-break |
| Log machine downtime with cause | Enables root-cause analysis and repair prioritisation |
| Clean and reset machine during short stops | Prepares workstation for fast recovery |
| Organise tools and components | Keeps process ready while waiting for power or material |
| Communicate with supervisors early | Prevents extended delays due to lack of coordination |
| Perform minor maintenance if trained | Keeps equipment in best working condition |

3. Role of the Operator in Efficiency

- Maintain awareness of production targets and cutting list progress

- Suggest or initiate productive tasks during machine idle time (e.g. offcut sorting, workspace cleaning)

- Ensure machine restart procedures are followed after a stop

- Record interruption duration and resolution actions, especially for traceability and reporting

Facilitator Demonstration Tip

Simulate an unplanned interruption:

- Pause a group activity mid-operation (e.g. power off scenario)

- Ask learners: What could be done during this time to maintain productivity?

Discuss the importance of:

- Quick tool checks

- Re-checking job card specs

- Staging the next material batch

- Communicating status updates to the supervisor or teammates

Activity Suggestion: Downtime Management Roleplay

Create 3–4 scenario cards (e.g. blade dullness, material shortage, lunch break, power failure).
Assign learners to:

- Identify type of interruption (planned/unplanned)

- Suggest 2–3 efficiency actions that could be taken during that time

- Roleplay how they would communicate with their team or supervisor

Have each group present their efficiency strategy and receive peer feedback.

Case Study: Power Failure Halts Edge Banding

Midway through a batch, the workshop experienced a power cut. One learner used the downtime to tidy offcuts, inspect toolboxes, and review the cutting list for the next job. Another learner idled without direction. When power was restored, the first learner resumed immediately, while the other still needed to prepare.

Facilitator Prompts:

- What differentiated the two learners’ approaches?

- How does initiative support workshop productivity and team performance?

- What tasks are safe and beneficial during a short-term power cut?

Critical Thinking Questions

- What is the risk of waiting passively during unexpected machine downtime?

- Why should you notify a supervisor early if you notice a developing machine fault?

- How does maintaining a clean and organised workspace support quick recovery?

- What safety procedures should be followed before restarting a machine after downtime?

- How can teams use communication boards or logs to reduce repeat interruptions?

### Facilitator Notes: PA0716 – Stop the Machine at the End of Use or in Case of an Emergency

Facilitator Purpose

This session teaches learners how to correctly shut down machinery after use and respond effectively in emergency situations requiring immediate machine stoppage. Proper shutdown ensures equipment safety, preserves tool condition, and prevents unintended reactivation.

Learners will also be introduced to emergency stop protocols, including how to recognise hazards that warrant emergency intervention and how to communicate and report such incidents quickly.

Key Concepts to Cover

1. Why Safe Shutdown Is Important

- Prevents accidental start-up by the next user

- Protects blades, belts, and motors from unnecessary wear

- Allows safe cleaning and maintenance

- Essential for team safety, especially in shared workspaces

- Ensures machinery is ready for the next shift or job

2. Shutdown Procedure – End of Use

| Step | Explanation |
| --- | --- |
| 1. Clear material | Ensure no timber is in contact with the blade or cutter head |
| 2. Turn off the power switch | Use the main machine switch, not just foot pedals or handles |
| 3. Isolate the machine (if applicable) | Lock out or tag for cleaning, blade change, or maintenance |
| 4. Wait for full stop | Allow moving parts to come to a complete stop before cleaning |
| 5. Clean the area | Remove offcuts, dust, and scrap material |
| 6. Log machine use (if required) | Record usage, issues, or next job details if operating logs used |

3. Emergency Stop Procedure

| Step | When to Use |
| --- | --- |
| Activate emergency stop button/pedal | Immediately when risk to safety or severe malfunction is noticed |
| Call for help if needed | Alert supervisor or safety officer |
| Do not reset or restart | Wait for clearance or inspection before machine is used again |
| Report the incident | Complete the correct organisational form or report verbally |

4. When to Trigger an Emergency Stop

- Material jammed or kicking back

- Unusual vibrations, smoke, or burning smell

- Blade damage or snapping

- Power surge or electrical flickering

- Operator injury or equipment failure

Facilitator Demonstration Tip

- Show a machine shutdown in real time: normal stop vs emergency stop

- Let learners observe how long it takes for a blade to fully stop

- Locate all emergency stop buttons, including those on walls and pedestals

- Demonstrate how to log a fault or tag a machine as “out of service”

Let learners practise pressing an emergency stop (machine off) and roleplay how they would report an issue.

Activity Suggestion: Emergency Response Simulation

- Create 3 short emergency scenarios (e.g. jammed panel, burning smell, electrical short sound)

- Ask learners to:

  - Simulate emergency stop procedure

  - Indicate what they would do next

  - Identify who they would inform

  - Complete a mock report

Use feedback sessions to reinforce speed, clarity, and safety responsibility.

Case Study: Machine Left Running Causes Minor Fire

A learner left the edge sander running unattended after a shift. Friction from a misaligned belt generated heat, igniting wood dust in the corner of the sander’s housing. The fire was contained, but the machine was damaged.

Facilitator Prompts:

- What key shutdown steps were missed?

- What workshop policy should prevent unattended machines from running?

- How can signage or shift-end checks reduce this risk?

Critical Thinking Questions

- Why must all machine movement stop before attempting cleaning or blade changes?

- What is the risk of assuming another team member will turn off the machine?

- How does an emergency stop button differ from the normal shutdown switch?

- What steps should be taken if the emergency stop mechanism fails to engage?

- Why is it essential to communicate a machine shutdown to other team members in the area?

### Facilitator Notes: PA0717 – Dispose/Store Off-Cuts Safely

Facilitator Purpose

This session enables learners to manage timber and board off-cuts generated during machining in a manner that is safe, organised, and sustainable. Proper disposal or storage of off-cuts contributes to fire prevention, trip hazard reduction, and material reusability.

The learner must be able to distinguish between scrap and reusable material, dispose of waste responsibly, and store usable off-cuts neatly, without creating obstructions or compromising safety standards.

Key Concepts to Cover

1. Why Off-Cut Management Matters

- Prevents tripping hazards around machines and walkways

- Reduces risk of dust ignition and fire caused by loose off-cuts

- Supports material savings when usable off-cuts are sorted for future use

- Keeps the production area organised, clean, and compliant with OHS standards

- Reinforces responsible workshop behaviour and care for shared spaces

2. Types of Off-Cuts

| Type | Example | Recommended Action |
| --- | --- | --- |
| Usable off-cuts | Square, undamaged pieces >150 mm | Stack neatly in designated off-cut storage |
| Scrap pieces | Small, cracked, or irregular shapes | Dispose of in wood waste bin |
| Hazardous off-cuts | Splintered ends, embedded nails (reclaimed wood) | Place in marked “Hazardous Scrap” container |
| Sheet/board edging | Trimmings or veneer strips | Store flat or bundle with tape, if reusable |

🛈 Clear sorting protocols help reduce material waste and improve accessibility for learners and production teams.

3. Off-Cut Storage and Disposal Best Practices

- Place bins or boxes near machines for immediate disposal of small scrap

- Store usable off-cuts in labelled shelves, racks, or bins by material type (e.g. pine, MDF, melamine)

- Do not stack off-cuts on machines or in walkways

- Regularly clear disposal bins to avoid overflow

- For edge trims, use clips or bundles to prevent tangling or slipping

- Ensure off-cut areas are clearly marked and kept dry and tidy

Facilitator Demonstration Tip

Set up a table with a variety of off-cuts. Walk learners through:

- Sorting them into “use again” vs “discard” categories

- Where to place each type in the workshop (e.g. usable rack, off-cut bin, hazardous scrap)

- How to stack without causing tipping or blockage

- What to do with sharp, jagged, or splintered pieces

Emphasise personal safety when handling broken or irregular boards.

Activity Suggestion: Sorting and Storing Challenge

Give learners a pile of mixed off-cuts from a simulated cutting task. Ask them to:

- Sort them into reusable and non-reusable

- Store the reusable items in the correct area by type and size

- Explain why they made those decisions

- Remove scrap safely using the proper container

Use a peer observation checklist for safety and tidiness.

Case Study: Injury Caused by Misplaced Off-Cuts

A learner tripped over a long pine off-cut left leaning against a machine table. It had not been stored or disposed of after a previous job. The fall resulted in minor injury and a near-miss report.

Facilitator Prompts:

- What could have prevented this incident?

- Why is it important to complete cleanup after every task?

- What should be in place to prevent similar oversights?

Critical Thinking Questions

- What are the safety hazards of leaving off-cuts on or near machines?

- How can proper off-cut sorting reduce material costs over time?

- What should be done if an off-cut has exposed nails or dangerous splinters?

- Why is it important to label or separate different types of off-cuts?

- How can off-cut management support lean production and workplace discipline?

### Facilitator Notes: PA0718 – Store and Label Components According to Specifications and Size

Facilitator Purpose

This session focuses on the proper organisation, labelling, and storage of furniture components after they have been machined. Learners are expected to understand how to store components in a way that ensures easy retrieval, maintains quality and condition, and supports order tracking and workflow continuity.

By developing these habits, learners contribute to a well-structured, traceable production environment and reduce the risk of mix-ups, damage, or production delays.

Key Concepts to Cover

1. Why Component Storage and Labelling Matter

- Prevents loss or misplacement of completed parts

- Maintains batch identity and tracks work-in-progress

- Protects components from damage, warping, or contamination

- Supports workflow efficiency, especially in multi-stage production

- Facilitates quality control inspections and final assembly

2. Labelling Requirements and Practices

| Label Detail | Purpose |
| --- | --- |
| Component name or ID (e.g. “Shelf A”) | Identifies the part type and ensures it matches cutting list |
| Quantity in stack | Tracks how many parts are in each group |
| Material type (e.g. melamine, pine) | Prevents material mix-ups |
| Date of production (optional) | Useful for batch tracking or ageing parts |
| Job number or order reference | Ensures components are routed to the correct client/project |

🛈 Labels may be written on masking tape, stickers, tags, or reusable boards. Digital or barcoded systems may be used in advanced settings.

3. Storage Best Practices

- Stack components by type and size in separate, clearly marked areas

- Use shelving, crates, pallets, or vertical racks depending on component size

- Protect surfaces with soft spacers, especially for high-gloss or veneered panels

- Store parts flat to avoid warping unless designed for upright storage

- Ensure safe stacking height to prevent tipping or difficulty accessing items

- Designate zones for pending QC, ready-for-assembly, or rework components

Facilitator Demonstration Tip

- Show a “good” vs “bad” storage example using real or mock components

- Demonstrate how to label a batch using masking tape and marker

- Explain how to separate parts based on project or size (e.g. all “Drawer Fronts 600 × 150” go together)

- Roleplay a request from assembly—how would you find and deliver the correct batch?

Encourage learners to reflect on how clear labelling speeds up the next phase in production.

Activity Suggestion: Sorting and Labelling Simulation

- Provide learners with a mix of mock components in various sizes and materials

- Ask them to:

  - Identify and label each part using sample job cards

  - Stack and store each batch according to its specification

  - Create a component record for each label (optional tracking form)

Include a short retrieval challenge—ask another team to find “Drawer Sides for Order 23”.

Case Study: Assembly Delayed by Missing Labels

A learner completed machining 80 shelf panels but failed to label and separate them from another similar-looking job. The panels were stacked together, causing a delay in assembly as the team had to re-measure and verify dimensions manually.

Facilitator Prompts:

- How could labelling have prevented this issue?

- What simple system could be introduced to avoid similar mistakes?

- Why is it important to think ahead to the next production phase?

Critical Thinking Questions

- What could happen if two batches of similar parts are not labelled correctly?

- Why should glossy or veneered components be stacked with protection between them?

- How can digital systems improve component tracking compared to manual labels?

- What role does component labelling play in quality control and final inspection?

- How can effective storage reduce rework and save time in large production runs?

### Facilitator Notes: PA0719 – Check Samples at Set Intervals (Spot Checks) for Correctness and Consistency of Cut Components

Facilitator Purpose

This session trains learners to perform regular sample checks (spot checks) during the cutting or machining of furniture components. Spot checks are a proactive quality control measure used to identify errors early in the production process, ensuring that parts consistently match the cutting list, design specification, and tolerances.

Learners will be introduced to the principles of visual inspection, dimensional verification, and documentation of checks, as well as what steps to take when a discrepancy is discovered.

Key Concepts to Cover

1. Why Spot Checks Are Necessary

- Prevents entire batches of incorrect components being produced

- Identifies blade wear or misalignment early

- Supports traceability and accountability within production teams

- Reduces rework, scrap, and material wastage

- Reinforces a culture of self-checking and responsibility

2. When and How to Conduct Spot Checks

| Check Interval | Example |
| --- | --- |
| After the first 3–5 components | To confirm machine setup and operator input |
| At 25% intervals | For large batches; e.g. every 10th component in a batch of 40 |
| After tool changes or breaks | Ensure consistency is maintained before restarting full production |
| If an issue is suspected | Uneven cuts, blade noise, material resistance – check immediately |

3. What to Check During a Spot Check

| Aspect | Measurement/Indicator |
| --- | --- |
| Dimensions | Length, width, thickness using tape measure or callipers |
| Angle/square | Use a set square to verify right angles |
| Surface quality | Check for tear-out, chipping, or rough edges |
| Grain orientation | Ensure consistency for visible parts (frames, tops) |
| Consistency | Compare with previously accepted sample or template |

4. Tools and Techniques for Spot Checking

- Measuring tape

- Vernier callipers

- Set square or try square

- Sample template piece or jig

- Visual inspection under good lighting

- Written or digital spot check log sheet

🛈 All deviations should be immediately reported and documented if outside tolerance limits.

Facilitator Demonstration Tip

- Perform a live check of a machined piece against a sample or job card

- Show learners how to read the cutting list dimensions and use a caliper or rule to confirm

- Demonstrate how to mark a component that fails inspection for rework or discard

- Emphasise maintaining a traceable record of spot checks during a batch run

Activity Suggestion: Spot Check Exercise

Provide:

- A batch of mock or sample components (some accurate, some with minor flaws)

- A job card with cut specifications

- Ask learners to:

  - Measure and inspect 1 out of every 5 pieces

  - Mark those that pass and flag those that do not

  - Complete a short inspection record or checklist

  - Present their findings and propose corrective action where needed

Case Study: Missed Spot Checks Result in Batch Failure

A group of learners was cutting 40 drawer sides using a band saw. They did not perform any interim checks, and the fence had shifted after the first 10. As a result, 30 units were 3 mm too narrow and could not be assembled correctly.

Facilitator Prompts:

- What simple check would have detected this issue earlier?

- How could the learners have reduced the impact of the error?

- What changes should be made to workshop routines to improve early error detection?

Critical Thinking Questions

- How often should spot checks be done in a production run of 100 parts?

- What tools would you use to check angles and squareness?

- Why is it important to check the first few pieces before continuing with a full batch?

- What should you do if one part in a spot check is incorrect, but the rest have been cut?

- How can spot checks be integrated into standard operating procedures without slowing production?

## Applied Knowledge Introduction – PM-01-PS07

Introduction to Applied Knowledge

The applied knowledge that underpins this practical module enables the learner to develop a sound understanding of the characteristics of different types of timber and board materials, the defects that affect their quality, and the correct methods of handling these materials throughout the machining process. A firm grasp of this knowledge ensures that learners produce furniture components to required specifications, maintain safety in the workplace, and contribute to the overall efficiency and quality of production.

### Facilitator Notes: AK0701 – Understanding of Material and Defects

Facilitator Purpose

This session enables learners to understand the characteristics of timber and board materials used in furniture production and to develop the skill to identify defects that affect quality, strength, and safety. This knowledge allows learners to make informed decisions during material selection, preparation, and machining, thereby supporting quality assurance and reducing waste.

Learners will also begin to appreciate how material choices and defects influence tool wear, component finish, and end-user satisfaction.

Key Concepts to Cover

1. Common Materials Used in Furniture Manufacturing

| Category | Examples | Applications |
| --- | --- | --- |
| Hardwoods | Oak, Kiaat, Meranti | Frames, legs, visible structural components |
| Softwoods | Pine, Spruce | Internal structures, drawer boxes, sub-frames |
| Engineered Boards | Chipboard, MDF, Melamine-faced board, Plywood | Carcass construction, shelving, door panels |
| Veneer Boards | MDF or chipboard with wood veneer | Decorative panels, cost-effective surface finishes |

2. Material Properties That Affect Machining

| Property | Why It Matters |
| --- | --- |
| Grain direction | Influences surface finish and cutting direction |
| Moisture content | Affects expansion, contraction, and machine feeding |
| Hardness | Determines cutter wear and feed rates |
| Surface finish | May require special blade types or handling methods (e.g. melamine) |
| Stability | Warping or cupping impacts component flatness and alignment |

3. Common Timber Defects and Their Consequences

| Defect | Cause | Impact |
| --- | --- | --- |
| Knots | Natural part of the tree branch system | May weaken structure or chip cutters if large or loose |
| Splits/Checks | Shrinkage during drying | Reduces strength, especially at edges or ends |
| Warping/Cupping | Uneven drying or poor storage | Causes misalignment and poor contact with machine tables |
| Blue stain/Fungal decay | Moisture retention | Aesthetic downgrade; may indicate rot or contamination |
| Embedded nails/staples | Often found in reclaimed timber | Damages blades; poses serious safety risk |

Facilitator Demonstration Tip

Bring a selection of timber and board samples:

- Include clean, high-quality pieces as well as those with defects (e.g. knots, cupping, staining)

- Pass samples around for visual and tactile inspection

- Use a moisture meter or a metal detector wand to simulate quality control in the field

Activity Suggestion: Material Identification and Grading

Give each learner or group:

- A variety of timber and board samples

- A worksheet listing material types, defects, and potential outcomes

Ask them to:

- Identify the type of material

- Detect and name any defects present

- Decide whether the material is usable, must be trimmed, or should be rejected

- Explain how the defect would affect machining or final appearance

Case Study: Tool Damage from Unidentified Metal

A learner used reclaimed pine without performing a metal check. During the planing process, the machine made a loud noise and shut down. Inspection revealed a small embedded nail, which had damaged the cutter head. Production stopped for two hours while the machine was repaired.

Facilitator Prompts:

- What checks should have been carried out before machining?

- How could the learner have detected the metal without cutting?

- What steps should be added to the material inspection routine to avoid this?

Case Study: Warped Panels Lead to Assembly Issues

A batch of veneered MDF panels was stored incorrectly, leaning against a wall. By the time they were machined, they had warped slightly. This led to misaligned cabinet doors that had to be re-cut.

Facilitator Prompts:

- What storage method would have prevented this?

- How can warp be detected before machining?

- What could be done to recover slightly warped panels?

Critical Thinking Questions

- Why is it important to inspect timber and board materials before cutting or planing?

- What are the risks of using a material with a large knot in a structural furniture component?

- How can defect identification support waste reduction and sustainability in production?

- What role does moisture content play in determining the suitability of timber for machining?

- What is your responsibility as a learner or operator when you detect a defect in a material batch?

### Facilitator Notes: AK0702 – Material Handling

Facilitator Purpose

This session introduces learners to safe and efficient material handling procedures in a woodworking and furniture manufacturing environment. Material handling involves not only the movement and storage of raw boards and timber, but also maintaining material integrity, preventing injury, and supporting production workflow.

Learners will be guided to adopt best practices in manual and mechanical handling, storage, and workstation preparation, particularly when dealing with heavy boards, long pieces of timber, and delicate laminated or veneered surfaces.

Key Concepts to Cover

1. Importance of Safe Material Handling

- Prevents personal injury, especially to the back, shoulders, and hands

- Preserves material quality by avoiding scratches, warping, and impact damage

- Maintains order and workflow efficiency within the machine shop

- Supports compliance with Occupational Health and Safety (OHS) standards

2. Manual Handling Best Practices

| Technique | Purpose |
| --- | --- |
| Bend the knees, not the back | Prevents musculoskeletal injuries |
| Team lifting | Ensures safe handling of heavy or large panels |
| Maintain clear visibility | Reduces chance of collision or dropping materials |
| Keep materials close to the body | Improves balance and control |
| Use gloves when appropriate | Protects hands from splinters or board edges |

3. Mechanical Aids and Their Use

| Mechanical Aid | Function |
| --- | --- |
| Trolleys | Transport materials over short distances |
| Pallet jacks | Move bundled materials or board stacks |
| Roller conveyors | Assist in feeding long or heavy boards into machines |
| Vacuum lifters or hoists | Used in larger workshops to lift heavy boards safely |

🛈 Learners must always be trained before operating material handling equipment.

4. Safe Material Storage Guidelines

- Store boards flat and fully supported to prevent warping

- Use vertical racks for sheet goods where appropriate (with dividers)

- Stack materials by type, size, and project

- Label stored materials clearly to avoid incorrect use

- Never block emergency exits, walkways, or machine access areas

Facilitator Demonstration Tip

Demonstrate:

- Safe lifting of a sheet board with and without assistance

- Correct use of a trolley or roller stand to support long timber during machine feeding

- How to stack material safely on a pallet or rack

- Point out good vs poor storage examples within the workshop environment

Activity Suggestion: Material Movement and Storage Simulation

Set up a practice zone with:

- A small batch of melamine boards, pine lengths, and chipboard

- Mechanical aids such as trolleys or dollies

- Ask learners to:

  - Collect and move the materials using correct lifting or handling methods

  - Store the materials safely in a designated area

  - Justify their method based on material type and size

Award points for posture, communication, efficiency, and organisation.

Case Study: Damaged Panels from Improper Handling

A learner dragged a stack of melamine-faced chipboard across a steel table without protective padding. The abrasive surface scratched the laminate, leading to a visible finish defect on the final product.

Facilitator Prompts:

- What should the learner have done differently?

- How could this damage have been prevented?

- What tools or materials (e.g. cloth, spacers) can support surface protection?

Case Study: Workplace Injury from Improper Lift

A learner attempted to lift a full-size plywood sheet alone, twisting awkwardly and injuring their shoulder. They had not asked for help and there were no trolleys in sight.

Facilitator Prompts:

- Why is team lifting encouraged for large materials?

- How can the workshop layout better support safe handling?

- What safety culture practices can prevent such incidents?

Critical Thinking Questions

- Why is it important to match your handling technique to the size and weight of the material?

- What could happen if boards are stacked too high or stored unevenly?

- How can a well-organised material storage area improve overall workshop productivity?

- When is it appropriate to ask for assistance when handling material?

- What are three signs that material has been handled improperly?

### INTEGRATED ASSESSMENT TASK – PM-01-PS07

Assessment Type: Practical Knowledge Application

NQF Level: 2

Assessment Context: Workplace simulation or production environment

Case Study: Preparing Materials for the Production of Office Cabinets

You have been assigned to the machining department at CabinetWorks, where a production order for 60 office cabinets is being prepared. You receive a cutting list and routing sheet, a selection of solid pine and melamine-faced chipboard, and must prepare the materials for machining and hand them over to the next stage of production.

Your responsibilities include:

- Selecting suitable boards from available stock

- Checking boards for defects

- Following PPE protocols

- Interpreting the cutting list and routing sheet

- Sorting and storing materials safely

- Reporting issues and following internal communication procedures

Assessment Questions

Question 1
You are presented with five boards. Two are warped, one has visible knots near the edge, and one contains a large split. One board appears clean and undamaged.

- Identify which boards are acceptable and which are non-conforming.

- Briefly justify your decision using tolerance or defect indicators.

Question 2
You receive a cutting list that states:

- 60 panels – 700 mm × 400 mm melamine-faced chipboard

- 60 frames – 750 mm × 20 mm × 45 mm solid pine

Using the routing sheet and cutting list:

- What key details do you check before cutting begins?

- How would you ensure accuracy across the entire batch?

Question 3
During your shift, you identify that several boards have inconsistent thickness and are causing machine jams. Outline how you would report this problem following typical organisational procedures.

Question 4
After cutting, the components need to be sorted and stored.

- How should you safely stack the panels and frame pieces?

- What safety considerations apply when storing large or narrow parts?

Question 5
List three examples of personal protective equipment (PPE) that must be used during machining and explain the purpose of each.

✅ MODEL ANSWERS

Answer 1

- Reject the two warped boards and the one with a large split. These are outside acceptable tolerance and may cause machine feeding issues or lead to rejected components.

- The board with knots may be usable if the knots do not affect the cutting area.

- Accept the clean, undamaged board for use.

Answer 2

- Check dimensions, material type, quantity, and grain direction

- Confirm if edging or finishing is required post-machining

- Use a stop block or measuring jig for repetitive cutting

- Perform spot checks at intervals and compare with routing sheet

Answer 3

- Notify the supervisor verbally and place a “Do Not Use” tag on the remaining boards

- Complete a material fault log (if required)

- Document the batch affected and what was already processed

Answer 4

- Store panels flat on pallets or racks with protective spacers

- Stack pine frames by size with small supports to prevent bowing

- Do not stack above shoulder height

- Keep the floor area around storage clean and walkways clear

Answer 5

- Safety glasses – Protect eyes from flying debris or dust

- Hearing protection – Reduces exposure to loud machine noise

- Dust mask – Prevents inhalation of fine particles from cutting and sanding

🧾 MARKING MEMO

| Question | Criteria | Marks |
| --- | --- | --- |
| Q1 | Identifies 3 or more defects and applies tolerance-based judgement | 6 |
| Q2 | Interprets cutting list correctly; outlines batch control techniques | 6 |
| Q3 | Follows logical reporting steps and includes escalation | 4 |
| Q4 | Demonstrates safe stacking principles and hazard awareness | 4 |
| Q5 | Lists 3 PPE items with purpose explained | 5 |
|  | Total | 25 |

📊 ASSESSMENT RUBRIC

| Assessment Criteria | Outstanding (4) | Competent (3) | Developing (2) | Not Yet Competent (1) |
| --- | --- | --- | --- | --- |
| IAC0701 – Material Defect ID | Identifies multiple defects with accurate judgement | Identifies major defects correctly | Limited identification or uncertain judgement | Misidentifies or ignores key defects |
| IAC0702 – Cutting List Use | Interprets fully; applies controls for batch consistency | Understands dimensions and procedures | Partial interpretation; lacks full quality control | Misinterprets instructions or skips checks |
| IAC0703 – Reporting Procedures | Clear, professional, timely reporting with documentation | Verbal and/or written report completed | Partial reporting or vague sequence | No reporting or fails to follow procedure |
| IAC0704 – Handling and Storage | Organised stacking with safety awareness and material preservation | Safe and logical stacking demonstrated | Some stacking awareness but with minor safety oversights | Unsafe or disorganised material handling |
| IAC0705 – PPE Use | Lists and explains full PPE usage per task | Identifies correct PPE and usage | Incomplete or limited understanding | No or incorrect PPE identified |

### Facilitator Assessment Briefing

Practical Module: PM-01 – Operate a Range of Machines in the Wood Machine Shop to Cut Components for Furniture Manufacturing

Sub-task: PM-01-PS07 – Operate Various Machines in the Machining Department in Laminating, Breakout, Planing and Sanding Operations to Produce Timber Components to Specifications

Assessment Type: Integrated Practical Knowledge Assessment

Internal Assessment Criteria:

- IAC0701: Materials and material defects are identified according to their uses, applications and the tolerance standards to which they are subject in order to identify quality raw materials and reject non-conforming materials

- IAC0702: Cutting lists and routing sheets are interpreted in order to ensure components are correct

- IAC0703: Organisational reporting procedures are followed

- IAC0704: Materials are accurately sorted, handled and stacked safely and securely

- IAC0705: Personal protective equipment are selected and used correctly according to Health and Safety regulations and requirements

Purpose of the Assessment

This integrated assessment evaluates the learner’s ability to manage materials effectively within a furniture manufacturing environment. It focuses on the application of technical knowledge and workshop practices related to:

- Interpreting production instructions (cutting lists and routing sheets)

- Identifying suitable materials and recognising defects

- Implementing safety measures, including correct PPE selection

- Sorting, handling, and storing materials to maintain productivity and workplace order

- Following organisational reporting procedures in the case of defective stock or process interruptions

The learner must demonstrate accuracy, safety awareness, process understanding, and quality control through this workplace-simulated scenario.

Assessment Context

This assessment is set within a realistic machining department simulation or active production area. The learner is provided with a case study, cutting list, and mock materials to work with. They will be observed and evaluated on their decision-making, interpretation, reporting, and safety compliance.

Facilitator Instructions

- Ensure all materials (sample cutting list, timber samples, PPE) are prepared prior to assessment

- Read the case study with the learner to confirm understanding

- Provide the learner with tools for inspection, marking, and measuring

- Observe performance during all phases (material review, sorting, labelling, reporting)

- Mark the learner’s responses using the provided model answers, memo, and rubric

- Provide structured feedback, with time for clarification and remediation if necessary

## PM-01-PS08: Produce Profiled, Shaped and Cut Components to Specifications from Timber or Board

1. Introduction to the Practical Skill

This sub-task develops the learner’s ability to produce shaped, profiled, and machined furniture components from a variety of timber and board materials, in accordance with technical specifications, drawings, and cutting lists. The skill requires the interpretation of drawings, the selection and use of appropriate machines, and the ability to perform both simple and complex cutting operations safely and accurately.

Learners are expected to demonstrate proficiency in a wide range of cutting and shaping techniques—including straight cuts, drilling, profiling, joint cutting, moulding, and lathe work—as well as the correct use of jigs, templates, and cutting tools to achieve consistency and quality.

2. Scope of Practical Skill

Given a set of drawings, cutting list, and access to appropriate machines, the learner must be able to:

- PA0801 Perform simple cuts using small pieces of wood, or straight cuts using the radial arm and rip saw cross-cut

- PA0802 Produce complex cuts including curved, irregular shapes and deep cuts, long cuts, angle cuts, multi-facet cuts, and use of moulding machines

- PA0803 Operate machines and perform straight cuts, drilling, sanding, dowel drilling, dovetail cutting, mortise and tenon joinery

- PA0804 Operate a lathe, multi-cutter machines, routers, spindle moulders, and sanders

- PA0805 Work with different timber types including solid wood, boards, ply products, softwoods, and hardwoods

3. Applied Knowledge

- AK0801: Knowledge of various cutting and shaping techniques, including:

  - Chamfers, rebates, grooves, curves, and straight cuts

  - Turning techniques used on lathes and rotary shaping machines

Learners must understand how these techniques are applied to meet specification requirements and ensure that safety, surface finish, and functional fit are maintained.

4. Internal Assessment Criteria

To demonstrate competence in this task, learners must be able to meet the following assessment standards:

- IAC0801: Different profiles, shapes, rebates, and grooves are cut accurately according to job specifications

- IAC0802: Jigs and templates are used appropriately to produce consistent components

- IAC0803: The correct machines are selected for each job and confirmed to be in safe, working condition

- IAC0804: The correct cutting tools are used for shaping and profiling tasks

### Facilitator Notes: PA0801 – Perform Simple Cuts Using Small Pieces of Wood, or Straight Cuts Using the Radial Arm and Rip Saw Cross Cut

Facilitator Purpose

This session introduces learners to the correct procedures for performing basic cutting operations, with a focus on straight cuts and handling small workpieces. These are foundational machining tasks in furniture production, and must be carried out with precision and strict adherence to safety protocols.

Learners will practise operating radial arm saws and rip saws, and learn to handle and secure smaller components, where the risk of kickback and operator injury is higher. Emphasis is placed on tool control, setup alignment, and the use of safety aids such as push sticks, hold-down clamps, and fences.

Key Concepts to Cover

1. Simple Cutting Defined

- Straight cuts along or across timber grain

- Typically performed on rectangular, square, or small stock

- Can be for part sizing, trimming, or preparation for joinery

2. Machines and Their Uses

| Machine | Function | Common Uses |
| --- | --- | --- |
| Radial arm saw | Cross-cutting boards to length | Cabinet sides, shelving, small framing pieces |
| Rip saw | Longitudinal cuts along the grain | Strips for drawer sides, rails, edging material |
| Cross-cut station | Manual or semi-automatic straight cuts | Sizing batches of small parts quickly and safely |

3. Operating Procedure for Safe Simple Cuts

- Inspect timber for defects or foreign objects

- Mark cut lines using measuring tape and square

- Check blade height and alignment

- Secure small components with clamps or jigs

- Use push sticks or push blocks for narrow stock

- Keep hands at a safe distance from the blade path

- Perform a test cut when in doubt

4. Risks and How to Prevent Them

| Risk | Preventative Measures |
| --- | --- |
| Kickback | Use fence correctly; never freehand rip; keep wood flat |
| Material slippage | Clamp securely; use sacrificial jigs |
| Blade contact | Maintain hand safety zones; use push tools |
| Splintering or tear-out | Sharp blade; cut with the grain or use a backing board |

Facilitator Demonstration Tip

- Set up both a rip saw and radial arm saw with appropriate guards and fences

- Demonstrate:

  - How to position small offcuts for cutting

  - Use of a hold-down or push stick

  - The audible and visual difference between a well-set and poorly set saw

- Allow learners to practise with scrap wood before attempting accurate sizing

Activity Suggestion: Cutting Practice Exercise

Give learners:

- A marked timber board

- A cutting list (e.g. cut four 300 mm × 100 mm strips)

Ask them to:

- Plan and mark each cut

- Perform cuts using both a radial arm saw and a rip saw

- Measure finished parts for accuracy

- Stack pieces safely and inspect for defects (e.g. chipping)

Case Study: Kickback Incident with Small Stock

A learner attempted to rip a 40 mm wide strip from a short pine board without using a push stick or outfeed support. The board was pulled from their hands and thrown backwards. Fortunately, no injury occurred, but the incident highlighted improper handling.

Facilitator Prompts:

- What tool or technique could have prevented this?

- Why are small workpieces riskier to cut than long boards?

- What workshop policy should be in place for cutting narrow or short stock?

Critical Thinking Questions

- Why must small timber pieces be secured or supported before cutting?

- How do radial arm and rip saws differ in their cutting action and setup?

- What are the risks of cutting without a push stick or guiding fence?

- Why should test cuts be done before batch processing?

- How can jigs and templates improve both safety and accuracy for simple cuts?

### Facilitator Notes: PA0802 – Produce Complex Cuts for Curved, Irregular Shapes and Deep Cuts, Long Cuts, Angle Cuts, Multi-Facet Cuts and Moulding Machines

Facilitator Purpose

This session builds learner proficiency in performing non-standard or intricate cutting operations, using appropriate machines and techniques to shape timber and board materials according to detailed specifications. These complex cuts are common in high-end furniture, customised components, and stylistic elements such as mouldings, angles, and decorative curves.

Learners will learn to use advanced tooling safely and accurately while interpreting cutting lists, drawings, and templates. This includes understanding tool profiles, machine adjustments, and setup precision.

Key Concepts to Cover

1. What Are Complex Cuts?

| Type of Cut | Example/Application |
| --- | --- |
| Curved and irregular shapes | Chair backs, decorative panels, arches |
| Deep and long cuts | Frame grooves, joinery slots, thick-section trimming |
| Angle and multi-facet cuts | Mitres, compound cuts, hexagonal frames, moulding transitions |
| Moulding | Skirtings, cornices, frame profiles using spindle moulders |

2. Machines Used for Complex Cuts

| Machine | Primary Use |
| --- | --- |
| Band saw | Curved cuts, internal shaping |
| Jig saw (scroll saw) | Tight radius, decorative detail work |
| Spindle moulder/router | Profiling, moulding, grooving, rebating |
| Mitre saw/compound saw | Accurate angle cuts, bevelled edges |
| Circular saw with jig | Deep or repeat angled cuts |

3. Setup and Execution Principles

- Use templates or jigs to guide complex shapes

- Clamp materials securely to prevent vibration or drift

- Select correct tool profiles or blade types for each job

- Make test cuts on offcuts to confirm accuracy and finish

- Cut in multiple shallow passes for deep or intricate profiles

- Use dust extraction and slow feed rate for delicate workpieces

- Always refer to drawings or routing sheets for profile accuracy

Facilitator Demonstration Tip

- Show how to cut a decorative curve on a band saw using a template

- Demonstrate moulding profile setup using a spindle moulder/router

- Use offcuts to show what happens when the feed is rushed or a blade is dull

- Let learners feel the difference between shallow passes vs deep single cuts

If available, show a side-by-side of a correctly cut vs overcut or chipped component.

Activity Suggestion: Complex Profile Practice

Assign each learner:

- A drawing of a curved or mitred profile

- A band saw or router station with safety aids

- Have them:

  - Trace the template onto a board

  - Perform the cut in stages

  - Sand or refine the shape using hand tools

  - Compare against the drawing or sample for dimensional accuracy

Case Study: Inconsistent Frame Mitres

A learner used a mitre saw to cut angles for a hexagonal table frame but failed to lock the saw at the correct angle each time. As a result, the mitre joints were inconsistent, causing visible gaps and misalignment.

Facilitator Prompts:

- What caused the inconsistency in this case?

- How should the saw setup have been verified?

- What tools or methods ensure repeatable cuts during angle-based batch work?

Critical Thinking Questions

- Why is it important to use templates or jigs for irregular shapes?

- What risks are associated with deep cutting in a single pass?

- How can moulding profiles be checked before running a full batch?

- What factors determine the choice of blade or bit for complex cuts?

- What precautions should be taken when changing from a simple cut to a multi-faceted angled cut?

### Facilitator Notes: PA0803 – Operate Machines and Perform Straight Cuts, Drilling, Sanding, Dowel Drilling, Dovetail Cutting, Mortise and Tenon

Facilitator Purpose

This session provides learners with the opportunity to develop their technical proficiency in a variety of precision machining operations, including straight cutting, joint preparation, and surface finishing. These operations are essential for producing furniture components that are both structurally sound and visually appealing.

The focus is on correct machine operation, tool selection, feed techniques, and maintaining accuracy and repeatability. Learners will practise producing parts that are ready for assembly, gluing, or finishing, using a range of machinery found in most furniture workshops.

Key Concepts to Cover

1. Machine-Based Operations in Focus

| Operation | Machine(s) Used | Purpose |
| --- | --- | --- |
| Straight cutting | Panel saw, table saw, radial arm saw | Sizing components and preparing blanks |
| Drilling | Drill press, hand drill | Creating dowel holes, screw holes, or fitting guides |
| Dowel drilling | Horizontal borer, dowel jig | Ensuring alignment for dowel-based joints |
| Dovetail cutting | Dovetail jig with router, specialised jointer | Joinery for drawers, boxes, traditional carcass work |
| Mortise and tenon | Mortiser, tenoner, router | Strong frame joints in tables, doors, and structural frames |
| Sanding | Edge sander, orbital sander, stroke or drum sander | Surface preparation for finishing and component smoothing |

2. Setup and Safety for Each Operation

| Machine | Key Setup Points | Safety Measures |
| --- | --- | --- |
| Panel/Table Saw | Align fence, adjust blade height | Use push sticks and safety guards |
| Drill Press | Secure workpiece, choose correct drill bit, set depth stop | Clamp small pieces, wear goggles, keep hands away from chuck |
| Horizontal Borer | Set drilling depth and fence stops | Clear shavings regularly, don’t lean into moving parts |
| Dovetail Jig + Router | Choose cutter size, test on scrap, set cutting depth | Use dust extraction, hold router firmly with both hands |
| Mortiser and Tenoner | Mark centreline, use stops for repeatable cuts | Never adjust while machine is running |
| Sanders (all types) | Use correct abrasive grit, check tracking and belt tension | Don’t apply excessive pressure; let the machine do the work |

Facilitator Demonstration Tip

Prepare a demonstration that shows:

- Drilling a dowel hole in one board, aligning with another using a jig

- Making a dovetail joint and showing a fitting sample

- Creating a basic mortise and tenon frame corner

- Sanding a machined panel and identifying how grit progression improves finish

Discuss how minor setup errors (e.g. a 1 mm shift in dowel alignment) can affect the whole assembly.

Activity Suggestion: Joint Accuracy Task

Provide:

- Pre-cut blank components for a simple box or frame

- Learners must:

  - Mark and drill dowel holes or create mortise and tenon joints

  - Assemble dry-fitted components to check for alignment

  - Sand all external faces using appropriate machines

  - Complete a short checklist confirming measurements and tolerances

Include an optional step for those ready: cut dovetails and fit a drawer front.

Case Study: Misaligned Dowel Joints in Drawer Assembly

During assembly, a learner found that the dowel holes in the drawer sides and fronts did not align, causing angled fitment and stress cracks during gluing. On inspection, the jig fence had not been clamped firmly, leading to offset holes.

Facilitator Prompts:

- What should have been checked before drilling began?

- How could a test piece have prevented this?

- What reporting steps should follow if incorrect joints are found during assembly?

Critical Thinking Questions

- What factors determine whether to use a dowel, dovetail, or mortise and tenon joint?

- Why is depth and spacing accuracy so critical in joint-making operations?

- How can sanding be optimised to ensure a smooth finish without rounding corners?

- What are the advantages of using a horizontal borer over a handheld drill for dowel placement?

- Why is it important to check cutter sharpness and rotation direction before router-based joinery work?

### Facilitator Notes: PA0804 – Operate a Lathe, Multi Cutter Machines, Routers, Spindle Moulders and Sanders

Facilitator Purpose

This session introduces learners to the operation of a diverse range of shaping machines, each of which plays a specialised role in producing furniture components with curves, profiles, contours, and refined surfaces. Emphasis is placed on machine familiarity, tool setup, material preparation, and operator safety.

Learners must demonstrate confidence in selecting the right machine for the job, preparing the machine correctly, and producing shaped components to specification, whether for legs, edges, mouldings, profiles, or turned elements.

Key Concepts to Cover

1. Overview of Machines and Functions

| Machine | Function/Use |
| --- | --- |
| Wood lathe | Produces turned components (e.g. chair legs, balusters, knobs) |
| Multi-cutter machine | Shapes complex or repetitive profiles using multiple heads or stages |
| Hand-held router | Used for edge shaping, groove cutting, and joinery slots |
| Spindle moulder | Shapes and moulds straight or curved edges using large rotating cutters |
| Sanding machines | Smooth surfaces or contours; includes drum, edge, and orbital sanders |

2. Safety and Setup Guidelines for Each Machine

| Machine | Key Safety Practices |
| --- | --- |
| Lathe | Check tool rest clearance, balance workpiece, wear face shield |
| Multi-cutter | Confirm cutter alignment and locking; feed material with push blocks |
| Router | Check rotation direction, use sharp bits, control depth per pass |
| Spindle moulder | Secure cutter head, use guide fence or pressure pad, feed against rotation |
| Sander | Use correct grit, adjust speed for material type, avoid applying pressure |

🛈 Always verify that safety guards, emergency stops, and dust extraction systems are functioning before operating.

3. Tool and Material Selection Considerations

- Choose cutter profile and diameter based on drawing or specification

- Select material appropriate for the tool and operation (e.g. softwood for turning; hardwood for detailed moulding)

- Use template jigs for repeatability where applicable (e.g. spindle moulder shaping of identical components)

- Inspect timber for knots or cracks that could cause dislodgement during turning or profiling

Facilitator Demonstration Tip

Set up a station for each machine (or use visual aids where equipment access is limited):

- Lathe: Turn a simple taper or rounded form. Emphasise balance, tool positioning, and consistent pressure.

- Router: Demonstrate creating a groove or decorative edge on pine.

- Spindle moulder: Set up a basic rebate or ogee profile using a cutter block and fence.

- Sander: Show proper feed and handling techniques on an edge sander or drum sander.

Encourage learners to practise machine setup procedures even before running materials through.

Activity Suggestion: Machine Operation Rotation

Create a machine-rotation circuit where learners spend 10–15 minutes at each station:

- Identify the machine and describe its purpose

- Perform basic setup (under supervision)

- Operate the machine to produce a small test piece

- Inspect the output and suggest adjustments if needed

Learners complete a log sheet noting tool type, setup steps, and outcome observations.

Case Study: Router Tear-Out on Hardwood Panel

A learner used a hand-held router to create a decorative groove on an oak door rail. The bit was dull and the feed direction went with the grain. The result was a jagged surface with splintering. The piece was unusable.

Facilitator Prompts:

- What were the technical errors in setup and operation?

- How can router direction and sharpness be checked?

- What steps should be added to a pre-operation checklist?

Critical Thinking Questions

- How does the function of a spindle moulder differ from that of a router?

- Why must lathes be balanced and tool rests adjusted before turning begins?

- What safety checks must always be done before using multi-head shaping machines?

- How can template use improve efficiency and consistency in shaping operations?

- What are the risks of sanding with excessive pressure, and how can they be avoided?

### Facilitator Notes: PA0805 – Work with Different Timber such as Boards, Ply Products, Softwoods and Hardwoods

Facilitator Purpose

This session is designed to ensure that learners can correctly identify, select, and work with various types of timber commonly used in the furniture manufacturing industry. Each material type—whether solid wood or board—requires specific techniques, tooling, and machine settings for safe and accurate machining.

Learners must develop an understanding of the behaviour and characteristics of these materials during shaping, cutting, sanding, and assembly, and adjust their approach accordingly to maintain quality and avoid tool damage or operator risk.

Key Concepts to Cover

1. Types of Timber and Board Materials

| Material Type | Examples | Typical Use |
| --- | --- | --- |
| Softwoods | Pine, spruce | Frames, carcasses, drawer sides |
| Hardwoods | Oak, kiaat, meranti | Visible components, legs, decorative panels |
| Plywood | Multi-layered veneer sheets | Drawer bottoms, cabinet backs, curved forms |
| Melamine/Chipboard | Particleboard with melamine coating | Carcasses, shelves, prefinished parts |
| MDF | Medium-density fibreboard | Flat panels, routed doors, shaped profiles |

2. Working Characteristics of Each Material

| Property | Softwood | Hardwood | Ply/Melamine/MDF |
| --- | --- | --- | --- |
| Tool wear | Low to moderate | High – dense fibres | Moderate to high – melamine is abrasive |
| Chipping risk | Low | Low to moderate | High (especially with melamine edges) |
| Cutting direction | With the grain | With the grain | Requires scoring to avoid tear-out |
| Surface quality | Smooth with sharp tools | Very smooth if cut well | Can splinter or burn if incorrect blade used |
| Feed rate | Fast | Slow and steady | Slow, constant speed with sharp blades |

3. Adapting Techniques to Timber Type

- Use fine-tooth blades for melamine and MDF to reduce chipping

- Reduce cutting speed or depth when shaping dense hardwoods

- Avoid forcing materials—let the blade do the work

- Use dust extraction and wear masks when cutting boards with resins or formaldehyde (e.g. MDF)

- Prepare different jigs or clamping systems for warped vs flat materials

- Apply correct sanding pressure and grit selection based on the hardness of the timber

Facilitator Demonstration Tip

Provide a variety of timber and board samples:

- Cut or route a straight groove in pine, then in MDF

- Let learners observe differences in resistance, edge quality, and dust

- Pass around finished and unfinished samples for tactile comparison

- Use magnification or raking light to show chipped vs clean-cut edges

Highlight real examples of why correct blade selection and setup is critical for each material.

Activity Suggestion: Timber Identification and Handling Drill

Set up a table with:

- Samples of pine, meranti, oak, MDF, melamine, plywood

- Identification tags and cutting guidelines

Ask learners to:

- Identify each material by sight and touch

- List at least two appropriate machining techniques for each

- Recommend the best blade or bit for machining that material

- Explain any health and safety considerations (e.g. dust, tool selection)

Case Study: Edge Tear-Out on Melamine Shelves

A learner cut melamine-faced chipboard on a panel saw using a general-purpose blade. The underside of each panel chipped severely, requiring edge filling and masking. The damage delayed the assembly of an entire cabinet batch.

Facilitator Prompts:

- What blade or setup change could have prevented the tear-out?

- Why is it important to use a scoring blade or fine-tooth saw for coated boards?

- How should the learner adjust the feed rate for board materials?

Critical Thinking Questions

- What makes hardwoods more challenging to machine than softwoods?

- Why do coated boards like melamine require specialised blades or scoring blades?

- What role does feed rate play in producing clean cuts across different timber types?

- What are the dangers of machining materials with hidden voids or knots?

- How can incorrect tool selection for a material lead to health and safety hazards in the workshop?

### Facilitator Notes: AK0801 – Chamfer, Rebates, Grooves, Curves, Straight Cuts, Turning Techniques

Facilitator Purpose

This session enables learners to understand the forms and functions of various cutting and shaping techniques, and how each is applied to timber and board materials during machining operations. These operations form the aesthetic and functional foundation of furniture joinery, detailing, and assembly.

The focus is on recognising when and how to apply each technique, the tools and machines required, and the tolerances and finish quality expected for each profile or shape. This theoretical grounding will support the successful completion of both basic and complex machining tasks.

Key Concepts to Cover

1. Understanding Each Technique

| Technique | Description | Common Application |
| --- | --- | --- |
| Chamfer | Angled edge cut, usually 45° | Decorative edges, easing corners, frame work |
| Rebate (Rabbet) | Step-like recess along edge or face of board | Cabinet backs, door and drawer joinery |
| Groove | Slot cut into surface (often parallel to the edge) | Panel inserts, shelf dadoes |
| Curve | Arched or rounded cuts using bandsaws, jigsaws, or lathes | Chair backs, decorative panels |
| Straight cut | Linear cut across or along the grain | Sizing material, forming the base of components |
| Turning | Shaping material while it spins on a lathe | Chair legs, balusters, decorative knobs and spindles |

2. Tools and Machines Typically Used

| Technique | Primary Equipment |
| --- | --- |
| Chamfer | Router with chamfer bit, table saw with blade tilt |
| Rebate | Spindle moulder, rebate cutter, router, or dado stack |
| Groove | Table saw with dado blade, router, spindle moulder |
| Curve | Bandsaw, scroll saw, jigsaw, template router |
| Straight cut | Panel saw, radial arm saw, table saw |
| Turning | Lathe with turning chisels and centres |

3. Functionality and Precision

- Chamfers and grooves often require exact depth and angle, especially if part of a joint

- Grooves and rebates must be clean, splinter-free, and cut with the grain for strength

- Curves must follow drawing or template lines, with consistent radius and smooth finish

- Straight cuts form the foundation for all other shaping; errors here carry through the entire component

- Turning techniques must consider symmetry, balance, and tool sharpness

Facilitator Demonstration Tip

Use timber samples to:

- Show what each profile looks like (real examples or cross-section diagrams)

- Cut a groove and a rebate using a router or moulder

- Turn a simple shape on a lathe and show progressive stages (block > rounded > finished form)

- Demonstrate a chamfer with a hand plane or a router with a guided bit

Encourage learners to inspect and label the different profiles and discuss where they’ve seen them in real furniture.

Activity Suggestion: Profiling Recognition and Function Task

Provide:

- A tray of offcuts or demo blocks, each with a different shaping technique applied

- Learners must:

  - Identify the technique used

  - Name the tool or machine used

  - Explain the purpose of the shape in a furniture application (e.g. “chamfer to soften edge of table leg”)

  - Match it to a photo or drawing of a real furniture component

Case Study: Rebate Too Deep on Cabinet Side

A learner set up a router to cut a 6 mm rebate on a cabinet side panel for a backboard. They misread the depth gauge and cut it at 10 mm. As a result, the panel edge became too thin and cracked when the cabinet was assembled.

Facilitator Prompts:

- How could this error have been prevented during setup?

- What effect did it have on the component’s structural integrity?

- How does this highlight the importance of understanding profile specifications?

Critical Thinking Questions

- What is the functional difference between a groove and a rebate?

- Why must turning on a lathe be done with balanced, properly mounted timber?

- What happens if the depth of a groove or rebate is too shallow or too deep?

- Why are chamfers often applied to visible edges of furniture components?

- How does understanding shaping techniques improve communication between design, machining, and assembly teams?

### INTEGRATED ASSESSMENT TASK – PM-01-PS08

Assessment Type: Practical Knowledge and Process-Based Task

NQF Level: 2

Credits: 20

Assessment Context: Workshop-based simulation or actual production task

Case Study: Producing and Finishing Wooden Bedside Table Components

You are working in the machining department of OakCraft Interiors, preparing shaped and profiled components for a batch of bedside tables. During the process, you notice that some of the shaped legs have minor surface faults, one panel is cracked, and a batch of shelf rails has mismatched profiles. You must decide how to deal with these issues, ensure that all materials are stacked safely, and identify the type of finishing products to be applied before the parts are sent to the spray booth.

Assessment Questions

Question 1
You inspect a batch of 10 profiled legs. Three have slight tear-out at the edges, and one has a deep groove not shown on the drawing.

- What actions would you take to rectify the faults or identify the rejects?

- What tools or techniques might you use?

Question 2
After machining is completed, you need to stack the legs and side panels in a shared storage area.

- Describe how you would handle and stack the components to ensure safety and prevent damage.

- What labelling or spacing precautions would you take?

Question 3
The routing sheet specifies that the components will be spray-finished. The label on the tin of wood stain says: “Clean brushes with mineral turpentine.”

- How would you categorise this finishing material?

- What health and safety considerations apply when working with this product?

✅ MODEL ANSWERS

Answer 1

- Light tear-out can be corrected by sanding or trimming; the deep groove is outside tolerance and must be rejected.

- Use fine-grit sandpaper or a hand plane to clean up small defects. Tag or mark unusable items as rejects and record them in the material fault log.

Answer 2

- Stack panels flat on a rack or pallet with spacers between layers; stand legs upright in a rack or tie them in bundles.

- Use padding to prevent rubbing or edge damage. Label each stack with job number, part type, and quantity. Keep aisle space clear and stack below shoulder height.

Answer 3

- The product is spirit-based (mineral turpentine is a solvent for spirit-based products).

- Ensure good ventilation, wear gloves and a respirator if spraying, and store the product away from heat and flame. Dispose of rags and brushes safely as they may be flammable.

🧾 MARKING MEMO

| Question | Criteria | Marks |
| --- | --- | --- |
| Q1 | Identifies repairable vs rejectable faults; outlines correct steps | 6 |
| Q2 | Describes safe handling and stacking with clear safety rationale | 6 |
| Q3 | Correctly categorises finishing product; lists relevant safety rules | 5 |
|  | Total | 17 |

📊 ASSESSMENT RUBRIC

| Assessment Criteria | Outstanding (4) | Competent (3) | Developing (2) | Not Yet Competent (1) |
| --- | --- | --- | --- | --- |
| IAC0901 – Fault Identification | Recognises fault severity; correct rectification or rejection applied | Identifies faults and attempts suitable response | Limited recognition or unclear rectification action | Fails to identify or improperly handles fault |
| IAC0902 – Material Handling | Safe, labelled, well-spaced storage; full explanation of method | Safe stacking; provides rationale for method | Some awareness of stacking principles; minor safety gaps | Unsafe stacking or disorganised material handling |
| IAC0903 – Product Classification | Correctly identifies base type; provides multiple safety measures | Identifies base type and mentions at least one safety rule | Unclear classification; limited safety consideration | Incorrect classification and no safety awareness |

## PM-01-PS09: Inspect the Physical Product Visually and by Feel, Checking Against Specification and Applying Tolerances to Ensure Quality and Accuracy

1. Introduction to the Practical Skill

This sub-task equips learners with the skills required to conduct systematic inspection of machined timber and board components, ensuring they comply with technical drawings, dimensional tolerances, and surface quality standards. Inspections must be conducted both visually and by feel, enabling early detection of faults caused by material defects, machine wear, or operator error.

The learner is required to identify and differentiate between component faults, process faults, and machine faults, and determine whether a part can be rectified or must be rejected. In addition, the learner must be able to inspect paintwork for issues such as incorrect viscosity, over-spraying, and contamination—thereby ensuring that finishing processes meet quality and safety expectations.

2. Scope of Practical Skill

Given a range of machined timber and board components, including examples with faults, defects, and paint inconsistencies, the learner must be able to:

- PA0901 Inspect the machined product visually and by feel to ensure compliance with product specifications

- PA0902 Check the machined product against specification while applying tolerances

- PA0903 Identify component faults such as:

  - Lack of squareness

  - Incorrect dimensions

  - Knots causing structural or visual issues

  - Roughness, scratches, or surface inconsistencies

- PA0904 Identify process faults such as:

  - Blade marks, burn marks, excess moisture content in timber

  - Paint defects including contamination, incorrect mixing, running, or overspray

- PA0905 Identify machine faults such as:

  - Blunt blades, incorrect sanding grit, nozzle defects

  - Air pressure issues and extraction imbalances affecting finishing quality

3. Applied Knowledge

- AK0901: Awareness of different types of faults related to components, processes, and equipment

- AK0902: Understanding of paints and their characteristics, including spirit-based and oil-based finishes, and the conditions required for proper application and drying

Learners must be capable of using this knowledge to make informed decisions about component conformity and how to respond when faults occur in the machining or finishing process.

4. Internal Assessment Criteria

Learners will be assessed on their ability to:

- IAC0901: Rectify minor faults where possible or clearly identify non-conforming parts for rejection

- IAC0902: Handle and stack inspected materials safely and according to size and finish sensitivity

- IAC0903: Accurately categorise paints used in the finishing process as spirit-based or oil-based, and explain relevant safety and application implications

### Facilitator Notes: PA0901 – Inspect the Machined Product Visually and by Feel to Ensure Compliance with Product Specifications

Facilitator Purpose

This session is aimed at developing the learner’s ability to perform quality inspections using sight and touch to assess whether machined components meet required specifications. In production, a visual and tactile inspection is often the first line of defence in detecting dimensional inaccuracies, surface flaws, or defects caused by material or machinery issues.

This foundational quality control skill supports accuracy, prevents defects from progressing to assembly, and ensures that only components of acceptable standard continue in the manufacturing process.

Key Concepts to Cover

1. What to Look for During a Visual and Tactile Inspection

| Inspection Focus Area | Examples of Faults Detected |
| --- | --- |
| Dimensions | Oversized or undersized components; misaligned cuts |
| Edges and corners | Rough edges, splinters, chips, sharp burrs |
| Surface quality | Scratches, tear-out, burns, dents, machine marks |
| Profile accuracy | Incorrect groove depth, misaligned rebates, off-centre chamfers |
| Flatness/squareness | Warped panels, bowed boards, out-of-square ends |
| Finish readiness | Inconsistent sanding, missed spots, signs of tool marks under finishes |

🛈 “By feel” includes running hands gently over surfaces to detect roughness, sharpness, or inconsistencies that may not be visible.

2. Tools to Support Visual Inspection

- Steel ruler or measuring tape

- Vernier calliper

- Set square or combination square

- Sample component for comparison

- Quality checklist or job card specification sheet

- Torch or raking light to highlight surface inconsistencies

3. Inspection Timing in the Workflow

| Stage | Why It Matters |
| --- | --- |
| Immediately after machining | Catches issues before sanding or assembly |
| After shaping or profiling | Ensures accuracy before complex joinery |
| Before finishing | Prevents coating over scratches or unresolved faults |

Facilitator Demonstration Tip

Use two contrasting boards:

- One machined correctly

- One with visible and tactile faults (e.g. a burn mark, scratch, slightly rounded edge)

Demonstrate:

- How to run your fingers along an edge to check for sharpness or splinters

- How to use a set square to check squareness

- How to compare against a specification or template piece

Encourage learners to inspect with their eyes at surface level and under proper lighting.

Activity Suggestion: Sample Fault-Finding Drill

Set up 5–6 machined components with intentional defects (e.g. undersize, uneven sanding, splintered edges).
Ask learners to:

- Visually inspect and touch each item

- Record all defects observed

- Categorise each item as acceptable, requires rework, or reject

- Justify decisions using the job specification

Allow peer discussion to compare inspection decisions and refine their approach.

Case Study: Missed Fault Causes Rework in Assembly

A learner passed a batch of side panels to assembly without noticing a subtle blade mark on the front edge. After finishing, the mark became more pronounced and the panels had to be sanded down and re-sprayed, delaying the project.

Facilitator Prompts:

- What inspection technique might have revealed the fault earlier?

- Why is tactile inspection just as important as visual inspection?

- How does missing a fault early affect time, cost, and morale?

Critical Thinking Questions

- What can your fingers detect that your eyes might miss during a component inspection?

- How can comparing components against a sample improve inspection accuracy?

- Why should inspection take place before finishing or assembling a component?

- What impact does a consistently applied inspection routine have on workshop productivity?

- What should be done with components that fail inspection—how should they be recorded or marked?

### Facilitator Notes: PA0902 – Check the Machined Product Against Specification While Applying Tolerances

Facilitator Purpose

This session teaches learners how to inspect furniture components against specified measurements and tolerances, ensuring that each part meets dimensional requirements within an acceptable range. Understanding tolerances is critical for achieving consistent part fit, avoiding rework or rejection, and supporting quality assurance in production.

The learner must demonstrate the ability to use measuring instruments, interpret dimensions from cutting lists or drawings, and apply tolerance allowances in a workshop environment.

Key Concepts to Cover

1. What Are Tolerances?

- Tolerance is the permissible variation from a specified measurement

- Usually stated as ± a specific value (e.g. ±1 mm)

- It allows for minor, acceptable deviations that do not affect fit, function, or appearance

2. Examples of Common Tolerances in Woodworking

| Component | Specification | Tolerance |
| --- | --- | --- |
| Cabinet shelf panel | 600 mm × 400 mm | ±1 mm |
| Drawer side thickness | 16 mm | ±0.5 mm |
| Dowel hole alignment | 32 mm centre distance | ±0.2 mm |

🛈 Tighter tolerances apply where parts must fit or align perfectly; looser tolerances may be allowed in hidden or trimmed areas.

3. Measuring Tools for Accuracy Checking

| Tool | Use |
| --- | --- |
| Measuring tape | General length and width measurements |
| Steel rule | More accurate straight measurements up to 300 mm |
| Vernier calliper | Precise measurements (e.g. thickness, hole diameters) |
| Set square | Ensures squareness and 90° angles |

Encourage learners to always measure from the same reference point and to avoid measuring against uneven surfaces.

Facilitator Demonstration Tip

Show how to:

- Read a specification (e.g. “Panel must be 500 mm × 300 mm ±1 mm”)

- Measure a board and decide if it is within tolerance

- Use a vernier calliper to check part thickness and interpret readings

- Mark components that pass, require trimming, or must be rejected

Let learners practise measuring from the same batch and discuss slight variations that fall within tolerance.

Activity Suggestion: Tolerance Verification Challenge

Provide:

- A job card with exact dimensions and tolerance

- 6–8 pre-cut sample parts with slight differences in size
Learners must:

- Measure and record each part’s dimensions

- Apply tolerance to determine acceptability

- Categorise each part (Accept / Rework / Reject)

- Justify decisions in writing or during discussion

Case Study: Assembly Delays Due to Misapplied Tolerance

A learner assumed a ±3 mm tolerance for a frame rail that was actually ±0.5 mm. The oversized rail caused poor alignment in the frame, requiring re-machining of all components.

Facilitator Prompts:

- Why is it important to confirm the stated tolerance before machining or checking?

- How might a tolerance mistake affect the entire batch of components?

- What communication can prevent these issues between planning, machining, and QC?

Critical Thinking Questions

- What happens if a component is within specification for length but not for squareness?

- Why is it important to understand both numerical size and tolerance in a job card?

- What role does consistency in measurement method play in quality control?

- When should a component outside of tolerance be reworked versus rejected?

- What are the risks of not recording which components passed or failed tolerance inspection?

### Facilitator Notes: PA0903 – Identify Component Faults Such as Squareness of the Component, Incorrect Size, Knots Causing Rejects, Smoothness and Scratches

Facilitator Purpose

This session provides learners with the ability to identify visible and dimensional faults in machined furniture components before they progress to finishing or assembly. These faults may be due to material defects, machine setup issues, or operator error, and must be identified early to maintain product quality, avoid rework, and reduce material wastage.

Learners will practise detecting faults using measuring tools, surface inspection techniques, and comparison against job specifications and tolerances.

Key Concepts to Cover

1. Common Component Faults

| Fault | Description | Effect |
| --- | --- | --- |
| Out of square | Edges are not 90°, caused by incorrect saw alignment | Poor fit in frames or panels, misalignment in final product |
| Incorrect size | Dimensions outside tolerance | Gaps, loose or tight joints, failed assemblies |
| Knots causing rejection | Large, loose, or cracked knots in critical areas | Weakens the structure or causes aesthetic issues |
| Roughness | Raised grain, poor sanding, or planing marks | Unacceptable feel, leads to poor finish adhesion |
| Scratches | Caused by handling or machine marks | Visible after finishing, may require re-sanding or filler |

2. Inspection Techniques

| Fault Type | Inspection Method |
| --- | --- |
| Squareness | Use a set square along all corners and joints |
| Size | Measure with a steel rule or tape; verify against job card |
| Knots | Visually inspect and press to check for looseness |
| Surface quality | Use touch to feel for inconsistencies; raking light for scratches |
| Profile conformity | Compare with template or sample component |

Encourage learners to record faults and tag non-conforming components clearly.

Facilitator Demonstration Tip

Use real or sample parts to:

- Show a panel that is just slightly out of square

- Show two panels—one with a tight knot, another with a cracked, failing knot

- Feel for raised grain or tooling scratches with fingertips

- Measure a drawer side against the specified size and explain the effect of a 2 mm deviation

Let learners practise inspections and explain their judgement as “acceptable”, “requires rework”, or “reject”.

Activity Suggestion: Fault Spotting Drill

- Lay out 6–8 pre-machined parts (some correct, others with faults)

- Give learners a specification sheet and basic tools

- Ask them to:

  - Identify faults

  - Categorise components

  - Record faults and suggest corrective action (if possible)

Debrief as a group, comparing interpretations and reinforcing the value of objective checking criteria.

Case Study: Assembly Issues Caused by Missed Squareness Fault

A learner approved a batch of small cabinet side panels without checking squareness. During assembly, several units had gaps at the joints, requiring planing and re-cutting of entire panels.

Facilitator Prompts:

- What tool could have revealed the squareness issue?

- How would a small error in angle cause a major alignment issue in a box-like product?

- What quality assurance system could prevent these oversights?

Critical Thinking Questions

- How do you decide whether a knot is acceptable or makes a component unsuitable?

- Why is it important to inspect all edges and faces, not just one or two?

- What are the consequences of not detecting scratches or rough areas before finishing?

- When a component is out of square, what process or setup should be rechecked?

- How can your inspection records support accountability and traceability in production?

### Facilitator Notes: PA0904 – Identify Process Faults

Facilitator Purpose

This session equips learners to identify process faults arising during the machining and finishing of timber and board materials. A process fault occurs when an issue in machine setup, tooling condition, material preparation, or finishing technique results in a defect—even when the material itself is sound.

Learners must be able to recognise the signs of process faults, understand their root causes, and recommend appropriate corrective actions to maintain quality control in the production cycle.

Key Concepts to Cover

1. Typical Machining and Finishing Process Faults

| Fault | Description | Possible Cause |
| --- | --- | --- |
| Blade marks | Lines or grooves visible after cutting or planing | Blunt blades, machine vibration, feed speed inconsistencies |
| Burn marks | Scorch marks along cuts or surfaces | Blunt blade, feed rate too slow, friction buildup |
| Moist timber defects | Swelling, warping, poor finish adhesion | Timber not dried to proper moisture content |
| Paint contaminated with water | Cloudy or streaky paint finish | Water mixed into spirit-based or oil-based paints |
| Over-spraying | Excess paint beyond intended area, causing texture problems | Incorrect spraying technique or air pressure too high |
| Running/dripping paint | Vertical paint runs on surfaces | Paint applied too thickly or incorrect viscosity |
| Wrong paint mixing | Poor curing, uneven colour, tacky finish | Mixing incompatible products (e.g., oil and spirit-based) |
| Viscosity issues | Paint either too thin or too thick | Incorrect thinning or poor product storage |
| Cut inconsistencies | Variable dimensions across batch | Inconsistent machine settings, operator error |

2. Inspection and Detection Methods

| Fault Type | Inspection Method |
| --- | --- |
| Machining marks | Visual inspection with raking light; feel with fingertips |
| Surface burns | Visual inspection for discolouration, roughness |
| Moisture content | Use a moisture meter; acceptable range typically 8–12% |
| Paint defects | Visual inspection in strong light; check product labels |
| Dimensional consistency | Measurement against specification sheet |

Learners must perform inspections systematically, noting both visual and tactile cues.

Facilitator Demonstration Tip

Set up a series of samples showing:

- Correct vs blade-marked cuts

- Smooth vs burnt surfaces

- Well-sprayed vs over-sprayed or runny finishes

- Properly mixed vs poorly mixed paints

Demonstrate how moisture meters are used, and explain how minor differences (e.g., blade sharpness) can lead to visible process faults.

Encourage learners to create a fault checklist for use during production inspections.

Activity Suggestion: Process Fault Identification Exercise

- Arrange a variety of defective and acceptable samples (e.g., panels, frames, sprayed test pieces)

- Give learners a blank inspection sheet

- Ask them to:

  - Identify any visible or tactile faults

  - Suggest the likely cause (process or setup issue)

  - Recommend corrective action (rework, machine adjustment, disposal)

Discuss findings in groups to compare approaches to fault identification.

Case Study: Over-Sprayed Frames Causing Rework

During finishing, a learner noticed that spray guns were over-spraying adjoining surfaces, leading to excessive sanding and refinishing. Investigation revealed that air pressure was set too high, causing uncontrolled paint mist.

Facilitator Prompts:

- What earlier inspection step could have detected or prevented the over-spraying?

- Why is it important to adjust machine settings for each job or material?

- What are the cost and time consequences of extensive re-spraying?

Critical Thinking Questions

- What are the early signs of a blade becoming too blunt for clean machining?

- How can a moisture meter reading affect the decision to proceed with machining timber?

- Why does incorrect viscosity in paint lead to poor finish quality?

- How can operator skill reduce risks of over-spraying or running paint?

- What procedures should be in place to ensure paints are mixed and applied correctly according to manufacturer specifications?

### Facilitator Notes: PA0905 – Identify Machine Faults

Facilitator Purpose

This session trains learners to identify faults related to machine setup, maintenance, and performance that may affect the quality of machining and finishing processes. Early detection of machine faults is critical to prevent component defects, reduce downtime, protect operator safety, and ensure consistent product standards.

Learners must demonstrate awareness of machine conditions and understand how different faults impact the finished product, enabling them to take timely corrective action or escalate issues to supervisors or maintenance teams.

Key Concepts to Cover

1. Common Machine Faults in Machining and Finishing

| Fault | Symptoms | Impact |
| --- | --- | --- |
| Blunt blade | Tear-out, rough surfaces, burning marks, high feed resistance | Poor surface quality, increased risk of material rejection |
| Wrong sanding grit | Over-sanding, visible scratches, insufficient material removal | Rough finishes, uneven surfaces, reduced finish quality |
| Incorrect spray nozzle | Paint running, uneven spray pattern, excessive overspray | Poor paint adhesion, wasted material, aesthetic defects |
| Pressure too high or too low | Uneven spraying, running paint, inefficient dust extraction | Poor finishing quality, dangerous dust accumulation |
| Poor balance of air extraction | Excessive dust in the air, poor visibility, machine clogging | Fire hazard, health hazard, machinery damage |

2. Signs of Machine Faults Learners Must Recognise

- Unusual vibration or noise from machines

- Increased resistance or uneven feeding when cutting or sanding

- Visual signs: scorch marks, rough cuts, inconsistent sanding patterns

- Irregularities in spray patterns (spitting, pulsing, running)

- Excessive dust buildup around sanding or spraying stations

3. Immediate Actions to Take Upon Fault Detection

- Stop the machine if the fault compromises safety or product quality

- Inspect the blade, sanding belt, nozzle, or settings before proceeding

- Report the issue clearly to the supervisor or maintenance technician

- Tag the machine as out of service if necessary

- Record the fault in a maintenance or fault log for traceability

Facilitator Demonstration Tip

Set up:

- A sample of wood with burn marks from a blunt blade

- A sanding belt with incorrect grit marks (e.g., scratches visible under light)

- A spray gun set incorrectly (if available, or use diagrams/photos)

Demonstrate:

- How a sharp blade cut differs from a blunt blade cut

- How sanding marks differ depending on grit coarseness

- The effect of nozzle selection and air pressure adjustment on a spray pattern

Invite learners to "diagnose" the faults based on visible signs and machine sounds.

Activity Suggestion: Machine Fault Simulation

Set up three stations:

- Cutting station with a slightly dull blade

- Sanding station with incorrect grit belt

- Spraying station (or mock setup) with an oversized nozzle or wrong pressure

Ask learners to:

- Operate or observe each station

- Identify the visible or tactile signs of a fault

- Suggest corrective action or maintenance needed

- Record findings in a basic troubleshooting report

Case Study: Poor Dust Extraction Causes Fire Risk

At a sanding booth, a malfunctioning extraction system led to excessive dust accumulation. Although sanding quality appeared acceptable initially, airborne fine dust created a hazardous environment. A spark later caused a minor fire outbreak, halting production.

Facilitator Prompts:

- What early warning signs could have indicated an extraction problem?

- How might regular checks of air extraction systems prevent such incidents?

- What daily maintenance tasks could learners perform to support system efficiency?

Critical Thinking Questions

- What are the first signs that a machine blade is becoming too dull for quality cutting?

- Why is it dangerous to continue using a machine with poor dust extraction?

- How does sanding with the wrong grit affect subsequent finishing processes like painting or varnishing?

- What are the visual signs that indicate a spray gun nozzle is clogged or inappropriate for the material?

- Why is it important to document machine faults, even minor ones, in a production environment?

## Applied Knowledge Introduction – PM-01-PS09

Introduction to Applied Knowledge

The applied knowledge associated with this module provides learners with the essential theoretical understanding required to inspect machined components, diagnose process and machine faults, and categorise finishing materials appropriately.

By mastering this knowledge, learners will be able to:

- Differentiate between component, process, and machine faults

- Understand the causes and consequences of defects in the production cycle

- Classify paints and coatings used in the finishing process and apply related health and safety considerations

- Support continuous quality improvement by ensuring only compliant parts progress through the production workflow

### AK0901 – Different Types of Faults

Learners are required to develop the ability to identify faults at various stages of furniture manufacturing, specifically:

- Component faults: such as incorrect dimensions, lack of squareness, knots causing rejects, surface scratches, and poor surface smoothness

- Process faults: including blade marks, burn marks, moisture-related issues in timber, and errors in finishing (such as over-spraying, incorrect paint mixing, or poor viscosity control)

- Machine faults: such as blunt blades, incorrect sanding grit usage, faulty spray nozzles, improper air pressure regulation, and insufficient dust extraction

Recognising and diagnosing these faults early supports better decision-making regarding rectification, rejection, or reworking of components.

### AK0902 – Paints and Their Characteristics

Learners are also expected to understand the fundamental types of paints used in furniture finishing, including:

- Spirit-based paints: such as solvent-based stains and lacquers, characterised by their quick drying times, strong odour, and requirement for ventilation and flame precautions

- Oil-based paints: characterised by longer drying times, deeper penetration into wood surfaces, and the need for specific curing conditions

Learners must be able to identify the type of finishing material based on labels, application instructions, or cleaning methods (e.g., use of mineral turpentine indicating a spirit-based product) and apply appropriate safety practices, such as PPE usage, proper ventilation, and safe storage of flammable materials.

Understanding the characteristics of paints also enables learners to identify faults such as running, poor adhesion, cracking, or discolouration, which may be caused by incorrect material choice, improper mixing, or application errors.

### Applied Knowledge Learning Content – AK0901: Different Types of Faults

Purpose of Learning Content

This learning content develops the learner’s ability to recognise, categorise, and understand faults that can occur during the machining, assembly, and finishing stages of furniture production. Early and accurate identification of faults ensures consistent quality, minimises wastage, and supports efficient rectification or rejection processes.

Key Learning Areas

1. Categories of Faults

| Fault Type | Definition | Examples |
| --- | --- | --- |
| Component faults | Defects in the machined workpiece itself, regardless of the process or machine used | Out-of-square edges, incorrect sizing, visible knots, scratches |
| Process faults | Defects caused by how the workpiece was machined or finished | Blade marks, burn marks, poor sanding, paint over-spraying |
| Machine faults | Defects caused by equipment malfunction or poor machine setup | Blunt blades, worn sanding belts, clogged spray nozzles |

2. Common Component Faults

| Fault | Identification Method | Possible Causes |
| --- | --- | --- |
| Incorrect size | Measure length, width, thickness | Inaccurate cutting, poor setup |
| Out of square | Check with set square | Fence misalignment, operator error |
| Knots causing rejects | Visual check; test knot tightness | Natural wood defects, poor material selection |
| Surface roughness | Visual and tactile inspection | Incomplete sanding, poor planing |
| Scratches and dents | Visual inspection under bright light | Poor handling, machine or material defects |

3. Common Process Faults

| Fault | Identification Method | Possible Causes |
| --- | --- | --- |
| Blade marks | Visual inspection of cut faces | Blunt blade, feed speed inconsistency |
| Burn marks | Visual discolouration and rough texture | Blunt blade, friction from slow feed rate |
| Over-spraying | Overshoot of paint beyond targeted surface | Incorrect spraying technique, wrong pressure settings |
| Running paint | Vertical drips or heavy streaks in finish | Incorrect viscosity, over-application |
| Poor adhesion or cracking | Finish peeling or cracking during curing | Surface contamination, wrong base preparation |

4. Common Machine Faults

| Fault | Identification Method | Possible Causes |
| --- | --- | --- |
| Blunt blade | Increased feed resistance; rough or burnt cuts | Blade wear through normal use |
| Wrong sanding grit | Visible deep scratches or polishing instead of smoothing | Using too coarse or too fine a sanding belt |
| Faulty nozzle or high pressure | Uneven paint application or overspray | Clogged or damaged nozzle; wrong gun settings |
| Poor dust extraction | Accumulation of dust on surfaces or in the air | Blocked ducts, inadequate suction |

5. Examples of Fault Impact

- Out of square components cause visible gaps in frame assemblies, leading to instability

- Rough surfaces prevent good paint adhesion and can result in an uneven finish

- Burn marks weaken material around joints, affecting long-term durability

- Paint faults like running or over-spraying diminish aesthetic appeal and require expensive rework

Facilitator Demonstration Tip

Prepare samples:

- Correctly machined component

- A component with blade marks, burn marks, and roughness

- Two painted panels: one correctly sprayed, one over-sprayed with runs

Allow learners to inspect by sight and touch, identify faults, and categorise the fault type (component, process, or machine).

Case Study: Failure to Detect Process Fault

A batch of table legs was approved without detecting fine blade marks from a dull saw. After staining, the blade marks became highly visible, requiring the entire batch to be sanded and re-sprayed at significant cost.

Facilitator Prompts:

- What type of fault was this (component, process, or machine)?

- How could earlier detection have saved time and cost?

- What inspection tools would have revealed the problem before staining?

Critical Thinking Questions

- What inspection method would best reveal scratches before painting a component?

- Why is it important to distinguish whether a fault is caused by material, process, or machinery?

- What is the risk of ignoring small blade marks during early inspection stages?

- How does a blunt blade indirectly lead to poor assembly fit?

- What workplace systems can support early identification and correction of faults?

### Applied Knowledge Learning Content – AK0902: Paints and Their Characteristics

Purpose of Learning Content

This learning content ensures that learners understand the different types of paints used in furniture manufacturing, their chemical and performance characteristics, and the safety and quality considerations that must be applied when selecting, handling, and applying finishing products.

By mastering this knowledge, learners will be able to:

- Correctly categorise paints as spirit- or oil-based

- Apply safe handling procedures

- Understand how different paint characteristics affect surface preparation, application, and curing

Key Learning Areas

1. Main Categories of Paints in Furniture Finishing

| Paint Type | Description | Key Characteristics |
| --- | --- | --- |
| Spirit-based paints | Solvent-based paints and finishes (e.g., spirit stains, nitrocellulose lacquers) | Fast drying, strong odour, flammable, smooth high-gloss finish |
| Oil-based paints | Paints where oils (e.g., linseed, tung) are the binder | Slow drying, durable finish, deeper penetration into timber |

2. Identifying Paint Types

| Identification Method | Indicator |
| --- | --- |
| Cleaning instruction | “Clean with mineral turpentine” → Spirit-based product |
| Drying time | Fast drying (minutes to a few hours) → Spirit-based; slow drying → Oil-based |
| Odour | Sharp solvent smell → Spirit-based; mild or “natural” smell → Oil-based |
| Consistency and flow | Thinner and runnier → Spirit-based; thicker and heavier → Oil-based |
| Product label terminology | Words like "lacquer", "sealer", or "solvent" → Spirit-based |

🛈 It is essential to always read product labels and technical data sheets to confirm paint type and application instructions.

3. Practical Characteristics to Understand

| Characteristic | Spirit-Based Paint | Oil-Based Paint |
| --- | --- | --- |
| Drying time | Rapid (minutes to hours) | Slow (hours to days) |
| Surface preparation required | High – surface must be smooth and dust-free | High – surface must be dry and sanded |
| Risk factors | Highly flammable vapours, need excellent ventilation | Slow drying can attract dust, needs curing space |
| Application method | Spraying, brushing, wiping | Brushing, wiping, sometimes spraying |

4. Importance of Correct Paint Selection

- Matching the paint type to surface conditions and end-use requirements ensures finish durability

- Incorrect paint selection or mixing (e.g., oil over spirit or vice versa) can cause:

  - Peeling

  - Poor adhesion

  - Surface bubbling

  - Uneven colour or sheen

5. Health, Safety and Environmental Considerations

- Always work in well-ventilated areas

- Wear respirators/masks, gloves, and eye protection

- Store spirit-based products away from heat, sparks, and flames

- Dispose of rags, brushes, and waste responsibly to avoid fire risks

- Keep containers sealed when not in use to prevent evaporation and contamination

Facilitator Demonstration Tip

Provide real (or empty) containers labelled:

- Spirit-based lacquer

- Oil-based wood stain

Show:

- How spirit-based products evaporate quickly from an open container

- How oil-based finishes take longer to dry when spread thinly on wood

Use real examples of surfaces finished with each type and discuss differences in touch, gloss, and colour depth.

Activity Suggestion: Paint Identification and Safety Task

Set up samples of labelled paints (or mock labels) and safety equipment.

Ask learners to:

- Identify each product as spirit- or oil-based

- List three key characteristics of each product

- Explain the safety precautions required for handling each type

- Match each product to the correct application method (spray, brush, wipe)

Case Study: Incorrect Paint Use Causing Rework

A learner applied an oil-based wood stain over a lacquer sealer, resulting in poor adhesion, patchy colour, and peeling during curing. The entire batch of panels had to be stripped and refinished.

Facilitator Prompts:

- How could correct identification of the base product have prevented this?

- What label warnings or cleaning instructions should have been checked?

- How should the workshop improve paint verification procedures?

Critical Thinking Questions

- Why is it important to know whether a paint is spirit- or oil-based before starting finishing work?

- How can you verify the drying and curing times before beginning an application?

- What might happen if spirit-based and oil-based products are mixed incorrectly?

- Why must spirit-based paints be handled differently from oil-based paints regarding fire safety?

- How does the environment (temperature, humidity) influence the behaviour of different paints?

### INTEGRATED ASSESSMENT TASK – PM-01-PS09

Assessment Type: Practical and Knowledge Application

NQF Level: 2

Credits: 20

Assessment Context: Practical workshop inspection and evaluation exercise

Case Study: Inspection of Machined and Finished Timber Components

You are responsible for conducting final inspections of a batch of components produced for a series of coffee tables. During inspection, you find several parts with minor surface issues, one part with a critical size error, and a finishing station where different paints are used for different batches.

Your duties are to:

- Assess faults and decide whether parts must be rectified or rejected

- Safely handle and store approved components

- Correctly identify the type of finishing materials used and apply appropriate handling guidelines

Assessment Questions

Question 1
During visual and tactile inspection, you find the following:

- A surface scratch on a side panel

- A coffee table leg that is 3 mm undersized beyond tolerance

- Two top panels with slight over-spray from finishing

- How would you decide which components can be rectified and which must be rejected?

- What action would you take for each identified fault?

Question 2
After inspection, you must move and stack the approved components safely.

- Describe the correct method for handling and stacking timber panels and legs to prevent damage.

- What safety rules apply to stacking in a workshop environment?

Question 3
You observe two different cans of finishing material at the spray booth:

- One label states: "Clean equipment with mineral turpentine"

- Another label states: "Based on natural drying oils"

- Categorise each product as spirit- or oil-based.

- What health and safety precautions must be followed when using each type?

✅ MODEL ANSWERS

Answer 1

- Surface scratch: Minor defect; can be rectified by fine sanding and re-checking.

- Undersized leg: Critical dimension error; must be rejected as it falls outside tolerance.

- Over-sprayed top panels: Minor process fault; may be sanded lightly and re-coated if within acceptable visual standard.

Action:

- Record defects; mark parts clearly for rework or rejection; report critical faults to the supervisor.

Answer 2

- Stack panels flat with spacers between them to prevent surface damage.

- Stack legs vertically in racks or bundle securely to prevent toppling.

- Do not stack materials above shoulder height.

- Ensure walkways and emergency exits remain clear.

- Use proper lifting techniques or mechanical aids to move heavy panels.

Answer 3

- "Clean with mineral turpentine" → Spirit-based paint.

- "Based on natural drying oils" → Oil-based paint.

Health and Safety:

- For spirit-based: Use in a well-ventilated area, wear respirators, keep away from heat and flames, proper disposal of rags.

- For oil-based: Ensure good airflow during curing, wear gloves, prevent skin contact, proper storage to avoid spoilage.

🧾 MARKING MEMO

| Question | Criteria | Marks |
| --- | --- | --- |
| Q1 | Correctly identifies rectifiable faults and rejects; outlines appropriate action | 8 |
| Q2 | Describes safe handling and stacking principles with clear rationale | 5 |
| Q3 | Correctly categorises paint types and lists appropriate safety precautions | 7 |
|  | Total | 20 |

📊 ASSESSMENT RUBRIC

| Assessment Criteria | Outstanding (4) | Competent (3) | Developing (2) | Not Yet Competent (1) |
| --- | --- | --- | --- | --- |
| IAC0901 – Faults Rectified or Rejects Identified | Consistently identifies faults accurately; appropriate rectification or rejection | Identifies most faults correctly; actions mostly suitable | Some errors in fault detection or inappropriate actions | Faults misidentified or incorrect actions taken |
| IAC0902 – Materials Handled and Stacked Safely | Stacking method fully complies with safety and protection standards | Safe handling with minor procedural lapses | Awareness shown but inconsistencies or safety concerns present | Unsafe handling or stacking |
| IAC0903 – Finishing Materials Categorised | Correct classification with full safety protocols articulated | Correct classification with basic safety measures explained | Partial or uncertain classification; limited safety awareness | Incorrect classification; no safety awareness |

Facilitator Assessment Briefing

Internal Assessment Criteria:

- IAC0901: Faults are rectified or rejects are identified

- IAC0902: Materials are handled and stacked safely and securely

- IAC0903: Finishing materials such as paint are categorised as spirit- or oil-based

Purpose of the Assessment

This assessment measures the learner’s ability to:

- Conduct visual and tactile inspections of machined furniture components

- Apply specifications and tolerances to determine component compliance

- Rectify minor faults, identify rejects, and record findings appropriately

- Handle and stack approved components safely and systematically

- Correctly categorise types of finishing materials and apply related health and safety protocols

Assessment Context

The assessment is set in a practical workshop environment where the learner is required to inspect a batch of components for defects, ensure proper handling and storage, and categorise paint products according to their base. Learners will respond to a realistic case study scenario and be assessed on both practical decision-making and technical knowledge.

Facilitator Instructions

- Present the case study and ensure the learner fully understands the context

- Allow the learner to complete the tasks independently

- Observe the learner’s inspection methods, decision-making process, and attention to health and safety

- Use the model answers, memo, and rubric to mark responses objectively

- Provide feedback based on learner performance, offering remediation opportunities where needed

rectified

## PM-01-PS10: Operate Pneumatic Machines/Tools and Compressed Air According to Manufacturer Specifications

1. Introduction to the Practical Skill

This sub-task develops the learner’s ability to safely operate pneumatic machines and compressed air tools within a woodworking or furniture production environment. Pneumatic tools are widely used due to their speed, efficiency, and precision, but require careful handling and monitoring of air pressure, connections, and system maintenance to ensure safe and effective operation.

Learners are required to adjust air pressure gauges, connect fittings correctly, set machines according to job specifications, run pneumatic operations, and perform routine maintenance such as draining water and oil from the system. They must also identify and rectify hazards related to the use of compressed air.

2. Scope of Practical Skill

Given access to pneumatic machines and compressed air systems, the learner must be able to:

- PA1001 Follow established safety routines and procedures for compressed air equipment

- PA1002 Adjust air pressure to the specified gauge settings for the task

- PA1003 Identify and correctly connect air fittings and pipes to the appropriate tools or machines

- PA1004 Ensure that all machine settings are correct according to product and process specifications

- PA1005 Start and stop pneumatic equipment using standard operating procedures

- PA1006 Operate pneumatic machines to produce the desired components, cuts, fixings, or surface treatments

- PA1007 Conduct clean-up procedures, including draining water and oil, cleaning tools, and safely disconnecting equipment

3. Applied Knowledge

- AK1001: Understanding of different pressure bar requirements for various pneumatic machines and tools, including how to read and adjust a pressure gauge safely and accurately

Learners must understand that different machines (e.g., staple guns, sanders, clamping systems) require different pressure settings and that improper pressure can cause poor quality work, damage to equipment, or safety risks.

4. Internal Assessment Criteria

Learners will be assessed on their ability to:

- IAC1001: Adjust the pressure gauge accurately to the required operating pressure for the specific tool or task

- IAC1002: Drain water and oil from the compressed air system to maintain efficiency and avoid contamination

- IAC1003: Use compressed air and pneumatic machines strictly according to standard safety and operating procedures

- IAC1004: Identify common hazards associated with compressed air (e.g., hose whip, over-pressurisation, air injection injuries) and rectify these hazards according to best practice

### Facilitator Notes: PA1001 – Follow Safety Routines and Procedures

Facilitator Purpose

This session develops the learner’s ability to understand and apply safety routines and operating procedures when working with pneumatic machines and compressed air systems. Due to the high pressure involved, pneumatic systems present unique safety risks that must be carefully managed.

Learners must demonstrate awareness of potential hazards, consistent use of personal protective equipment (PPE), and the ability to follow correct startup, operation, and shutdown procedures in a pneumatic environment.

Key Concepts to Cover

1. Importance of Pneumatic Safety Routines

- Compressed air under pressure can cause serious injury if misused

- Improper connections or pressure settings can damage machines and materials

- Air leaks can lead to energy loss, tool failure, or hose whip injuries

- Routine safety checks protect both operator safety and production efficiency

2. Standard Pneumatic Safety Procedures

| Safety Procedure | Why It Is Critical |
| --- | --- |
| Inspect hoses, fittings, and tools before use | To identify damage, cracks, or leaks that could cause failure |
| Check that pressure settings match machine requirements | Prevents over-pressurisation or under-performance |
| Secure all connections firmly | Prevents hose whip and accidental disconnection |
| Wear appropriate PPE | Safety glasses, gloves, hearing protection for loud tools |
| Never use compressed air to clean skin or clothing | Risk of air embolism or injury |
| Always shut off and depressurise system before maintenance | Prevents unexpected activation |
| Drain water and oil regularly from system | Avoids corrosion and contamination of tools |
| Use tools only for their designed purpose | Misuse can lead to dangerous malfunctions |

3. Key PPE for Pneumatic Work

- Safety glasses or face shield – Protection from flying particles or hose whip

- Hearing protection – Particularly when operating pneumatic sanders, nailers, or grinders

- Gloves – Grip and hand protection, but loose gloves must be avoided with rotating tools

- Dust masks or respirators – If pneumatic tools are used for sanding or spraying operations

Facilitator Demonstration Tip

Set up a basic pneumatic system:

- A portable compressor

- A connected tool (e.g., pneumatic nailer or sander)

- Display examples of safe and unsafe hose setups (e.g., loose fittings)

Demonstrate:

- How to perform a visual inspection of hoses and connections

- How to adjust and read a pressure gauge

- Correct start-up and shutdown sequence

- How to identify an unsafe situation and shut down equipment immediately

Allow learners to practice conducting a "pre-start" safety inspection before tool use.

Activity Suggestion: Safety Inspection Simulation

Provide a series of equipment setups:

- Some correctly connected and safe

- Some with small faults (e.g., cracked hose, wrong pressure setting)

‘’

Learners must:

- Inspect the equipment

- Identify any faults or risks

- Suggest corrective actions

- Complete a basic pneumatic safety checklist for each station

Reward accuracy, thoroughness, and clear explanations during the exercise.

Case Study: Hose Whip Incident

During a production shift, a pneumatic hose disconnected from a sander due to a loose fitting. The pressurised hose flailed uncontrollably, narrowly missing a worker. Investigation showed that the fitting had not been checked before starting.

Facilitator Prompts:

- What safety routine was missed in this situation?

- How could this risk have been eliminated?

- What routine should be added to the daily equipment inspection checklist?

Critical Thinking Questions

- Why is it dangerous to exceed the recommended air pressure on a pneumatic tool?

- What are the risks of using compressed air to clean clothing or skin?

- Why must hoses and fittings be inspected every shift, even if they appeared fine previously?

- What should you do if you discover a damaged hose during your pre-use inspection?

- How does following safety routines contribute to both worker health and workshop productivity?

## Facilitator Notes: PA1002 – Adjust Pressure to the Required Gauge

Facilitator Purpose

This session teaches learners to correctly adjust air pressure settings for pneumatic machines and tools according to manufacturer specifications and job requirements. Adjusting the air pressure accurately is critical for tool performance, product quality, and safe operation.

Learners will practise reading pressure gauges, setting required pressure levels, and verifying that the pressure remains stable during operation.

Key Concepts to Cover

1. Importance of Correct Air Pressure

- Too low pressure:

  - Tool may not function correctly (e.g., nails not fully driven, sander underpowered)

  - Incomplete work leading to poor product quality

- Too high pressure:

  - Risk of tool damage

  - Component damage (e.g., over-penetrated nails, material breakage)

  - Increased hazard to operator safety (e.g., hose whip, tool recoil)

🛈 Each pneumatic tool has an optimal operating pressure range stated by the manufacturer (e.g., 5–8 bar or 70–115 psi).

2. Reading and Adjusting a Pressure Gauge

| Step | Action |
| --- | --- |
| Locate the pressure regulator | Typically on the compressor or in-line with the air supply |
| Read the gauge | Check that it displays in bar or psi (confirm units) |
| Turn the regulator knob | Clockwise to increase pressure, counter-clockwise to decrease pressure |
| Observe the gauge while adjusting | Adjust slowly to avoid overshooting |
| Set pressure to match tool specification | Confirm by observing stable gauge reading while tool is running |

3. Example Operating Pressures for Common Tools

| Tool | Typical Pressure Range |
| --- | --- |
| Pneumatic nail gun | 5.5–7 bar (80–100 psi) |
| Pneumatic sander | 6–7 bar (85–100 psi) |
| Pneumatic stapler | 4.5–6 bar (65–90 psi) |
| Pneumatic spray gun | 2–3 bar (30–45 psi) depending on material viscosity |

Facilitator Demonstration Tip

Prepare:

- A portable compressor with a visible gauge and regulator

- A connected pneumatic tool (e.g., a stapler or small sander)

Demonstrate:

- How to read the gauge

- How small adjustments of the regulator affect pressure

- The importance of making adjustments before tool activation

- Observing the "drop" in pressure when the tool first activates, and stabilising accordingly

Let each learner practise setting the pressure according to a given tool specification.

Activity Suggestion: Pressure Adjustment Practical Drill

Create workstations with compressors and gauges:

- Provide each learner with a set of operating pressures for different tools

Learners must:

- Set the compressor pressure to the correct value

- Confirm stable pressure under tool load

- Adjust if necessary

- Record the tool and final set pressure

Use a checklist to assess correct setting and process adherence.

Case Study: Tool Malfunction Due to Incorrect Pressure

A learner connected a pneumatic nailer to a compressor without adjusting the pressure. The pressure was too low (3 bar instead of the required 6 bar), causing nails to sit proud above the surface. The learner attempted to drive the nails manually, damaging several workpieces.

Facilitator Prompts:

- What step was missed before starting work?

- Why is "running pressure" different from static pressure in some systems?

- How could this mistake have been prevented?

Critical Thinking Questions

- Why must the tool manufacturer's pressure recommendation always be followed?

- What can happen if pressure settings are adjusted while the tool is already running?

- How do you confirm that pressure remains correct when the tool is operating, not just idle?

- What effect does air hose length and diameter have on working pressure?

- How could inaccurate gauge readings lead to production and safety risks?

## Facilitator Notes: PA1003 – Identify Correct Connections (Fittings for Pipes)

Facilitator Purpose

This session develops learners’ skills in recognising, selecting, and securing the correct fittings for connecting pneumatic tools and machines to compressed air supply systems. Correct connection ensures safe operation, prevents air leaks, and protects equipment and users from hazards like hose whip and pressure drops.

Learners will be able to match pipes and fittings, check compatibility, and properly install or replace connectors to maintain pneumatic system efficiency and safety.

Key Concepts to Cover

1. Importance of Correct Connections

- Ensures airtight sealing for stable air pressure delivery

- Prevents air leaks, reducing compressor load and energy consumption

- Minimises risk of hose disconnection during tool use

- Protects operator safety against sudden hose whip or tool failure

- Avoids damage to fittings, tools, and compressor components

2. Common Types of Pneumatic Fittings

| Fitting Type | Description and Use |
| --- | --- |
| Quick-connect coupling | Enables fast connection/disconnection without tools |
| Push-to-connect fitting | Hose is pushed into fitting for quick attachment (small tools) |
| Barbed fitting | Hose slides over barbed fitting and is secured with clamp |
| Threaded fitting | Male/female threads screwed together, often sealed with thread tape |
| Claw coupling (for high-pressure systems) | Heavy-duty connections, locked with safety clips |

3. Identifying the Right Fitting

| Check | What to Look For |
| --- | --- |
| Size compatibility | Ensure fitting size matches hose inner/outer diameter |
| Pressure rating | Confirm fitting rated for the system’s maximum working pressure |
| Material type | Metal (e.g., brass, stainless steel) preferred for durability |
| Connection type | Match male to female threads; ensure correct coupling type |
| Condition | Check for wear, cracks, corrosion, or deformation before fitting |

4. Key Connection Procedures

- Insert hose securely into push fitting or screw fitting tightly using hand tools if needed

- Ensure quick-connect couplings click firmly into place

- Use clamps over barbed fittings to secure hoses

- Use thread seal tape (PTFE) on threaded fittings to prevent air leaks

- Pull-test hoses lightly after connection to check security

- Avoid using damaged or ill-fitting connectors

Facilitator Demonstration Tip

Prepare a table with different fittings:

- Quick-connects, barbed fittings, push-fittings, threaded fittings

- Hoses of various diameters

- Sample tools with matching and mismatching connectors

Demonstrate:

- How to attach a quick-connect coupling properly

- How to inspect a fitting before use

- How to secure a hose to a barbed fitting with a clamp

- How to apply thread tape on threaded fittings without over-wrapping

Allow learners to practise identifying, selecting, and connecting fittings correctly.

Activity Suggestion: Fitting Identification and Assembly Task

Set up a fitting station:

- Provide hoses, fittings, clamps, and basic hand tools

Learners must:

- Select the correct fitting for a given hose and tool

- Attach fittings securely

- Test connections for leaks (using a small air supply if available)

- Complete a connection checklist before declaring setup safe

Case Study: Air Leak Caused by Incorrect Fitting Selection

A learner fitted a high-pressure tool using an undersized push-in fitting without clamps. Under pressure, the fitting failed, causing a sudden loss of pressure and halting production for two hours.

Facilitator Prompts:

- What fitting error occurred?

- How would correct fitting inspection have prevented this?

- What standard checks should be performed before commissioning pneumatic setups?

Critical Thinking Questions

- Why must fittings be matched both by size and pressure rating?

- What risks arise if a quick-connect fitting is not properly latched?

- How can regular fitting inspection support workshop safety?

- What tool or method helps ensure airtight seals on threaded connections?

- How does using damaged or worn fittings affect overall system efficiency and safety?

### Facilitator Notes: PA1004 – Ensure All Settings Are Correct According to Product Specifications

Facilitator Purpose

This session develops learners’ ability to set up pneumatic machines and tools correctly according to manufacturer specifications and production requirements. Ensuring correct settings is vital for achieving quality output, efficient operation, and operator safety.

Learners will practise interpreting job cards or manufacturer manuals to verify correct settings, adjusting machines accordingly, and confirming readiness before starting production runs.

Key Concepts to Cover

1. What “Correct Settings” Include

| Setting Type | Examples |
| --- | --- |
| Air pressure | Adjusting compressor or in-line regulator to tool specification |
| Tool-specific settings | Nail depth on nailers, spray pattern adjustment on spray guns |
| Material-specific settings | Adjusting air pressure or feed rates for softwood vs hardwood |
| Hose and connection security | Ensuring tight and compatible fittings |
| Startup and shutdown sequences | Confirming readiness and depressurisation steps |

2. Importance of Following Product Specifications

- Prevents over-driving or under-performing pneumatic tools

- Ensures consistent quality (e.g., consistent nail depth, even sanding, uniform spray coverage)

- Reduces wear and tear on tools and fittings

- Supports safe operation under the intended pressure and load conditions

- Complies with manufacturer warranties and maintenance schedules

🛈 Each machine or tool should have a manual or data plate indicating recommended settings.

3

. Examples of Settings for Pneumatic Tools

| Tool | Key Settings |
| --- | --- |
| Pneumatic nail gun | Air pressure, depth-of-drive adjustment |
| Pneumatic sander | Air pressure, speed setting (if variable) |
| Pneumatic spray gun | Air pressure, spray pattern adjustment, paint viscosity |
| Pneumatic clamps | Air pressure matched to holding force requirements |

Facilitator Demonstration Tip

Use a real pneumatic tool (e.g., a nailer or spray gun):

- Show how to locate and read the manufacturer’s recommended settings

- Demonstrate adjusting air pressure at the regulator

- If applicable, show tool-specific adjustments (depth gauge, spray fan width)

Have learners practise setting up different tools for different tasks based on given job cards.

Activity Suggestion: Setup Accuracy Challenge

Create job cards with different product requirements:

- E.g., "Nail depth flush with surface, 6 bar pressure"

- "Spray wide fan pattern, 2.5 bar pressure for lacquer finish"

Learners must:

- Set the tool and air pressure correctly

- Demonstrate or simulate a short operation

- Verify with facilitator inspection before beginning simulated production

Award points for accuracy, readiness, and safety check compliance.

Case Study: Incorrect Settings Cause Production Defects

A learner adjusted a spray gun to maximum pressure without adjusting the spray pattern. As a result, paint overspray covered adjacent components, requiring extensive rework and cleaning.

Facilitator Prompts:

- What specification check was missed in this situation?

- How could adjusting both pressure and pattern have avoided the fault?

- Why should a test sample always be used before full production?

Critical Thinking Questions

- Why is it important to set both air pressure and tool-specific controls before starting work?

- What problems can occur if a tool operates at a higher pressure than recommended?

- How can you verify that your setup matches product specifications before production starts?

- What role does a test run play in ensuring correct settings?

- Why must setup adjustments be recorded or verified in quality assurance systems?

### Facilitator Notes: PA1005 – Start and Stop the Machine Using Standard Operating Procedures

Facilitator Purpose

This session trains learners to correctly start and stop pneumatic machines and tools according to standard operating procedures (SOPs). Correct start-up and shutdown are essential for ensuring operator safety, protecting machine integrity, and maintaining production quality.

Learners must demonstrate step-by-step procedures, verify equipment readiness before starting, and apply proper shutdown techniques to depressurise systems, prevent accidents, and extend equipment lifespan.

Key Concepts to Cover

1. Importance of Following Start and Stop Procedures

- Reduces risk of sudden tool movement or activation

- Ensures machines are operating under safe conditions

- Prevents pressure surges that can damage hoses, fittings, or components

- Protects against residual air pressure injuries during maintenance

- Supports workshop discipline and prevents downtime due to errors

2. Standard Start-Up Procedure for Pneumatic Equipment

| Step | Action |
| --- | --- |
| 1. Inspect the machine, hoses, and connections | Look for damage, loose fittings, or leaks |
| 2. Verify air pressure is set correctly | Adjust regulator if necessary, match tool specification |
| 3. Secure tool and work area | Ensure tool is unloaded (no nails, pins) and area is clear |
| 4. Connect tool to air supply | Use correct quick-connect fitting or approved connector |
| 5. Open air supply valve slowly | Pressurise the system gradually to operating pressure |
| 6. Test tool briefly at low speed or without load | Check for normal function, leaks, abnormal sounds |

3. Standard Stopping and Shutdown Procedure

| Step | Action |
| --- | --- |
| 1. Stop tool operation completely | Release trigger or control lever |
| 2. Shut off air supply at main valve or compressor | Isolate pressure from the system |
| 3. Disconnect tool safely | Depressurise hose first if system allows |
| 4. Drain any remaining air from tool | Prevent pressure buildup in storage |
| 5. Inspect and clean tool if necessary | Remove debris, moisture, or leftover materials |
| 6. Store tool and hoses properly | Avoid bending hoses sharply; hang or coil neatly |

Facilitator Demonstration Tip

Prepare a pneumatic station:

- Compressor or air source

- Tool such as a nailer or sander

Demonstrate:

- Pre-start inspections

- Connecting the tool properly

- Performing a controlled start-up

- Normal operation observation

- Correct shutdown and depressurisation

- Disconnecting and storing equipment

Allow learners to practise full start-up and shutdown cycles.

Activity Suggestion: Start-Up and Shutdown Checklist Drill

Give each learner a printed checklist:

- Pre-start inspection points

- Start-up sequence

- Shutdown sequence

Learners must:

- Perform all steps in order

- Tick off completed steps

- Report any faults found during inspection

Evaluate precision, sequence adherence, and safety awareness.

Case Study: System Damage Due to Incorrect Shutdown

A learner disconnected a pneumatic tool before shutting off the main air valve. The compressed air caused the hose to whip violently, hitting another worker and causing minor injury. An investigation revealed that proper shutdown procedures had not been followed.

Facilitator Prompts:

- What critical shutdown step was missed?

- How could a simple routine have prevented the incident?

- Why should shutdown and depressurisation be non-negotiable in the workshop?

Critical Thinking Questions

- What is the risk of opening the air supply valve too quickly during start-up?

- Why must the tool be unloaded or disengaged before connecting to compressed air?

- What hazards arise if residual air remains trapped in disconnected hoses?

- Why is gradual pressurisation important during start-up?

- How can documenting start-up and shutdown procedures improve workshop safety culture?

### Facilitator Notes: PA1006 – Run the Machine to Produce the Desired Components or Effects

Facilitator Purpose

This session builds learners' capability to operate pneumatic machines and tools efficiently and accurately to produce components or surface effects that meet product specifications. It focuses on controlled operation, monitoring machine performance, and adjusting technique to maintain quality standards throughout production runs.

Learners must understand that machine operation requires continuous attention, observation of results, and the ability to make small adjustments to maintain consistency, accuracy, and safety.

Key Concepts to Cover

1. Objectives During Pneumatic Machine Operation

- Produce components that meet size, shape, and surface finish specifications

- Maintain steady and consistent machine/tool operation

- Identify and correct minor operation faults immediately

- Protect workpieces from damage during pneumatic tool use

- Ensure operator and equipment safety at all times

2. Best Practice Guidelines for Running Pneumatic Machines

| Best Practice | Why It Matters |
| --- | --- |
| Maintain steady feed speed | Avoids inconsistent machining marks or over-driving fasteners |
| Monitor tool response during operation | Detects early signs of air starvation, leaks, or tool malfunction |
| Keep hands, hoses, and cables clear | Prevents entanglement or unintended tool movement |
| Follow the machine’s natural rhythm | Do not force the machine; allow compressed air to drive the action |
| Make sample runs when settings are adjusted | Ensures quality before starting full production |

3. Examples of Pneumatic Machines/Tools in Operation

| Machine/Tool | Typical Component or Effect Produced |
| --- | --- |
| Pneumatic nail gun | Consistent fastening of cabinet frames or panels |
| Pneumatic sander | Smooth sanding of timber or MDF panels |
| Pneumatic spray gun | Even application of stain, sealer, or lacquer |
| Pneumatic clamp system | Secure, uniform clamping pressure during gluing |

Facilitator Demonstration Tip

Prepare:

- A pneumatic nail gun or sander

- A sample board or frame for demonstration

Demonstrate:

- Steady handling of the tool

- Monitoring operation (e.g., listening for compressor cycle, feel of tool action)

- Stopping operation immediately if abnormalities occur (e.g., weak nail driving, inconsistent sanding)

Allow learners to perform controlled operations using sample materials under supervision.

Activity Suggestion: Production Accuracy Simulation

Set up different workstations:

- Nailing frames

- Sanding sample panels

- Spraying mock finishes (if facilities allow)

Learners must:

- Operate the machine to complete a simple production task

- Check the quality of their output (e.g., consistent nail depth, even sanding, smooth spray coverage)

- Adjust technique if needed based on immediate feedback

Facilitators observe and record operational consistency, safety adherence, and product quality.

Case Study: Poor Surface Finish from Incorrect Machine Operation

A learner using a pneumatic sander applied uneven pressure and moved too slowly across an MDF panel. As a result, the surface became gouged in areas, requiring heavy re-sanding and material loss.

Facilitator Prompts:

- What operational error caused the surface damage?

- How could a steady movement technique have prevented this?

- Why must tool weight and movement, not force, guide pneumatic sanding?

Critical Thinking Questions

- Why is it important to monitor both the machine’s action and the quality of the workpiece while operating?

- What signs during operation indicate that immediate shutdown or adjustment is needed?

- Why should operations begin with a test piece before proceeding to production components?

- How can consistent machine operation improve production efficiency and reduce waste?

- What role does operator feedback (hearing, touch, visual inspection) play during pneumatic tool use?

### Facilitator Notes: PA1007 – Conduct Clean-Up Procedures as Required

Facilitator Purpose

This session trains learners to perform essential clean-up and maintenance procedures after using pneumatic machines and compressed air systems. Proper clean-up ensures safe workshop conditions, extends equipment lifespan, prevents contamination of materials, and prepares the equipment for the next use.

Learners must develop habits of responsibility, attention to detail, and compliance with organisational standards in maintaining both machines and the work environment.

Key Concepts to Cover

1. Why Clean-Up Procedures Are Essential

- Removes moisture, oil, and debris that can damage equipment

- Prevents slipping hazards and air quality issues from dust or residue

- Ensures compressed air systems remain efficient (free of water and oil buildup)

- Keeps tools ready for next operation without costly downtime

- Supports workshop cleanliness and safety culture

2. Typical Clean-Up Tasks for Pneumatic Systems

| Task | Action |
| --- | --- |
| Shut down and depressurise system | Release air pressure after turning off air supply |
| Drain water and oil from air tanks | Open drain valves carefully; ensure no moisture buildup |
| Clean tool surfaces and hoses | Wipe down dust, grease, or adhesive residue |
| Coil hoses properly | Prevent kinks and tripping hazards; hang hoses if possible |
| Inspect fittings and connections | Check for wear, cracks, and leaks after use |
| Store tools and accessories correctly | Place in designated racks, shelves, or containers |
| Dispose of waste properly | Follow workshop protocols for rags, dust, offcuts, and fluids |

3. Draining Water and Oil from the System

- Moisture naturally condenses inside compressors and air tanks

- Failure to drain can lead to:

  - Corrosion inside tanks and pipes

  - Poor air quality (moisture in paint or pneumatic actuators)

  - Reduced system efficiency and increased maintenance costs

🛈 Many systems have automatic drains, but manual draining is often necessary at least daily.

Facilitator Demonstration Tip

Prepare a compressor unit:

- Demonstrate safe depressurisation after use

- Show how to locate and operate the water/oil drain valve

- Wipe down a pneumatic tool after mock use

- Properly coil a hose and store it safely

Let learners each practise the full clean-up cycle under supervision.

Activity Suggestion: Clean-Up Drill

Set up an end-of-task scenario:

- Assume a small production run has been completed

Learners must:

- Shut down the pneumatic system correctly

- Drain water and oil from the compressor tank

- Wipe down tools

- Coil hoses and store equipment safely

- Dispose of any waste properly

Provide a checklist and time learners on their clean-up efficiency and completeness.

Case Study: Compressor Damage Due to Missed Drainage

A team neglected to drain water from the air receiver tank for several weeks. Eventually, corrosion weakened the tank structure, causing a costly compressor failure and workshop downtime for safety inspections.

Facilitator Prompts:

- What daily or weekly maintenance task could have prevented this incident?

- How does moisture in compressed air affect both tools and finished products?

- Why is workshop discipline around clean-up just as important as production performance?

Critical Thinking Questions

- Why must a pneumatic system be fully depressurised before draining water or oil?

- What are the risks of leaving hoses lying loosely around the workshop after tool use?

- How does proper tool cleaning and storage extend the lifespan of pneumatic equipment?

- What are the consequences of neglecting compressor maintenance for workshop operations?

- How can clean-up procedures be built into daily routines to improve overall workshop productivity?

Would you like me to now continue with the Applied Knowledge Introduction for AK1001: Different Pressure Bar Requirements, Adjusting Pressure Gauge? 🌟